Supplementary information

Figure S1. Schematic energy level diagram of the band alignment at p-Si/MoS2 interface in terms of vacuum level and normal hydrogen electrode level in electrolyte of pH = 0.3. The p-Si doping level is ~1.6×1015cm-3.

Figure S2. (a) Nyquist plot of 700–ALD-cycles and 300-ALD-cycles on p-Si photocathode under 1sun illumination at 0 bias. (b) Equivalent circuit corresponding to the EIS measurement. Rbulk is bulk resistance of the silicon, Qjc is constant phase element (CPE) of p-Si/MoS2 junction along with junction resistance Rjc, CPE of MoS2/electrolyte interface is denoted as QMoS2 and the resistance of RMos2.

Table S1. Measured charge transfer resistances.

| Condition | Rbulk (Ωcm2) Back contact/p-Si | Rjc (Ωcm2) p-Si/SiOx/MoS2 | RMoS2 (Ωcm2) MoS2/electrolyte |
| --- | --- | --- | --- |
| Dark (500) | 5.94 | 702.5 | 9517 |
| 600 | 5.514 | 77.98 | 157.4 |
| 500 | 4.974 | 27.38 | 22.38 |
| 300 | 4.642 | 22.26 | 16.95 |
| 100 | 4.108 | 83.11 | 77.1 |

List of symbols with values and Units

Na         Acceptor density 	1.6 x1015cm-3

Nd        Donor density                                	1019 cm-3

ni_Si       Intrinsic carrier density of p-silicon           	1010 cm-3

ni_MoS2   	Intrinsic carrier density of MoS2               	1013 cm-3

n0	Electron concentration in p-Si at dark equilibrium	66,000 cm-3

p0	Hole concentration in n-MoS2 at dark equilibrium	1013 cm-3

ns0	Surface electron concentration across the	cm-3

electrode/electrolyte interface at light

ns	Surface electron concentration across the 	cm-3

Electrode/electrolyte interface at dark equilibrium

W	Depletion width	cm

χp	Electron negativity of p-Si	eV

χn	Electron negativity of MoS2	eV

xp	Interface to p-Si depletion width	cm

xn	Interface to n-MoS2 depletion width	cm

Ln       	Minority carrier diffusion length in p-Si        	cm

Lp      	Minority carrier diffusion length in MoS2       	cm

Nc      	Density of states in the conduction band       	cm-3

Nv      	Density of states in the valence band          	cm-3

k       	Boltzmann’s constant                        	1.38×10-23JK-1

q      	Charge of an electron                       	1.6×10-19C

εr	Relative permittivity	Fm-1

ε0	Vacuum permittivity	Fm-1

Vph   	Photovoltage                                 	V

Von   	On-Set voltage                                 	V

Vbi 	Built-in potential                               	V

Vfb    	Flatband potential 	V

VA	Applied voltage	V

V0	The maximum restriction of photovoltage	V

Vo	band bending of silicon	V

ϕB	Barrier height	eV

ϕw	Work function 	eV

Jph	Saturated photocurrent density	mA·cm-2

Jsc	Photocurrent density at 0 V vs RHE	mA·cm-2

T      	Temperature                                  	T

C        	Capacitance	Fcm-2

Rs 	Series resistance	Ωcm2

Fp	Quasi-Fermi level in p-Si   	eV

Fn	Quasi-Fermi level in n-MoS2	eV

gop	Optical generation rate	cm-3s-1