Supplementary Information

Supramolecular Organogels Based on N-Benzyl, N’-Acylbispidinols

Alexey V. Medved'ko,1 Alexander I. Dalinger,1 Vyacheslav N. Nuriev,1 Vera S. Semashko,1 Andrei V. Filatov,2 Alexander A. Ezhov,3,4 Andrey V. Churakov,5 Judith A. K. Howard,6 Andrey A. Shiryaev,7,8 Alexander E. Baranchikov,6 Vladimir K. Ivanov,1,5 Sergey Z. Vatsadze1*

1	Faculty of Chemistry, Lomonosov Moscow State University, 119991 Moscow, Russian Federation; szv@org.chem.msu.ru

2	N. D. Zelinsky Institute of Organic Chemistry, Russian Academy of Sciences, 119991 Moscow, Russian Federation

3	Faculty of Physics, Lomonosov Moscow State University, 119991 Moscow, Russian Federation

4	A.V.Topchiev Institute of Petrochemical Synthesis, Russian Academy of Sciences, 119991 Moscow, Russian Federation

5	N. S. Kurnakov Institute of General and Inorganic Chemistry, Russian Academy of Sciences, 119991 Moscow, Russian Federation

6	Department of Chemistry, University of Durham, Durham DH1 3LE, U.K

7	A. N. Frumkin Institute of Physical Chemistry and Electrochemistry, Russian Academy of Sciences, 119071 Moscow, Russian Federation

8	Institute of geology of ore deposits, petrography, mineralogy and geochemistry, Russian Academy of Sciences, 119017 Moscow, Russian Federation

*	Correspondence: szv@org.chem.msu.ru ; Tel.: +7-903-748-7892

Preparation of unsymmetrical bispidines				pp. 2-6

Fig. S1-S2								p. 7

Fig. S3-S4								p. 8

Fig. S5-S6								p. 9

Fig. S7								p. 10

Tabl. S1								p. 11

Fig. S8								p. 12

Tabl. S2								p. 12

Fig. S9								p. 13

Fig. S10-S12								p. 15

Fig. S13-S15								p. 16

Fig. S16-S17								p. 17

Fig. S18-S19								p. 18

Fig. S20-S22								p. 19

Fig. S23-S25								p. 20

Preparation of unsymmetrical bispidines. General method.

To a suspension of bispidine 3 in dry benzene was added a solution of acyl halide (1 eq) in dry benzene. Then the mixture was refluxed under vigorous stirring for 3.5 hours. To obtain the product as the hydrochloride, the resulting gelatinous mass (precipitate or colloidal solution) was centrifuged for 10-15 minutes (6000 rpm) or filtered on a Schott filter (por.40) and then was dried. The free base was isolated from the aqueous solution by treatment with sodium bicarbonate (3 eq.).

Anti-1,5-dimethyl-3-benzoyl-7-benzyl-3,7-diazabicyclo[3.3.1]nonane-9-ol (4aa).

140 mg (0.54 mmol) of bispidine 3a and 75.6 mg (0.54 mmol) of benzoyl chloride in 10 ml of dry benzene give colloidal solution, from which 0.134 g of the free base was isolated. Yield 68%.

NMR 1H (DMSO-d6, δ/ ppm, J/Hz): 0.65 (s, 3H, CH3); 0.79 (s, 3H, CH3); 2.13 (d, 1H, H6e/8e/6a/8a, J = 10.2 Hz); 2.24-2.32 (m, 2H, H6e/8e/6a/8a); 2.37 (d, 1Н, H6e/8e/6a/8a, J = 11.3 Hz); 2.65 (d, 1Н, Н4а, J = 12,5 Hz); 3.04 (d, 1Н, Н2а, J = 12.5 Hz); 3.13-3.18 (m, 2Н, СН2Ph, H9); 3.42 (d, 1Н, Н2е, J = 12.9 Hz); 3.54 (d, 1Н, СН2Ph, J = 13.3 Hz); 4.47 (d, 1Н, Н4е, J = 13.2 Hz); 4,95 (d, 1Н, ОН, J = 4.7 Hz), 7.21-7.39 (m, 10Н, Н(Ar)).

NMR 13С (characteristic signals) (DMSO-d6, δ/ ppm, J/Hz): 21.5 (s, CH3); 21.8 (s, СН3); 35.17 (br. s, С1, С5); 52.2 (s, C2); 57.3 (s, C4); 57.8 (s, C6); 58.1 (s, С8); 63.4 (s, СН2Ph); 75.5 (s, С9); 126.2 (s, Ar), 128.3 (s, Ar), 129.0 (s, Ar), 130.16 (s, Ar), 130.45 (s, Ar), 130,56 (s, Ar), 133.15 (s, Ar); 168,5 (s, C=O).

Found (%): С, 75.80; H, 7.95; N, 7.46. Calculated for C23H28N2O2 (%): C, 75.79; H, 7.74; N, 7.69.

Anti-1,5-dimethyl-3-benzoyl-7-(4-fluorobenzyl)-3,7-diazabicyclo[3.3.1]nonane-9-ol (4ca)

70 mg (0.25 mmol) of bispidine 3с and 35.4 mg (0.25 mmol) of benzoyl chloride in 5 ml of dry benzene give colloidal solution, from which 0.082 g of the free base was isolated. Yield 85%.

NMR 1H (DMSO-d6, δ/ ppm, J/Hz): 0.65 (s, 3H, CH3), 0.79 (s, 3H, CH3); 2.13 (d, 1H, H6e/8e/6a/8a, J = 10.2 Hz); 2.24-2.32 (m, 3H, H6e/8e/6a/8a); 2.65 (d, 1Н, Н4а, J = 12.9 Hz); 3.05 (d, 1Н, Н2а, J = 12.9 Hz); 3.13-3.17 (m, 2Н, СН2Ph, H9); 3.42 (d, 1Н, Н2е, J = 13.3 Hz); 3.52 (d, 1Н, СН2Ph, J = 12.9 Hz); 4.48 (d, 1Н, Н4е, J = 13.1 Hz); 4,95 (d, 1Н, ОН, J = 4.5 Hz); 7.08 (tr, 2Н, СН(3,5) (С6Н4F) J = 8,4 Hz); 7.29-7.41 (m, 6Н, Н(Ar)).

NMR 13С (characteristic signals) (DMSO-d6, δ/ ppm, J/Hz): 21.4, 21.8 (both s, 2СН3); 36.1, 36.6 (both s, С1, С5); 52.1, 57.1, 57.8, 58.1 (all s, С2, С4, С6, С8); 62.5 (s, СН2Ph); 75.95 (s, С9); 127, 128.7, 129, 132.3, 130.85, 130.93, 134.9, 137.74 (all s, Ar); 168,5 (s, C=O).

Found (%):С, 72.57; H, 7.09; N, 7.12. Calculated for C23H27FN2O2 (%):C, 72.23; H, 7.12; N, 7.32.

Anti-1,5-dimethyl-3-benzoyl-7-(4-chlorobenzyl)-3,7-diazabicyclo[3.3.1]nonane-9-ol (4ba)

70 mg (0.24 mmol) of bispidine 3b and 33.4 mg (0.24 mmol) of benzoyl chloride in 5 ml of dry benzene give colloidal solution, from which 0.084 g of the free base was isolated. Yield 88%.

NMR 1H (DMSO-d6, δ/ ppm, J/Hz): 0.65, 0.79 (both s, 6H, 2CH3); 2.13 (d, 1H, H6e/8e/6a/8a, J = 10.8 Hz); 2.23-2.36 (m, 3H, H6e/8e/6a/8a); 2.65 (d, 1Н, Н4а, J = 12.5 Hz); 3.05 (d, 1Н, Н2а, J = 13.9 Hz); 3.13-3.17 (m, 2Н, СН2Ph, H9); 3.44 (d, 1Н, Н2е, J = 14.0 Hz); 3.53 (d, 1Н, СН2Ph, J = 13.9 Hz); 4.49 (d, 1Н, Н4е, J = 12.9 Hz); 4,95 (d, 1Н, ОН, J = 5.28 Hz); 7.29-7.41 (m, 9Н, CН(Ar)).

NMR 13С (characteristic signals) (DMSO-d6, δ/ ppm, J/Hz): 21.4, 21.8 (both s, 2СН3); 36.1, 36.6 (both s, С1, С5); 54.9, 55.7, 57.1, 58.1 (all s, С2, С4, С6, С8); 62.5 (s, СН2Ph); 75.9 (s, С9); 127, 128.5, 128.74, 129.25, 132.3, 130.85, 130.93, 137.71(br.) (all s, Ar); 168,5 (s, C=O).

Found (%): С, 69.35; H, 6.95; N, 6.93. Calculated for C23H27ClN2O2 (%): C, 69.25; H, 6.82; N, 7.02.

Anti-1,5-dimethyl-3-benzoyl-7-(4-bromobenzyl)-3,7-diazabicyclo[3.3.1]nonane-9-ol (4da)

140 mg (0.4 mmol) of bispidine 3d and 56.5 mg (0.4 mmol) of benzoyl chloride in 10 ml of dry benzene give gel, from which 0.14 g of the free base was isolated. Yield 79%.

NMR 1H (DMSO-d6, δ/ ppm, J/Hz): 0.65, 0.79 (both s, 6H, 2CH3); 2.15 (d, 1H, H6e/8e/6a/8a, J = 10.2 Hz); 2.23-2.36 (m, 3H, H6e/8e/6a/8a); 2.65 (d, 1Н, Н4а, J = 12.5 Hz); 3.05 (d, 1Н, Н2а, J = 13.3 Hz); 3.12-3.15 (m, 2Н, СН2Ph, H9); 3.42 (d, 1Н, Н2е, J = 13.7 Hz); 3.53 (d, 1Н, СН2Ph, J = 13.9 Hz); 4.48 (d 1Н, Н4е, J = 12.1 Hz); 4,95 (d, 1Н, ОН, J = 5.09 Hz); 7.29-7.31 (m, 4Н, CН(Ar)); 7.40-7.41 (m, 3Н, CН(Ar)); 7.44-7.46 (d, 2 Н, СН(2,6)(Ar), J = 8.4 Hz).

NMR 13С (characteristic signals) (DMSO-d6, δ/ ppm, J/Hz): 21.4, 21.8 (both s, 2СН3); 36.1, 36.6 (both s, С1, С5); 54.6, 57.1, 58.1 (all s, С2, С4, С6, С8); 75.90 (s, С9); 127, 128.7, 131.3, 131.41 (all s, Ar).

Found (%): С, 62.32; H, 6.14; N, 6.10. Calculated for C23H27BrN2O2 (%): C, 62.31; H, 6.14; N, 6.32.

Anti-1,5-dimethyl-3-(4-chlorobenzoyl)-7-benzyl-3,7-diazabicyclo[3.3.1]nonane-9-ol (4ab)

70 mg (0.27 mmol) of bispidine 3a and 47.1 mg (0.27 mmol) of 4-chlorobenzoyl chloride in 5 ml of dry benzene give gel, from which 0.093 g of the free base was isolated. Yield 78%.

NMR 1H (DMSO-d6, δ/ ppm, J/Hz): 0.66, 0.79 (both s, 6H, 2CH3); 2.13 (d, 1H, H6e/8e/6a/8a, J = 10.9 Hz); 2.25-2.32 (m, 2H, H6e/8e/6a/8a); 2.37 (d, 1H, H6e/8e/6a/8a, J = 10.6 Hz); 2.65 (d, 1Н, Н4а, J = 12.9 Hz); 3.06 (d, 1Н, Н2а, J = 13.3 Hz); 3.12-3.18 (m, 2Н, СН2Ph, H9); 3.37 (d, 1Н, Н2е, J = 13.5 Hz); 3.52 (d, 1Н, СН2Ph, J = 13.3 Hz); 4.45 (d, 1Н, Н4е, J = 12.9 Hz); 4,95 (d, 1Н, ОН, J = 4.9 Hz); 7.29-7.31 (m, 4Н, CН(Ar)); 7.22-7.34 (m, 7Н, CН(Ar)); 7.44-7.46 (d, 2 Н, СН(2,6)(Ar), J = 8.2 Hz).

NMR 13С (characteristic signals) (DMSO-d6, δ/ ppm, J/Hz): 21.4, 21.8 (both s, 2СН3); 36.1, 36.6 (s, С1, С5); 52.2, 57.3, 57.8, 58.1 (all s, С2, С4, С6, С8); 63.4 (s, СН2Ph); 75.9 (s, С9); 127.2, 128.6, 128.9, 129.0, 133.8, 136.5, 138,77 (all s, Ar); 167,5 (s, C=O).

Found (%): С, 69.48; H, 6.93; N, 6.93. Calculated for C23H27ClN2O2 (%): C, 69.25; H, 6.82; N, 7.02.

Anti-1,5-dimethyl-3-(4-chlorobenzoyl)-7-(4-fluorobenzyl)-3,7-diazabicyclo[3.3.1]nonane-9-ol (4cb)

70 mg (0.25 mmol) of bispidine 3c and 44.1 mg (0.25 mmol) of 4-chlorobenzoyl chloride in 5 ml of dry benzene give gel, from which 0.089 g of the free base was isolated. Yield 92%.

NMR 1H (DMSO-d6, δ/ ppm, J/Hz): 0.66, 0.78 (both, 6H, 2CH3); 2.13 (d, 1H, H6e/8e/6a/8a, J = 11.49 Hz); 2.23-2.36 (m, 3H, H6e/8e/6a/8a); 2.68 (d, 1Н, Н4а, J = 13.45 Hz); 3.06-3.15 (m, 3Н, Н2а, СН2Ph, H9); 3.41 (d, 1Н, Н2е, J = 13.33 Hz); 3.54 (d, 1Н, СН2Ph, J = 13.57 Hz); 4.48 (d, 1Н, Н4е, J = 14.18 Hz); 4,98 (d, 1Н, ОН, J = 5.14 Hz); 7.09 (tr, 2Н, СН(3,5) (С6Н4F) J = 8,86 Hz); 7.31-7.37 (m, 4Н, Н(Ar)); 7.49 (d, 2Н, Н(Ar), J=8.44 Hz).

NMR 13С (characteristic signals) (DMSO-d6, δ/ ppm, J/Hz): 21.4, 21.8 (both s, 2СН3); 36.1, 36.6 (s, С1, С5); 52.2, 57.0, 57.8, 58.0 (all s, С2, С4, С6, С8); 62.5 (s, СН2Ph); 75.9 (s, С9); 128.9, 129.0, 133.9, 136.5 (all s, Ar); 167,5 (s, C=O).

Found (%): С, 66.37; H, 6.35; N, 6.61. Calculated for C23H26ClFN2O2 (%): С, 66.26; H, 6.29; N, 6.72.

Anti-1,5-dimethyl-3-(4-chlorobenzoyl)-7-(4-chlorobenzyl)-3,7-diazabicyclo[3.3.1]nonane-9-ol (4bb)

70 mg (0.24 mmol) of bispidine 3b and 41.7 mg (0.24 mmol) of 4-chlorobenzoyl chloride in 5 ml of dry benzene give gel, from which 0.072 g of the free base was isolated. Yield 69%.

NMR 1H (DMSO-d6, δ/ ppm, J/Hz): 0.66, 0.79 (both s, 6H, 2CH3); 2.14 (d, 1H, H6e/8e/6a/8a, J = 11.49 Hz); 2.24-2.35 (m, 3H, H6e/8e/6a/8a); 2.68 (d, 1Н, Н4а, J = 13.45 Hz); 3.09 (д, 1Н, Н2а, J = 13.45 Hz); 3.12-3.16 (m, 2Н, СН2Ph, H9); 3.41 (d, 1Н, Н2е, J = 12.69 Hz); 3.55 (d, 1Н, СН2Ph, J = 13.45 Hz); 4.48 (d, 1Н, Н4е, J = 13.45 Hz); 4,98 (d, 1Н, ОН, J = 5.01 Hz); 7.31-7.37 (m, 6Н, CН(Ar)), 7.47(d, 2Н, Н(2,6)(ArС=O), J = 8.19 Hz).

NMR 13С (characteristic signals) (DMSO-d6, δ/ ppm, J/Hz): 21.4, 21.7 (both s, 2СН3); 36.6 (br. s, С1, С5); 52.1, 53.9, 57.1, 58.0 (all s, С2, С4, С6, С8); 62.45 (s, СН2Ph); 75.8 (s, С9); 128.5, 128.9, 130.9, 137.8 (all s, Ar); 167,5 (s, C=O).

Found (%): С, 63.70; H, 6.25; N, 6.34. Calculated for C23H26Cl2N2O2 (%): С, 63.74; H, 6.05; N, 6.46.

Anti-1,5-dimethyl-3-(4-chlorobenzoyl)-7-(4-bromobenzyl)-3,7-diazabicyclo[3.3.1]nonane-9-ol (4db)

140 mg (0.4 mmol) of bispidine 3d and 72.2 mg (0.4 mmol) of 4-chlorobenzoyl chloride in 5 ml of dry benzene give gel, from which 0.149 g of the free base was isolated. Yield 79%.

NMR 1H (DMSO-d6, δ/ ppm, J/Hz): 0.66, 0.79 (both s, 6H, 2CH3); 2.12 (d, 1H, 6a/6e/8a/8e, J = 9.78 Hz); 2.23-2.35 (m, 3H, 6a/6e/8a/8e); 2.65 (d, 1H, H4a, J = 13.30 Hz); 3.06-3.15 (m, 3H, H2a, H9, -CH2-Ar); 3.38 (d, 1H, ,H2e, J = 13.5 Hz); 3.49 (d, 1H, -CH2-Ar, J = 13.30 Hz); 4.45 (d, 1H, 4He, J = 13,69 Hz); 4.96 (d, 1H, -OH, J = 5.09 Hz); 7.26-7.32 (m, 4H, Ar-Br); 7.45-7.48 (m, 4H, Ar-Cl).

NMR 13С (characteristic signals) (DMSO-d6, δ/ ppm, J/Hz): 21.2, 21.7 (both s, 2СН3); 36.1 (br. s, С1, С5); 128.9, 129.0, 131.4, 131.6 (all s, Ar); 171,9 (s, C=O).

Found (%): С, 57.69; H, 5.51; N, 5.85. Calculated for C23H26BrClN2O2 (%): С, 57.81; H, 5.48; N, 5.86.

Anti-1,5-dimethyl-3-(2-thiophenecarbonyl)-7-benzyl-3,7-diazabicyclo[3.3.1]nonane-9-ol (4ae)

70 mg (0.27 mmol) of bispidine 3a and 39.3 mg (0.27 mmol) of 2-thiophenecarbonyl chloride in 5 ml of dry benzene give gel, from which 0.081 g of the free base was isolated. Yield 81%.

NMR 1H (DMSO-d6, δ/ ppm, J/Hz): 0.72, 0.80 (both s, 6H, 2CH3); 2.16 (d, 1H, H6e/8e/6a/8a, J = 13.69 Hz); 2.24-2.30 (m, 2Н, H6e/8e/6a/8a ); 2.35 (d, 2H, H6e/8e/6a/8a, J = 12.32 Hz); 2.67 (d, 1Н, Н4а, J = 13.3 Hz); 3.16 (d, 1Н, Н9, J = 5.09 Hz); 3.19-3.24 (m, 2Н, Н2а, СН2Ph); 3.37 (Н2е, under H2O signal); 3.90 (d, 1Н, СН2Ph, J = 13.3 Hz); 4.49 (d, 1Н, Н4е, J = 12.9 Hz); 4,96 (d, 1Н, ОН, J = 5.28 Hz); 7.07-7.09 (dd, 1Н, CH(4)(C4H3S), J1 = 5.0 Hz, J2 = 3.81 Hz), 7.16-7.28 (m, 6Н, СН(Ph), CH(3)(C4H3S)), 7.70 (d, 1Н, CH(5)(C4H3S), J=4.9 Hz).

NMR 13С (characteristic signals) (DMSO-d6, δ/ ppm, J/Hz): 21.5, 21.7 (both s, 2СН3); 36.2, 36.7 (s, С1, С5); 52.8, 57.6, 57.9 (br.) (all s, С2, С4, С6, С8); 63.4 (s, СН2Ph); 75.9 (s, С9); 127.0, 127.2, 128.5, 128.7, 128.9, 129.0, 138.9 (all s, Ar); 162,2 (s, C=O)

Found (%): С, 68.43; H, 7.10; N, 7.35; S, 8.60. Calculated for C21H26N2O2S (%): С, 68.08; H, 7.07; N, 7.56; S, 8.65.

Anti-1,5-dimethyl-3-(2-thiophenecarbonyl)-7-(4-fluorobenzyl)-3,7-diazabicyclo[3.3.1]nonane-9-ol (4ce)

70 mg (0.25 mmol) of bispidine 3c and 36.8 mg (0.25 mmol) of 2-thiophenecarbonyl chloride in 5 ml of dry benzene give gel, from which 0.085 g of the free base was isolated. Yield 88%.

NMR 1H (DMSO-d6, δ/ ppm, J/Hz): 1.49, 1.56 (both s, 6H, 2CH3); 2.93 (d, 1H, H6e/8e/6a/8a, J = 8.19 Hz); 3.02 (m, 2Н, H6e/8e/6a/8a), 3.12 (d, 1Н, H6e/8e/6a/8a, J = 10.76 Hz), 3.43 (d, 1Н, Н4а, J = 12.84 Hz); 3.93-4.01 (m, 3Н, Н2а, СН2Ph, H9); 4.11 (Н2е, under H2O signal); 4.70 (d, 1Н, СН2Ph, J = 13.69 Hz); 5.26 (d, 1Н, Н4е, J = 13.2 Hz); 5.75 (d, 1Н, ОН, J = 4.77 Hz); 7.77 (tr, 2Н, СН(3,5) (С6Н4F) J = 8,56 Hz); 7.84-7.87 (m, 1Н, CH(4)(C4H3S)), 8.03-8.06 (m, 3Н, СН(2,6), (С6Н4F), CH(3)(C4H3S)), 8.48 (d, 1Н, CH(5)(C4H3S), J =4.52 Hz)

NMR 13С (characteristic signals) (DMSO-d6, δ/ ppm, J/Hz): 21.5, 21.7 (both s, 2СН3); 36.2, 36.7 (s, С1, С5); 52.7, 57.8 (br.) (all s, С2, С4, С6, С8); 62.4 (s, СН2Ph); 75.9 (s, С9); 127.3, 128.4, 128.9, 129.0, 130.9, 131.6, 138.0 (all s, Ar); 162,3 (s, C=O).

Found (%): С, 64.89; H, 6.41; N, 6.99. Calculated for C21H25FN2O2S (%): C, 64.92; H, 6.49; N, 7.21.

Anti-1,5-dimethyl-3-(2-thiophenecarbonyl)-7-(4-chlorobenzyl)-3,7-diazabicyclo[3.3.1]nonane-9-ol (4be)

70 mg (0.24 mmol) of bispidine 3b and 34.8 mg (0.24 mmol) of 2-thiophenecarbonyl chloride in 10 ml of dry benzene give gel, from which 0.87 g of the free base was isolated. Yield 90%.

NMR 1H (DMSO-d6, δ/ ppm, J/Hz): 0.72, 0.79 (both s, 6H, 2CH3); 2.19 (d, 1H, H6e/8e/6a/8a, J = 10.39 Hz); 2.24-2.35 (m, 3H, H6e/8e/6a/8a); 2.68 (d, 1Н, Н4а, J = 13.45 Hz); 3.09 (d, 1Н, Н2а, J = 13.45 Hz); 3.12-3.16 (m, 2Н, СН2Ph, H9); 3.41 (d, 1Н, Н2е, J = 12.69 Hz); 3.55 (d, 1Н, СН2Ph, J = 13.45 Hz); 4.48 (d, 1Н, Н4е, J = 13.45 Hz); 4,98 (d, 1Н, ОН, J = 5.01 Hz); 7.31-7.31 (m, 6Н, CН(Ar)), 7.49(d, 2Н, H(2,6)(ArC=O), J = 8.19 Hz).

NMR 13С (characteristic signals) (DMSO-d6, δ/ ppm, J/Hz): 21.5, 21.7 (both s, 2СН3); 36.2, 36.7 (s, С1, С5); 52.7, 57.5, 57.8 (br.) (all s, С2, С4, С6, С8); 62.4 (s, СН2Ph); 75.8 (s, С9); 127.3, 128.4, 128.9, 129.0, 130.9, 131.6, 138.0 (all s, Ar); 162,2 (s, C=O).

Found (%): С, 62.21; H, 6.15; N, 6.81. Calculated for C21H25ClN2O2S (%): C, 62.28; H, 6.22; N, 6.92.

Anti-1,5-dimethyl-3-(2-thiophenecarbonyl)-7-(4-bromobenzyl)-3,7-diazabicyclo[3.3.1]nonane-9-ol (4de)

140 mg (0.4 mmol) of bispidine 3d and 60 mg (0.4 mmol) of 2-thiophenecarbonyl chloride in 10 ml of dry benzene give gel, from which 0.149 g of the free base was isolated. Yield 83%.

NMR 1H (DMSO-d6, δ/ ppm, J/Hz): 0.72, 0.79 (both s, 6H, 2CH3); 2.16-2.34 (m, 4H, H6e/8e/6a/8a); 2.66 (d, 1Н, Н4а, J = 12.7 Hz); 3.09 (m, 3Н, Н2а, СН2Ph, H9); 3.49 (Н2е, under H2O signal); 3.91 (d, 1Н, СН2Ph, J = 12.72 Hz); 4.45 (d, 1Н, Н4е, J = 13.5 Hz), 4,98 (d, 1Н, ОН, J = 4.89 Hz); 7.31-7.31 (m, 6Н, CН(Ar)), 7.49(d, 2Н, СН(Ar), J = 8.19 Hz).

Found (%): С, 56.09; H, 5.77; N, 6.03. Calculated for C21H25BrN2O2 (%): C, 56.12; H, 5.61; N, 6.23.

4ae*HCl in nitrobenzene.

To a suspension of 70 mg (0.27 mmol) of bispidine 3a in 2.5 ml of nitrobenzene was added dropwise a solution of 39 mg (0.27 mmol) of 2-thiophenecarbonyl chloride in 2.5 ml of nitrobenzene. Then the mixture was refluxed (210 oC) under vigorous stirring for 3.5 hours. Highly viscous and dense amber gel was formed after 2 days at room temperature.

Figure S1. Photo of 4ae*HCl in nitrobenzene

4ae*HCl in ethoxybenzene.

To a suspension of 70 mg (0.27 mmol) of bispidine 3a in 2.5 ml of ethoxybenzene was added dropwise a solution of 39 mg (0.27 mmol) of 2-thiophenecarbonyl chloride in 2.5 ml of ethoxybenzene. Then the mixture was stirred at 80 oC for 3.5 hours. Highly viscous and dense colourless gel was formed after 1 hour at room temperature.

Figure S2. Photo of 4ae*HCl in ethoxybenzene,

4ae*HCl in mesitylene.

To a suspension of 70 mg (0.27 mmol) of bispidine 3a in 2.5 ml of mesitylene was added dropwise a solution of 39 mg (0.27 mmol) of 2-thiophenecarbonyl chloride in 2.5 ml of mesitylene. Then the mixture was stirred at 80 oC for 3.5 hours. Loose colourless gel was formed after 1 hour at room temperature.

Figure S3. Photo of 4ae*HCl in mesitylene.

4ab*HCl in nitrobenzene.

To a suspension of 70 mg (0.27 mmol) of bispidine 3a in 2.5 ml of nitrobenzene was added dropwise a solution of 47.1 mg (0.27 mmol) of 4-chlorobenzoyl chloride in 2.5 ml of nitrobenzene. Then the mixture was stirred at 80 oC for 3.5 hours. A precipitate was formed.

Figure S4. Photo of 4ab*HCl in nitrobenzene.

4ab*HCl in ethoxybenzene.

To a suspension of 70 mg (0.27 mmol) of bispidine 3a in 2.5 ml of ethoxybenzene was added dropwise a solution of 47.1 mg (0.27 mmol) of 4-chlorobenzoyl chloride in 2.5 ml of ethoxybenzene. Then the mixture was stirred at 80 oC for 3.5 hours. Loose colourless gel was formed after 1 hour at room temperature.

Figure S5. Photo of 4ab*HCl in ethoxybenzene.

4ab*HCl in mesitylene.

To a suspension of 70 mg (0.27 mmol) of bispidine 3a in 2.5 ml of mesitylene was added dropwise a solution of 47.1 mg (0.27 mmol) of 4-chlorobenzoyl chloride in 2.5 ml of mesitylene. Then the mixture was stirred at 80 oC for 3.5 hours. Loose colourless gel was formed after 1 hour at room temperature.

Figure S6. Photo of 4ab*HCl in mesitylene.

|  | 100X | 25X |
| --- | --- | --- |
| 4cb*HCl |  |  |
| 4ce*HCl |  |  |
| 4bb*HCl |  |  |
| 4bc*HCl |  |  |

Figure S7. POM photomicrography of benzenogels obtained by Carl Zeiss microscope.

Table S1. Dependence of shear rate on viscosity benzene@4ce*HCl

| Shear rate, Pa | Viscosity, Pa*s |
| --- | --- |
| 100 | 0,0975 |
| 63,1 | 0,124 |
| 39,8 | 0,174 |
| 25,1 | 0,246 |
| 15,9 | 0,39 |
| 10 | 0,546 |
| 6,31 | 0,824 |
| 3,98 | 1,46 |
| 2,51 | 1,71 |
| 1,59 | 2,36 |
| 1 | 3,54 |
| 0,631 | 5,81 |
| 0,398 | 9,27 |
| 0,251 | 15 |
| 0,158 | 24,5 |
| 0,1 | 39,1 |
| 0,0631 | 62,2 |
| 0,0398 | 98,6 |
| 0,0251 | 158 |
| 0,0158 | 248 |
| 0,01 | 390 |
| 0,00631 | 613 |
| 0,00398 | 972 |
| 0,00251 | 1520 |
| 0,00158 | 2340 |
| 0,001 | 3680 |

Figure S8. Dependence of viscosity of benzene@4ce*HCl on shear rate.

Table S2. Dependence of the loss and storage moduli on angular frequency benzene@4ce*HCl.

|  | Moduli |  |
| --- | --- | --- |
| Angular frequency (ω),Rad/s | Loss (G”), Pа | Storage (G´), Pa |
| 0,996 | 56,9 | 70,1 |
| 1,58 | 119 | 155 |
| 2,5 | 168 | 219 |
| 3,96 | 204 | 278 |
| 6,28 | 246 | 343 |
| 9,96 | 292 | 421 |
| 15,8 | 357 | 516 |
| 25 | 427 | 599 |
| 39,6 | 535 | 702 |
| 62,8 | 689 | 746 |
| 99,6 | 904 | 851 |
| 158 | 945 | 934 |
| 250 | 1150 | 1130 |
| 396 | 1160 | 1110 |

Figure S9. Dependence of the loss and accumulation modules on angular frequency benzene@4ce*HCl

Table S3. Crystal data, data collection, structure solution and refinement parameters for 4cb, 2c, 3a, 3c, 1b, 5,7-dimethyl-1,3-diazaadamantan-6-one and 4da*HCl.

| Compound | 4cb | 2c | 3a | 3c | 1b | 5,7-dimethyl-1,3-diazaadamantan-6-one | 4da*HCl*(C6H6)2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Empirical formula | C23H26Cl1F1N2O2 | C17H23F1N2O2 | C16H24N2O1 | C16H23F1N2O1 | C34H50Cl2F2N4O5 | C10H16N2O1 | C29H34Br1Cl1N2O2 |
| Formula weight | 416.91 | 306.37 | 260.37 | 278.36 | 703.68 | 180.25 | 557.94 |
| Colour, habit | Colourless block | Colourless block | Colourless block | Colourless prism | Colourless block | Colourless prism | Colourless plate |
| Crystal size/mm | 0.350.180.08 | 0.350.350.20 | 0.400.200.10 | 0.400.300.20 | 0.200.150.06 | 0.400.200.10 | 0.250.080.01 |
| Crystal system | orthorhombic | orthorhombic | orthorhombic | monoclinic | monoclinic | orthorhombic | monoclinic |
| Space group | Pna21 | Pbcn | Pbca | P21/n | P21 | Fdd2 | C2/c |
| Unit cell dimensions: a/Å b/Å c/Å /° | 14.4619(10) 17.2081(12) 8.3953(6) 90 | 19.3091(11) 8.4233(5) 19.6775(12) 90 | 12.1577(4) 14.6409(5) 16.6996(6) 90 | 7.8747(5) 16.6186(10) 12.0211(8) 107.649(1) | 7.623(6) 14.139(11) 15.983(13) 95.175(13) | 14.7493(16) 44.868(5) 5.7913(6) 90 | 27.43(8) 10.69(3) 19.81(5) 112.93(4) |
| Volume/Å3 | 2089.3(3) | 3200.5(3) | 2972.52(18) | 1499.11(16) | 1716(2) | 3832.5(7) | 5349(26) |
| Z | 4 | 8 | 8 | 4 | 2 | 16 | 8 |
| Density (calculated)/g·cm-3 | 1.325 | 1.272 | 1.164 | 1.233 | 1.362 | 1.250 | 1.386 |
| Abs. coefficient/mm-1 | 0.213 | 0.091 | 0.073 | 0.086 | 0.247 | 0.082 | 1.666 |
| F(000) | 880 | 1312 | 1136 | 600 | 748 | 1568 | 2320 |
| Temperature/K | 120.0(2) | 120.0(2) | 160(2) | 160(2) | 150(2) | 150(2) | 160(2) |
|  range/ | 1.84 to 26.00 | 2.07 to 25.05 | 2.44 to 28.00 | 2.16 to 28.00 | 1.28 to 25.25 | 1.82 to 30.00 | 2.07 to 25.25 |
| Index ranges | -15  h  17 -9  k  21 -10  l  10 | -22  h  23 -9  k  10 -23  l  13 | -15  h  16 -19  k  19 -22  l  22 | -10  h  10 -21  k  21 -15  l  15 | -9  h  9 -16  k  16 -19  l  19 | -20  h  20 -62  k  62 -6  l  8 | -32  h  32 -12  k  12 -23  l  16 |
| Reflections collected | 11202 | 16298 | 28966 | 15258 | 11580 | 9106 | 13547 |
| Unique reflections [Rint] | 3955 [Rint=0.0440] | 2829 [Rint=0.0437] | 3579 [Rint=0.0315] | 3617 [Rint=0.0236] | 6117 [Rint=0.0903] | 1517 [Rint=0.0376] | 4817 [Rint=0.235] |
| Data / restraints / params | 3955 / 1 / 269 | 2829 / 0 / 225 | 3579 / 0 / 182 | 3617 / 0 / 273 | 6117 / 1 / 429 | 1517 / 1 / 183 | 4817 / 39 / 295 |
| Reflections with I>2(I) | 3377 | 2117 | 2862 | 3017 | 3711 | 1367 | 2030 |
| Goodness-of-fit on F2 | 1.024 | 1.040 | 1.085 | 1.064 | 0.972 | 1.074 | 0.985 |
| Final R indices [I>2(I)] | R1 = 0.0418 wR2 = 0.0811 | R1 = 0.0581 wR2 = 0.1198 | R1 = 0.0414 wR2 = 0.1120 | R1 = 0.0399 wR2 = 0.1047 | R1 = 0.0783 wR2 = 0.1699 | R1 = 0.0339 wR2 = 0.0874 | R1 = 0.1159 wR2 = 0.2769 |
| R indices (all data) | R1 = 0.0540 wR2 = 0.0848 | R1 = 0.0810 wR2 = 0.1306 | R1 = 0.0543 wR2 = 0.1188 | R1 = 0.0489 wR2 = 0.1098 | R1 = 0.1320 wR2 = 0.1943 | R1 = 0.0388 wR2 = 0.0904 | R1 = 0.2320 wR2 = 0.3363 |
| Abs. structure parameter | 0.21(7) | — | — | — | 0.24(12) | — | — |
| Largest diff. peak/hole (e·Å-3) | 0.170 / -0.180 | 0.242 / -0.265 | 0.347 / -0.173 | 0.360 / -0.200 | 0.607 / -0.391 | 0.243 / -0.163 | 1.413 / -0.682 |
| CCDC deposition number | 1838470 | 1838469 | 1838468 | 1838467 | 1838471 | 1838466 | 1838465 |

Figure S10. Molecular structure of 4cb. Displacement ellipsoids are shown at 50% probability level. Hydrogen atoms are omitted for clarity.

Figure S11. Molecular structure of 2c. Displacement ellipsoids are shown at 50% probability level. Hydrogen atoms are omitted for clarity. Minor components of disorder are drawn as open lines.

Figure S12. Molecular structure of 3a. Displacement ellipsoids are shown at 50% probability level. Hydrogen atoms are omitted for clarity.

Figure S13. Molecular structure of 3c. Displacement ellipsoids are shown at 50% probability level. Hydrogen atoms are omitted for clarity.

Figure S14. Molecular structure of 4da*HCl*(C6H6)2. Displacement ellipsoids are shown at 50% probability level. Solvent benzen molecules are not shown for cleraty.

Figure S15. Hydrogen-bonded finite motif in the structure 1c+H2O.

Figure S16. Molecular structure of 5,7-dimethyl-1,3-diazaadamantan-6-one. Displacement ellipsoids are shown at 50% probability level.

a)

a)

b)

b)

Figure S17. The structures a) and b) of ketone and its diol form in the crystal 1c. Displacement ellipsoids are shown at 50% probability level. Hydrogen atoms are omitted for clarity.

Figure S18. Scatterplot of C9…N separations in structures of neutral organic flexible bispidines.

Figure S19. Histogram of absolute differences between C9…N separations.

Figure S20. TEM micrograph of 4bc*HCl.

Figure S21. AFM micrograph of 4bc*HCl (the left picture is topography and the right picture is error signal).

Figure S22. AFM micrograph of 4bc*HCl (the left picture is topography and the right picture is error signal).

Figure S23. AFM micrograph of 4bc*HCl (15 Kx).

b)

a)

Figure S24. SEM micrographs of dry gel samples made by different methods of solvent removal from ethoxybenzene@4ae*HCl: under reduced pressure (a), sc-CO2 drying (b). Scale bar is 1 m.

Figure S25. FT IR spectra of the native gels benzene@4de*HCl and benzene@4ce*HCl.