Supporting Information

Hybrid delivery systems for methotrexate - lipidic liquid crystalline cubic phases and cubosomes with magnetic nanoparticles

Monika Mierzwa, Paweł Krysiński, Renata Bilewicz *

Faculty of Chemistry, University of Warsaw, Pasteura 1, PL 02-093 Warsaw, Poland

S1

The SAXS measurement, allows to obtain one dimensional function of scattering intensities in function of q - I(q) where q (nm-1) is the length of the scattering vector.

The scattering vector is related to the scattering angle – θ – and the wavelength of radiation – λ (in our case it is λCu,Kα = 0.1542 nm) by the relation [1]:

q=4πsinθλ   [1s]

The qi peak values are marked starting with q0 and the ratio qi/q0 is calculated. The ratio defines the phase symmetry and Miller indices of the Bragg peak. The lattice parameter a (nm-1) is calculated from the distance between 2 reflection plans d.

For cubic phases:

a=dhklh2+k2+l2   [2s]

dhkl=2πq  [3s]

a=2πqh2+k2+l2  [4s]

Size of the water channels was calculated using the lattice parameter and the composition of cubic phases:

φw = CwCw+1-Cwρwρl      [5s]

where φw - water volume fraction, Cw - water weight fraction, ρw - density of water = 0.997 g/cm3,  ρl - density of lipid, in our case ρMO = 0.942 g/cm3.

Lipid volume fraction was determined from the equation:

φl = 1- φw         [6s]

Lipid chain length (l) was determined by solving the following equation [2]:

φlipid=2δla+43πχla3       [7s]

δ - ratio of the minimal surface in a unit cell to the quantity (unit cell volume)2/3, χ - Euler–Poincare´ characteristic, a - lattice parameter of corresponding phase, l - lipid chain length/monolayer thickness.

Radius of water channels - rw was obtained by equation [3]:

rw=-δ2πχ12a-l         [8s]

- Kulkarni, Ch. V.; Wachter, W.; Iglesias-Salto, G.; Engelskirchenb, S.; Ahualliac, S.Monoolein: a magic lipid? Physical Chemistry Chemical Physics 2011, 13, 3004–3021, doi:10.1039/c0cp01539c2.

- Turner, D. C.; Wang, Z.-G.; Gruner, S. M.; Mannock, D. A.; McElhaney, R. N. Structural Study of the Inverted Cubic Phases of di- Dodecyl Alkyl-β-D-Glucopyranosyl-rac-Glycerol. Journal de Physique II 1992, 2, 2039−2063, doi:10.1051/jp2:1992250.

- 3. Anderson, D. M.; Gruner, S. M.; Leibler, S. Geometrical Aspects of the Frustration in the Cubic Phases of Lyotropic Liquid Crystals. Proceedings of the National Academy of Sciences of the United States of America 1988, 85, 5364−5368, www.jstor.org/stable/32152.

S2 Scheme of the reduction process of methotrexate [1].

- Pontinha, A. D. R.; Jorge, S. M. A.; Diculescu, V. C.; Vivan, M.; Oliveira-Brett, A. M. Antineoplasic Drug Methotrexate Redox Mechanism Using a Glassy Carbon Electrode. Electroanalysis 2012, 24, 917–923, doi:10.1002/elan.201100558.

S3 Release profiles of MTX from a cubic phase in pH 7.4 at 25[A] and 37ºC [B].

S4 DPV on GC electrode modified with phases without [A] and with [B] magnetic nanoparticles and the release profiles of MTX from LCPs [C] at pH 7.4 at 25ºC.

S5 The size [A] and zeta potential [B] of magnetocubosomes containing MTX determined with DLS at 25ºC.

S6 Standard calibration curve for methotrexate based on measurement at 303 nm in 0.1 M phosphate buffer, pH 7.4.

S7 Electron cryo-microscopy images of cubosomes [A] and magnetocubosome [B].