

(A)

(B)

A screenshot of a cell phone

Description automatically generated

(C)

A screenshot of a cell phone

Description automatically generated

Fig. S1. Characterization of CuONPs used in the present study.

Fig. S1A Transmission electron microscopy (TEM) image of CuONPs nanorods with average size of 68.92 ± 3.49 nm,

Fig. S1B zeta potential of -15.5 mV, and

Fig. S1C the composition analysis by energy-dispersive X-ray spectroscopy (EDX) of the constituents showing the presence of copper and oxygen elements.