Supplementary information for Strain and grain size of CeO2 and TiO2 nanoparticles: Comparing structural and morphological methods

Yamerson Canchanya-Huaman 1, Angie F. Mayta-Armas 1, Jemina Pomalaya-Velasco 1, Yéssica Bendezú-Roca 1, Jorge Andres Guerra 2 and Juan A. Ramos-Guivar 3,*

1	Laboratorio de No Metálicos, Facultad de Ingeniería Química, Universidad Nacional del Centro del Perú (UNCP), Av. Mariscal Ramón Castilla Nº 3909, El Tambo, Huancayo 12000,  Perú; yamerson2016@gmail.com (Y.C.H), armasfiorella23@gmail.com (A.F.M.A), jpomalayavelasco@gmail.com (J.P.V.), ybendezu@uncp.edu.pe (Y.B.R)

2	Departamento de Ciencias, Sección Física, Pontificia Universidad Católica del Perú, Av. Universitaria 1801, 15088, Lima, Perú; guerra.jorgea@pucp.edu.pe (J.A.G.)

3	Grupo de Investigación de Nanotecnología Aplicada para Biorremediación Ambiental, Energía, Biomedicina y Agricultura (NANOTECH), Facultad de Ciencias Físicas, Universidad Nacional Mayor de San Marcos, Av. Venezuela Cdra 34 S/N, Ciudad Universitaria, Lima 15081, Perú

*	juan.ramos5@unmsm.edu.pe; Tel.: +51-1-914728212

Supplementary Figures and Tables

Figure S1. Pure p-XRD pattern of CeO2 (a) and TiO2 NPs (b).

Figure S2. The modified W-H analysis of CeO2 (a) and TiO2 NPs (b), assuming USDM. The modified W-H analysis of CeO2 (c) and TiO2 NPs (d), assuming UDEDM.

Rietveld Refinement of LaB6 nano standard

Figure S3a shows the Rietveld refinement of the LaB6 pattern which allowed us to obtain crystal structure information by X-ray diffraction (XRD). The Rietveld refinement with the TCH function of this pattern gave a unit-cell parameter (a) and boron atomic position (z) of 4.155728 Å and 0.20395, respectively (Rwp = 11.4 %, RB = 5.104%).  Therefore, refinement of the pattern subtracts the broadening caused by the instrument, so that the sample contributes 100% of the peak broadening, thus being able to calculate the mean apparent size of the LaB6 standard, which was 40.5 nm.

a)

b)

c)

d)

Figure S3. Rietveld refinement using the TCH function for LaB6 (a). The observed experimental diffractograms are given by the red lines (Iobs), the black lines (Ical) are calculated diffractograms, and the residual lines are shown in blue color. Electron density model with 0.4 Å resolution of LaB6 for the (hkl) lattice planes (1 0 0) (b), (0 0 1) (c), and (0 1 0) (d).

Table S1. Rietveld refinement parameters of nano LaB6 standard using the Fullprof program.

| Refinement Parameters | LaB6 |
| --- | --- |
| a (Å) | 4.155728 |
| b (Å) | 4.155728 |
| c (Å) | 4.155728 |
| α (Å) | 90 |
| β (Å) | 90 |
| γ (Å) | 90 |
| V (Å3) | 71.7697 |
| FWHM parameters |  |
| U | 0.075526 |
| V | -0.068130 |
| W | 0.059013 |
| Global average size (nm) | 40.5 |
| Rp (%) | 11.6 |
| Rwp (%) | 11.44 |

| Supplementary Matlab code R2017b clear,clc betha=input('Enter betha in brackets (rad): '); theta_1=input('Enter 2*tetha in brackets (rad): '); theta=theta_1*pi/180; betha_S=betha.*(pi/180); h=input('Enter the plane h: '); k=input('Enter the plane k: '); l=input('Enter the plane l: '); a=input('Enter the cell parameter a: '); b=input('Enter the cell parameter b: '); c=input('Enter the cell parameter c: '); n=length(betha); crystal=input('Enter the crystal system: ','s'); for i=1:n %betha correction betha_Cor(i)=sqrt(betha(i)^2-0.01^2); betha_C(i)=betha_Cor(i)*pi/180; %radians %scherrer D0(i)=0.154056*0.94/(betha_C(i)*cos(theta(i)/2)); %Modified Scherrer Equation (Monshi–Scherrer Method) x0(i)=log(1/cos(theta(i)/2));%(degree) y0(i)=log(betha_C(i));%(radians) %Williamson–Hall’s (W-H) (UDM) x1(i)=4*sin(theta(i)/2);y1(i)=betha_C(i)*cos(theta(i)/2); %Williamson–Hall’s (W-H) (USDM) %young's modulus and interplanar distance switch crystal case 'cubic' C11=455.06*10^9;C12=188.74*10^9;C44=81.48*10^9;%N/m^2 s11=(C11+C12)/((C11-C12)*(C11+2*C12));s12=-C12/((C11-C12)*(C11+2*C12));s44=1/C44; l_yhkl(i)=s11-2*((s11-s12)-1/2*s44)*((h(i)^2*k(i)^2+k(i)^2*l(i)^2+... l(i)^2*h(i)^2)/(h(i)^2+k(i)^2+l(i)^2)^2); Yhkl(i)=(1/l_yhkl(i))*10^-12; %Tpas Yhkl2(i)=(1/l_yhkl(i))*10^-9; %Gpas l_d(i)=(h(i)^2+k(i)^2+l(i)^2)/a^2; dhkl(i)=sqrt(1/l_d(i)); case 'tetragonal' s11=5.1*10^-12;s12=-8*10^-13;s13=-3.3*10^-12;s33=1.07*10^-11; s44=1.85*10^-11;s66=1.67*10^-11; Yhkl(i)=((h(i)^2+k(i)^2+l(i)^2)^2/(s11*(h(i)^4+k(i)^4)+(2*s12+s66)*... h(i)^2*k(i)^2+(2*s13+s44)*(h(i)^2+k(i)^2)*l(i)^2+s33*l(i)^4))*10^-12; l_d(i)=(h(i)^2+k(i)^2)/a^2+l(i)^2/c^2; dhkl(i)=sqrt(1/l_d(i)); Yhkl2(i)=(Yhkl(i))*10^3; %Gpas otherwise disp('error') end x2(i)=4*sin(theta(i)/2)/Yhkl(i);y2(i)=betha_C(i)*cos(theta(i)/2); %UDEDM x3(i)=4*sin(theta(i)/2)*(2/Yhkl(i))^0.5;y3(i)=betha_C(i)*cos(theta(i)/2); %size-strain (SSP) x4(i)=(dhkl(i)*0.1)^2*betha_C(i)*cos(theta(i)/2)/0.154056; y4(i)=(dhkl(i)*0.1*betha_C(i)*cos(theta(i)/2)/0.154056)^2; %Halder–Wagner (H-W) x5(i)=betha_C(i)*(cos(theta(i)/2)/0.154056)/(2*dhkl(i)*sin(theta(i)/2)/0.154056)^2; y5(i)=(betha_C(i)*(cos(theta(i)/2)/0.154056)/(2*dhkl(i)*sin(theta(i)/2)/0.154056))^2; end disp('--------------------------------------------------------------------------') disp('hkl 2*theta theta(Degree) betha b_corrected betha yhkl dhkl') disp(' (Degree) (Degree) (Degree) (Degree) (radian) (Tpa) (A°)') disp('--------------------------------------------------------------------------') for i=1:n fprintf('%1.0f%1.0f%1.0f %4.4f %4.4f %2.4f %2.4f %2.4f %2.4f %2.4f\n',... h(i),k(i),l(i),theta_1(i),theta_1(i)/2,betha(i),betha_Cor(i),betha_C(i),Yhkl(i),dhkl(i)) end disp('=============Scherrer´s method================') D_prom=sum(D0)/n; fprintf(' Crystal size =%6.6f nm \n',D_prom) disp('==Modified Scherrer (Monshi–Scherrer Method)===') Ec0=polyfit(x0,y0,1);D00=0.154056*0.94/(exp(Ec0(2)));R0=corrcoef(x0,y0); R0_1=1-(n-1)/(n-length(Ec0))*(1-R0(1,2)^2); fprintf('intercept=%6.6f\n slope=%6.6f\n R^2=%2.4f\n',Ec0(2),Ec0(1),R0_1) fprintf('Crystal size=%6.6f nm\n',D00) disp('============== UDM method ===================') Ec1=polyfit(x1,y1,1);D1=0.154056*0.94/Ec1(2);R1=corrcoef(x1,y1); R2_1=1-(n-1)/(n-length(Ec1))*(1-R1(1,2)^2); fprintf('intercept=%6.6f\n slope=%6.6f\n R^2=%2.4f\n',Ec1(2),Ec1(1),R2_1) fprintf('Crystal size=%6.6f nm\n strain=%6.6f\n',D1,Ec1(1)) disp('============== USDM method ==================') Ec2=polyfit(x2,y2,1);D2=0.154056*0.94/Ec2(2); R2=corrcoef(x2,y2);R2_3=1-(n-1)/(n-length(Ec2))*(1-R2(1,2)^2); ep=Ec2(1)/(sum(Yhkl(i))/n); Young=sum(Yhkl2)/n; fprintf('intercept=%6.6f\n slope=%6.6f\n R^2=%2.4f\n Young=%6.5f Gpas\n',Ec2(2),Ec2(1),R2_3,Young) fprintf('Crystal size=%6.6fnm\n stress=%6.6f TPa\n eps=%6.6f\n',D2,Ec2(1),ep) disp('============== UDEDM method ================') Ec3=polyfit(x3,y3,1);D3=0.154056*0.94/Ec3(2);R3=corrcoef(x3,y3); R2_5=1-(n-1)/(n-length(Ec3))*(1-R3(1,2)^2); U=sqrt(Ec3(1));sigmaprom=sqrt(U*2*(sum(Yhkl(i))/n)); epsprom1=sigmaprom/(sum(Yhkl(i))/n); fprintf('intercept=%6.6f\n slope=%6.6f\n R^2=%2.4f\n',Ec3(2),Ec3(1),R2_5) fprintf('Crystal size=%6.6fnm\n U=%6.6f TJ/m^3\n',D3,U) fprintf('stress=%6.6f TPa\n eps=%6.6f\n\n',sigmaprom,epsprom1) disp('==============size-strain (SSP)==============') Ec4=polyfit(x4,y4,1);D4=0.75/Ec4(1);R4=corrcoef(x4,y4); R2_7=1-(n-1)/(n-length(Ec4))*(1-R4(1,2)^2); epsprom2=sqrt(abs(Ec4(2))*4); fprintf('intercept=%6.6f\n slope=%6.6f\n R^2=%2.4f\n ',Ec4(2),Ec4(1),R2_7) fprintf('Crystal size=%6.6fnm\n eps=%6.6f\n',D4,epsprom2) disp('==============Halder–Wagner (H-W)==============') Ec5=polyfit(x5,y5,1);D5=1/Ec5(1);R5=corrcoef(x5,y5); R2_9=1-(n-1)/(n-length(Ec5))*(1-R5(1,2)^2); eps5=sqrt(abs(Ec5(2))*4); fprintf('intercept=%6.6f\n slope=%6.6f\n R^2=%2.4f\n ',Ec5(2),Ec5(1),R2_9) fprintf('Crystal size=%6.6fnm\n eps=%6.6f\n',D5,eps5) 1.- TiO2 Crystal system: tetragonal Enter betha in brackets (rad): [0.58184;1.22664;0.53095;0.99278;0.68039;0.95882;0.85614;0.91353;1.11756;1.04971;1.48319;1.32014] Enter 2*tetha in brackets (rad): [25.41164;37.29742;37.94847;38.51314;48.16671;54.12399;55.16213;62.78055;69.00174;70.38002;75.31759;82.91796] Enter the plane h: [1;1;0;1;2;1;2;2;2;1;2;2] Enter the plane k: [0;0;0;1;0;0;1;1;0;1;2;1] Enter the plane l: [1;3;4;2;0;5;1;3;4;6;0;5] Enter the cell parameter a: 3.7892 Enter the cell parameter b: 3.7892 Enter the cell parameter c: 9.5370 Enter the crystal system: tetragonal -------------------------------------------------------------------------- hkl 2*theta theta(Degree) betha b_corrected betha yhkl dhkl (Degree) (Degree) (Degree) (Degree) (radian) (Tpa) (A°) -------------------------------------------------------------------------- 101 25.4116 12.7058 0.5818 0.5818 0.0102 0.1444 3.5214 103 37.2974 18.6487 1.2266 1.2266 0.0214 0.1022 2.4354 004 37.9485 18.9742 0.5310 0.5309 0.0093 0.0935 2.3843 112 38.5131 19.2566 0.9928 0.9927 0.0173 0.1234 2.3359 200 48.1667 24.0834 0.6804 0.6803 0.0119 0.1961 1.8946 105 54.1240 27.0620 0.9588 0.9588 0.0167 0.0967 1.7037 211 55.1621 27.5811 0.8561 0.8561 0.0149 0.1657 1.6684 213 62.7805 31.3903 0.9135 0.9135 0.0159 0.1265 1.4954 204 69.0017 34.5009 1.1176 1.1175 0.0195 0.1117 1.4833 116 70.3800 35.1900 1.0497 1.0497 0.0183 0.0979 1.3670 220 75.3176 37.6588 1.4832 1.4832 0.0259 0.1581 1.3397 215 82.9180 41.4590 1.3201 1.3201 0.0230 0.1081 1.2668 =============Scherrer´s method================ Crystal size =10.493920 nm ==Modified Scherrer (Monshi–Scherrer Method)=== intercept=-4.472674 slope=2.678714 R^2=0.4342 Crystal size=12.684231 nm ============== UDM method =================== intercept=0.008894 slope=0.003206 R^2=0.1455 Crystal size=16.281429 nm strain=0.003206 ============== USDM method ================== intercept=0.010850 slope=0.000256 R^2=0.0757 Young=127.01714 Gpas Crystal size=13.347166nm stress=0.000256 TPa eps=0.028390 ============== UDEDM method ================ intercept=0.009573 slope=0.000698 R^2=0.1288 Crystal size=15.127003nm U=0.026424 TJ/m^3 stress=0.021824 TPa eps=2.421569 ==============size-strain (SSP)============== intercept=-0.000011 slope=0.099077 R^2=0.7394 Crystal size=7.569883nm eps=0.006751 ==============Halder–Wagner (H-W)============== intercept=-0.000087 slope=0.196469 R^2=0.9657 Crystal size=5.089850nm eps=0.018624 2.- CeO2 Crystal system: cubic matlab program: Enter betha in brackets (rad): [0.37541;0.38647;0.40748;0.43751;0.41716;0.47768;0.54051;0.51532;0.66622;0.73322] Enter 2*tetha in brackets (rad): [28.56556;33.11107;47.55147;56.42074;59.16356;69.80874;76.80871;79.17714;88.55375;95.5336] Enter the plane h: [1;2;2;3;2;4;3;4;4;3] Enter the plane k: [1;0;2;1;2;0;3;2;2;3] Enter the plane l: [1;0;0;1;2;0;1;0;2;3] Enter the cell parameter a: 5.4097 Enter the cell parameter b: 5.4097 Enter the cell parameter c: 5.4097 Enter the crystal system: cubic -------------------------------------------------------------------------- hkl 2*theta theta(Degree) betha b_corrected betha yhkl dhkl (Degree) (Degree) (Degree) (Degree) (radian) (Tpa) (A°) -------------------------------------------------------------------------- 111 28.5656 14.2828 0.3754 0.3753 0.0065 0.2226 3.1233 200 33.1111 16.5555 0.3865 0.3863 0.0067 0.3444 2.7048 220 47.5515 23.7757 0.4075 0.4074 0.0071 0.2442 1.9126 311 56.4207 28.2104 0.4375 0.4374 0.0076 0.2739 1.6311 222 59.1636 29.5818 0.4172 0.4170 0.0073 0.2226 1.5616 400 69.8087 34.9044 0.4777 0.4776 0.0083 0.3444 1.3524 331 76.8087 38.4044 0.5405 0.5404 0.0094 0.2375 1.2411 420 79.1771 39.5886 0.5153 0.5152 0.0090 0.2728 1.2096 422 88.5537 44.2769 0.6662 0.6661 0.0116 0.2442 1.1043 333 95.5336 47.7668 0.7332 0.7332 0.0128 0.2226 1.0411 =============Scherrer´s method================ Crystal size =20.778772 nm ==Modified Scherrer (Monshi–Scherrer Method)=== intercept=-5.115142 slope=1.827695 R^2=0.9608 Crystal size=24.114843 nm ============== UDM method =================== intercept=0.004994 slope=0.000992 R^2=0.6279 Crystal size=28.995433 nm strain=0.000992 ============== USDM method ================== intercept=0.005262 slope=0.000219 R^2=0.6747 Young=262.93949 Gpas Crystal size=27.519766nm stress=0.000219 TPa eps=0.009852 ============== UDEDM method ================ intercept=0.005077 slope=0.000340 R^2=0.6808 Crystal size=28.525735nm U=0.018450 TJ/m^3 stress=0.028663 TPa eps=1.287381 ==============size-strain (SSP)============== intercept=0.000005 slope=0.039794 R^2=0.9964 Crystal size=18.846957nm eps=0.004653 ==============Halder–Wagner (H-W)============== intercept=-0.000023 slope=0.096611 R^2=0.9986 Crystal size=10.350833nm eps=0.009584 |  |  |  |
| --- | --- | --- | --- |