Supplementary Information

Original Article

Biocompatibility and antibacterial properties of TiCu(Ag) thin films produced by physical vapor deposition magnetron sputtering

Saqib Rashida,#, Gian Marco Vitab,#, Luca Persichettib, Giovanna Iuccib, Chiara Battocchiob, Rostislav Danielc, Daniela Visaggiob, Martina Marsottob, Paolo Viscab, Edoardo Bemporada, Paolo Ascenzib,d, Giovanni Capellinib, Marco Sebastiania*, Alessandra di Masib*

aUniversità degli Studi Roma Tre, Engineering Department, via della Vasca Navale 79, 00146 Rome, Italy

bUniversità degli Studi Roma Tre, Department of Science, Viale Guglielmo Marconi, 446, 00146 Rome, Italy

cDepartment of Materials Science, Montanuniversität Leoben, Franz-Josef-Straße 18, Leoben, 8700, Austria

dAccademia Nazionale dei Lincei, Via della Lungara 10, 00165 Rome, Italy

# These Authors contributed equally to this work

Running title: Biocompatibility and antibacterial properties of TiCu(Ag) thin films

*Corresponding authors:

Marco Sebastiani, e-mail: marco.sebastiani@uniroma3.it

Alessandra di Masi, e-mail: alessandra.dimasi@uniroma3.it

Table S1. Measured Binding Energies (BE), full widths at half maximum (FWHM) and calculated atomic ratios for the investigated samples; the fifth column (n2/n1) shows the atomic ratios between the first and the second component, in increasing BE order, for Cu2p3/2 and Ag3d5/2 core level signals; the sixth column between the atomic ratio (nX/nTi) between silver or copper and titanium (for copper and silver, the sum of both components is considered).

| Sample | Signal | Assignment | BE (eV) | FWHM (eV) | Atomic ratios |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | ±0.2 | ±0.2 | n2/n1 | nX/nTi |
| TiCu | Ti2p3/2 | TiO2 | 485.7 | 1.6 |  | 1 |
|  | Cu2p3/2 | Cu | 932.7 | 2.2 | 1 | 0.58 |
|  |  | CuO | 934.9 |  | 0.87 |  |
| TiCu | Ti2p3/2 | TiO2 | 485.7 | 1.6 |  | 1 |
| (F) | Cu2p3/2 | Cu | 932.8 | 2.5 | 1 | 0.67 |
|  |  | CuO | 935.3 |  | 0.41 |  |
| TiCu-10%Ag | Ti2p3/2 | TiO2 | 485.7 | 1.5 |  | 1 |
|  | Cu2p3/2 | Cu | 932.9 | 2.1 | 1 | 3.7 |
|  |  | CuO | 935.1 |  | 1.1 |  |
|  | Ag3d5/2 | Ag | 368.3 | 1.3 | 1 | 0.37 |
|  |  | Ag2O | 369.7 | 1.3 | 0.11 |  |
| TiCu-10%Ag | Ti2p3/2 | TiO2 | 485.7 | 1.6 |  | 1 |
| (F) | Cu2p3/2 | Cu | 933.2 | 2.4 | 1 | 3.3 |
|  |  | CuO | 935.2 | 2.4 | 2.2 |  |
|  | Ag3d5/2 | Ag | 368.5 | 1.3 | 1 | 0.41 |
|  |  | Ag2O | 369.9 | 1.3 | 0.08 |  |
| TiCu-20%Ag | Ti2p3/2 | TiO2 | 485.7 | 2.1 |  | 1 |
|  | Cu2p3/2 | Cu | 933.5 | 2.7 | 1 | 5.3 |
|  |  | CuO | 935.2 | 2.7 | 1.04 |  |
|  | Ag3d5/2 | Ag | 368.3 | 1.2 | 1 | 0.77 |
|  |  | Ag2O | 369.7 | 1.2 | 0.15 |  |
| TiCu-20%Ag | Ti2p3/2 | TiO2 | 485.7 | 1.7 |  | 1 |
| (F) | Cu2p3/2 | Cu | 933.1 | 2.1 | 1 |  |
|  |  | CuO | 935.2 | 2.1 | 1.24 | 7.8 |
|  | Ag3d5/2 | Ag | 368.5 | 1.2 | 1 | 0.72 |
|  |  | Ag2O | 369.9 | 1.2 | 0.09 |  |
| TiCu-30%Ag | Ti2p3/2 | TiO2 | 485.7 | 1.9 |  | 1 |
|  | Cu2p3/2 | Cu | 932.5 | 2.6 | 1 |  |
|  |  | CuO | 934.7 | 2.6 | 6.3 | 3.4 |
|  | Ag3d5/2 | Ag | 368.2 | 1.2 | 1 | 0.63 |
|  |  | Ag2O | 369.6 | 1.2 | 0.13 |  |
| TiCu-30%Ag | Ti2p3/2 | TiO2 | 485.7 | 1.6 |  | 1 |
| (F) | Cu2p3/2 | Cu | 933.6 | 2.3 | 1 | 11 |
|  |  | CuO | 935.6 | 2.3 | 0.7 |  |
|  | Ag3d5/2 | Ag | 368.6 | 1.3 | 1 | 2.1 |
|  |  | Ag2O | 369.9 | 1.3 | 0.14 |  |

Table S2. XPS results after human MRC5 fibroblasts detachment with trypsin.

| Sample | Signal | Assignment | BE (eV) ±0.2 | FWHM (eV) ±0.2 | Atomic ratios |
| --- | --- | --- | --- | --- | --- |
| TiCu | C1s | C-C C-N;C-O C=O COOH | 285.0 286.6 288.4 290.1 | 1.9 | 1 0.33 0.26 0.04 |
|  | N1s | C=N C-N N+ | 398.5 400.1 402.8 | 2.3 | 1 7.5 0.3 |
|  | O1s | TiO2 C=O C-O H2O | 530.1 531.8 532.8 534.5 | 1.8 | 1 1.4 1.4 0.18 |
|  | Ti2p | TiO2 | 458.4 | 1.9 |  |
|  | Cu2p | Cu CuO | 932.8 935.7 | 2.5 | 1 0.12 |
| TiCu-10% Ag | C1s | C-C C-N; C-O C=O COOH | 285.0 286.4 288.1 289.0 | 1.9 | 1 0.4 0.26 0.07 |
|  | N1s | C=N C-N N+ | 398.8 400.1 402.5 | 2.1 | 1 3.7 0.22 |
|  | O1s | TiO2 C=O C-O H2O | 530.1 531.7 533.0 535.2 | 2.0 | 1 1.1 0.55 0.12 |
|  | Ag3d | Ag Ag2O | 368.1 369.5 | 1.6 | 1 0.14 |
|  | Ti2p | TiO2 | 458.5 | 1.7 | 1 |
|  | Cu2p | Cu CuO | 933.8 935.8 | 2.5 | 1 0.17 |
| TiCu-20% Ag | C1s | C-C C-N;C-O C=O COOH | 285.0 286.5 288.2 289.7 | 1.9 | 1 0.49 0.33 0.09 |
|  | N1s | C=N C-N N+ | 399.0 400.4 402.3 | 2.2 | 1 1.8 0.2 |
|  | O1s | TiO2 C=O C-O H2O | 530.1 532.0 533.5 535.7 | 2.1 | 1 2.0 0.71 0.14 |
|  | Ag3d | Ag Ag2O | 368.3 369.9 | 1.5 | 1 0.13 |
|  | Ti2p | TiO2 | 458.5 | 1.7 |  |
|  | Cu2p | Cu CuO | 932.7 935.6 | 2.4 | 8.4 1 |
| TiCu-30% Ag | C1s | C-C C-N; C-O C=O COOH | 285.0 286.8 288.4 290.1 | 1.9 | 1 0.42 0.02 0.06 |
|  | N1s | C=N C-N N+ | 399.0 400.5 402.1 | 1.7 | 1 0.33 0.14 |
|  | O1s | TiO2 C=O C-O H2O | 530.1 532.5 534.6 536.9 | 2.3 | 1 2.3 5.6 1 |
|  | Ag3d | Ag Ag2O | 368.5 370.2 | 1.7 | 1 0.25 |
|  | Ti2p | TiO2 | 458.4 | 1.7 |  |
|  | Cu2p | Cu CuO | 932.9 935.5 | 2.3 | 1 0.085 |