Supporting Information

Effects of MWCNTs on char layer structure and ablative resistance of EPDM-based insulators

Zhiheng Chena, Shida Hana, Yuan Jia, Hong Wua,*, Shaoyun Guoa, Ning Yanb,**, Hongyan Lib

aThe State Key Laboratory of Polymer Materials Engineering, Polymer Research Institute of Sichuan University, Chengdu 610065, China

bXi’an Modern Chemistry Research Institute, Shaanxi, Xi’an, 710065, China

- The dispersion of MWCNTs in EPDM-based insulators

Fig. S1. The dispersion of 3 phr MWCNTs in EPDM-based insulators with (a) and without silica (b).

2.	TGA of MWCNTs, silica and EPDM-based insulators

Fig. S2. Thermal stability of MWCNTs (a) and the effects of MWCNTs content on the residual mass of insulators (group S (b), group NS (c)) after thermogravimetric analysis.

3.	SEM image and pore diameter statistics of char layer surface in group NS

Fig. S3. Effects of MWCNTs content on the average pore diameter of char layer surface of NS-C-0 (a), NS-C-0.3 (b), NS-C-0.7 (c), NS-C-1.5 (d), NS-C-3 (e), NS-C-6 (f).

4.	SEM image and EDS results of char layer section in group NS

Fig. S4. Effects of MWCNTs content on section structure and the element content of char layer: NS-C-0 (a), NS-C-0.3 (b), NS-C-0.7 (c), NS-C-1.5 (d), NS-C-3 (e), NS-C-6 (f).

5.	SEM image and pore diameter statistics of char layer surface in group S

Fig. S5. Effects of MWCNTs content on the average pore diameter of char layer surface of S-C-0 (a), S-C-0.3 (b), S-C-0.7 (c), S-C-1.5 (d), S-C-3 (e), S-C-6 (f).

6.	SEM image and EDS results of char layer section in group S

Fig. S6. Effects of MWCNTs content on section structure and the element content of char layer: S-C-0 (a), S-C-0.3 (b), S-C-0.7 (c), S-C-1.5 (d), S-C-3 (e), S-C-6 (f)

7.	Magnifying SEM image of char layer cross-section

Fig. S7. Effects of MWCNTs content on char layer cross-section of the EPDM-based insulators: NS-C-0 (a), NS-C-0.3 (b), NS-C-3 (c), NS-C-6 (d), S-C-0 (e), S-C-0.3 (f), S-C-3 (g) and S-C-6 (h).

8.	Magnifying SEM image of char layer

Fig. S8. Effects of MWCNTs content on char layer surface of the EPDM-based insulators: NS-C-0 (a), NS-C-0.3 (b), NS-C-3 (c), NS-C-6 (d), S-C-0 (e), S-C-0.3 (f), S-C-3 (g) and S-C-6 (h).

Table S1. Formulations of EPDM-based insulators (phra)

| Samples | EPDM (phr) | Silica (phr) | MWCNTs (phr) |
| --- | --- | --- | --- |
| S-C-0 | 100 | 20 | 0 |
| S-C-0.3 | 100 | 20 | 0.3 |
| S-C-0.7 | 100 | 20 | 0.7 |
| S-C-1.5 | 100 | 20 | 1.5 |
| S-C-3 | 100 | 20 | 3 |
| S-C-6 | 100 | 20 | 6 |
| NS-C-0 | 100 | 0 | 0 |
| NS-C-0.3 | 100 | 0 | 0.3 |
| NS-C-0.7 | 100 | 0 | 0.7 |
| NS-C-1.5 | 100 | 0 | 1.5 |
| NS-C-3 | 100 | 0 | 3 |
| NS-C-6 | 100 | 0 | 6 |

AF: 10phr, Boron phenolic resin: 20phr, Sulphur: 0.5phr, BIPB: 4phr, TAIC: 2phr, zinc oxide: 5phr, stearic acid: 1phr, Paraffin oil: 4phr.

a phr: parts per hundred grams of EPDM.

Table S2. Effects of MWCNTs on mass ablation rate and linear ablation rate of EPDM-based insulators with and without silica.

| Samples | Rm (g/s) | Rd (mm/s) | Rc (mm/s) |
| --- | --- | --- | --- |
| S-C-0 | 0.0396±0.0028 | 0.0980±0.0039 | 0.1635±0.0054 |
| S-C-0.3 | 0.0480±0.0029 | 0.1029±0.0060 | 0.1807±0.0064 |
| S-C-0.7 | 0.0508±0.0037 | 0.1076±0.0014 | 0.1778±0.0070 |
| S-C-1.5 | 0.0412±0.0034 | 0.0973±0.0057 | 0.1656±0.0068 |
| S-C-3 | 0.0389±0.0023 | 0.0880±0.0061 | 0.1559±0.0037 |
| S-C-6 | 0.0427±0.0007 | 0.0837±0.0023 | 0.1519±0.0006 |
| NS-C-0 | 0.0413±0.0011 | 0.1173±0.0051 | 0.1901±0.0087 |
| NS-C-0.3 | 0.0413±0.0016 | 0.1092±0.0027 | 0.1911±0.0021 |
| NS-C-0.7 | 0.0376±0.0019 | 0.1004±0.0039 | 0.1832±0.0065 |
| NS-C-1.5 | 0.0402±0.0031 | 0.0904±0.0037 | 0.1790±0.0063 |
| NS-C-3 | 0.0366±0.0007 | 0.0801±0.0016 | 0.1714±0.0053 |
| NS-C-6 | 0.0390±0.0020 | 0.1011±0.0038 | 0.1720±0.0088 |

Table S3. Effects of MWCNTs content on thermal conductivity and back-face temperature (Tmax, b) of EPDM-based insulators with and without silica.

| Samples | Back-face Temperature (°C) | Thermal Conductivity （W/mK） |
| --- | --- | --- |
| S-C-0 | 84.5±3.6 | 0.233±0.003 |
| S-C-0.3 | 86.8±3.1 | 0.238±0.004 |
| S-C-0.7 | 87.4±2.3 | 0.243±0.003 |
| S-C-1.5 | 98.0±6.7 | 0.258±0.002 |
| S-C-3 | 99.1±3.7 | 0.272±0.003 |
| S-C-6 | 106.1±3.8 | 0.304±0.006 |
| NS-C-0 | 66.1±2.9 | 0.221±0.003 |
| NS-C-0.3 | 68.0±4.0 | 0.220±0.001 |
| NS-C-0.7 | 72.1±4.0 | 0.228±0.005 |
| NS-C-1.5 | 78.9±5.4 | 0.235±0.003 |
| NS-C-3 | 81.3±3.2 | 0.253±0.001 |
| NS-C-6 | 97.9±2.1 | 0.289±0.002 |

Table S4. Effects of MWCNTs on mechanical property of EPDM-based insulators with and without silica

| Samples | Tensile strength (Mpa) | Elongation at break (%) | Density (g/cm3) |
| --- | --- | --- | --- |
| S-C-0 | 5.51±0.41 | 147.8±26.0 | 1.035±0.002 |
| S-C-0.3 | 5.79±0.22 | 182.5±12.1 | 1.040±0.001 |
| S-C-0.7 | 5.89±0.16 | 211.6±24.6 | 1.042±0.001 |
| S-C-1.5 | 5.98±0.33 | 284.6±14.8 | 1.051±0.002 |
| S-C-3 | 6.07±0.25 | 310.5±31.1 | 1.058±0.005 |
| S-C-6 | 6.31±0.14 | 362.8±43.7 | 1.064±0.002 |
| NS-C-0 | 3.50±0.10 | 17.5±2.3 | 0.944±0.001 |
| NS-C-0.3 | 3.77±0.31 | 10.6±0.8 | 0.951±0.001 |
| NS-C-0.7 | 4.12±0.41 | 14.2±0.6 | 0.952±0.002 |
| NS-C-1.5 | 5.02±0.18 | 16.4±1.8 | 0.960±0.004 |
| NS-C-3 | 5.14±0.40 | 27.7±2.3 | 0.976±0.003 |
| NS-C-6 | 5.31±0.21 | 49.5±5.3 | 0.994±0.001 |