Supplementary Material

Anti-Bacterial Iron Oxide Magnetic Nanoparticles based on Orange Peel Extract

David Giancarlo García Vélez 1, Cristina C. Garzón-Romero3, Mateo Alejandro Salazar Salazar3, Karina J. Lagos1, Kleber Orlando Campaña Cruz1, Alesis Debut5, Karla Vizuete5, Miryan Rosita Rivera 3, Dario Niebieskikwiat4, Maria J. Benitez2, María Paulina Romero Obando1*.

1Department of Materials, Escuela Politécnica Nacional (EPN), Quito, Ecuador

2Departmento de Física, Escuela Politécnica Nacional (EPN), Quito, Ecuador

3Laboratorio de Investigación en Citogenética y Biomoléculas de Anfibios (LICBA), Centro de Investigación para la Salud en América Latina (CISeAL), Facultad de Ciencias Exactas y Naturales, Pontificia Universidad Católica del Ecuador (PUCE), Quito, Ecuador

4Department of Physics, Colegio de Ciencias e Ingenierías, Universidad San Francisco de Quito, Quito, Ecuador.

5 Centro de Nanociencia y Nanotecnología, Universidad de Las Fuerzas Armadas ESPE, Sangolquí 171103, Ecuador

* Correspondence: 
María Paulina Romero Obando
maria.romerom@epn.edu.ec

# Supplementary Figures

Figure S1. a) Initial and final pH measured in the green synthesis, b) initial and final pH measured in the microwave synthesis, c) initial and final pH measured in the coprecipitation synthesis.

Figure S2. SEM micrographs of the samples a) 0GS-MNPs-Fe, b) 50GS-MNPs-Fe, c) 75GS-MNPs-Fe and d) 100CO-MNPs-Fe. Filters used: Smooth, Gaussian blur (sigma radius: 1.0) and Median (Radius 0.8 pixels).

Figure S3a. Indexed diffractograms of the samples; a) 0GS-MNPs-Fe, b) 25GS-MNPs-Fe, c) 50GS-MNPs-Fe, d) 75GS-MNPs-Fe and e) 100GS-MNPs-Fe

Figure S3b. Indexed diffractograms of the samples; a) 25MW-MNPs-Fe, b) 50MW-MNPs-Fe and c) 75MW-MNPs-Fe.

Figure S3c. Indexed diffractograms of the samples; a) 25CO-MNPs-Fe, b) 50CO-MNPs-Fe, c) 75CO-MNPs-Fe and d) 100CO-MNPs-Fe

Figure S4. EDS spectra of the samples a) 0GS-MNPs-Fe, b) 25GS-MNPs-Fe, and c) 75GS-MNPs-Fe.

Figure S5. Full Raman spectra (100-2000 cm-1) of the samples; a) 100CO-MNPs-Fe, b) 75GS-MNPs-Fe, c) 50GS-MNPs-Fe, d) 25GS-MNPs-Fe and e) 0GS-MNPs-Fe

Figure S6. ZFC/FC curve of the samples a) 50GS-MNPs-Fe, b) 50CO-MNPs-Fe and c) 50MW-MNPs-Fe

Figure S7. Size distribution of the MNPs-Fe corresponding to the samples; a) 50Gs-MNPs-Fe, b) 100CO-MNPs-Fe and c) 50MW-MNPs-Fe

# Supplementary Tables

Table S1. Yield by weight of MNPS-Fe obtained by GS, MW and CO

| Samples | Average weight (mg) |  |
| --- | --- | --- |
| 0GS-MNPs-Fe | 8.97 | ± 2.32 |
| 10GS-MNPs-Fe | 13.43 | ± 5.26 |
| 25GS-MNPs-Fe | 25.93 | ± 6.23 |
| 50GS-MNPs-Fe | 88.13 | ± 13.33 |
| 75GS-MNPs-Fe | 95.03 | ± 9.85 |
| 100GS-MNPs-Fe | 84.20 | ± 3.10 |
| 10CO-MNPs-Fe | 79.63 | ± 6.20 |
| 25CO-MNPs-Fe | 79.73 | ± 5.61 |
| 50CO-MNPs-Fe | 72.33 | ± 8.96 |
| 75CO-MNPs-Fe | 68.67 | ± 5.70 |
| 100CO-MNPs-Fe | 64.73 | ± 8.90 |
| 10MW-MNPs-Fe | 79.30 | ± 3.87 |
| 25MW-MNPs-Fe | 79.97 | ± 6.85 |
| 50MW-MNPs-Fe | 80.10 | ± 4.61 |
| 75MW-MNPs-Fe | 85.87 | ± 5.56 |

Table S2. Average roughness, obtained from the AFM topographies, for the samples obtained by GS.

| Average roughness - Ra (pm) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| ID | 0GS-MNPs-Fe | 25GS-MNPs-Fe | 50GS-MNPs-Fe | 75GS-MNPs-Fe | 100GS-MNPs-Fe |
| 1 | 153 | 186 | 122 | 139 | 81 |
| 2 | 74 | 181 | 78 | 70 | 42 |
| 3 | 118 | 105 | 61 | 116 | 69 |
| 4 | 93 | 107 | 63 | 50 | 53 |
| 5 | 110 | 66 | 90 | 56 | 59 |
| 6 | 75 | 131 | 102 | 94 | 42 |
| 7 | 73 | 119 | 51 | 61 | 62 |
| 8 | 86 | 143 | 102 | 57 | 61 |
| 9 | 117 | 183 | 71 | 51 | 46 |
| 10 | 68 | 132 | 45 | 67 | 47 |
| 11 | 62 | 113 | 96 | 71 | 50 |
| 12 | 172 | 97 | 103 | 86 | 66 |
| 13 | 105 | 115 | 66 | 84 | 48 |
| 14 | 166 | 75 | 74 | 52 | 47 |
| 15 | 78 | 85 | 64 | 63 | 63 |
| 16 | 183 | 146 | 77 | 61 | 54 |
| 17 | 86 | 117 | 54 | 92 | 69 |
| 18 | 65 | 132 | 56 | 52 | 49 |
| 19 | 101 | 108 | 72 | 65 | 74 |
| 20 | 78 | 134 | 112 | 99 | 75 |
| Average | 103 | 124 | 78 | 74 | 58 |
| DS | 38 | 33 | 22 | 24 | 12 |

Table S3a. Active Raman bands of functional groups found in the Raman spectra of the 0GS-MNPs-Fe, 25GS-MNPs-Fe, 50GS-MNPs-Fe, 75GS-MNPs-Fe and 100Co-MNPs-Fe samples

| Active Raman bands of functional groups (cm-1) - HORIBA | Raman bands in samples (cm-1) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 0GS-MNPs-Fe | 25GS-MNPs-Fe | 50GS-MNPs-Fe | 75GS-MNPs-Fe | 100CO-MNPs-Fe |
| 550-800, δ(C-Cl) (strong) | 564,6 (strong) | - | - | - | - |
| 600-1300, ν(C-C) aliphatic (medium) 630-790, ν(C-S) aliphatic (strong) 800-970, ν(O-C-O) (medium) | 628,4 (strong) | - | - | - | - |
|  | 645,7 (strong) | - | 710 (strong) | - | - |
|  | 798,2 (medium) | - | 854 (medium) | - | - |
| 600-1300, ν(C-C) aliphatic (medium) 800-970, ν(O-C-O) (medium) 1000, ν(C-C) aromatic (medium) | 952 (medium) | - | 950-1015 (medium) | 1004 (weak) | - |
| 600-1300, ν(C-C) aliphatic (medium) 1080-1100, ν(C-S) aromatic (strong) | 1100 (strong) | - | 1131 (medium) | - | - |
| 600-1300, ν(C-C) aliphatic (medium) 1060-1150, νas(C-O-C) (weak) 1000-1250, ν(C=S) (strong) | 1172 (strong) | 1162 (weak) | 1165 (medium) | 1160 (weak) | - |
| 600-1300, ν(C-C) aliphatic (medium) 1000-1250, ν(C=S) (strong) | 1274 (strong) | 1307 (medium) | 1300 (medium) | 1305 (media) | - |
| 1400-1470, δas(CH3), δ(CH2) (medium) 1450,1500, ν(C-C) aromatic (medium) | 1486 (medium) | 1479 (medium) | 1486 (medium) | 1477 (medium) | - |
| ~1600, δ(H2O) (weak wide) 1500-1900, ν(C=C) (strong) | 1604 (strong) | 1598 (medium) | 1591 (strong) | 1592 (medium) | 1608 (weak) |
| 1500-1900, ν(C=C) (strong) 1680-1820, ν(C=O) (medium) | 1676 (strong) | - | 1696 (medium) | - | - |
| 1500-1900, ν(C=C) (strong) 1680-1820, ν(C=O) (medium) | 1808 (strong) | - | 1805 (medium) | - | - |
| 1500-1900, ν(C=C) (strong) | 1904 (strong) | - | 1905 (medium) | - | - |
| Stretching symmetrical (ν), asymmetric (νas), symmetrical bending (δ), asymmetric (δas) |  |  |  |  |  |

Table S3b. Active bands found in the samples 0GS-MNPs-Fe, 25GS-MNPs-Fe, 50GS-MNPs-Fe, 75GS-MNPs-Fe and 100CO-MNPs-Fe by FT-IR

| FT-IR Bands, Functional Group | Bands obtained in the FT-IR spectra / sample |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 0GS-MNPs-Fe | 25GS-MNPs-Fe | 50GS-MNPs-Fe | 75GS-MNPs-Fe | 100CO-MNPs-Fe |
| (3700-3584)ν (O-H), alcohols | 3866 (weak) | 3886 (weak) | 3800 (weak) | --- | --- |
| (3700-3584)ν (O-H), alcohols | 3662 (weak) | 3706 (weak) | 3700 (weak) | 3690 (weak) | 3650 (weak) |
| (3000-2840),ν (C-H) alkanes (CH3) (~2872), ν (C-H), (CH3) (~2853), ν (C-H), (CH2) | --- | --- | 2856 (weak) | 2862 (weak) | --- |
| (2600-2550), ν (S-H), compounds S | 2576 (weak) | 2586 (weak) | 2532 (medium) | --- | --- |
| (2700-2250), ν (N-H), amine salts | 2336 (weak) | 2334 (weak) | 2350 (medium) | 2348 (weak) | 2354 (weak) |
| (2000-1900), ν (C=C=C), alkenes (1870-1540), ν (C=O) ketones (~ 1640), δ (H2O) | 1960 (weak) | 1932 (weak) | 1886 (medium) | --- | 1776 (weak) |
| (1670-1600), ν (C=C), (lineal, cíclicos) (1600-1585), δ (C-C), (aromatic) (1870-1540), ν (C=O), ketones (1710-1685), ν (C=O), aldehydes (~ 1640), δ (H2O) | 1698 (medium) | 1580 (medium) | 1600 (medium) | 1638 (weak) | --- |
| (1350-1150), ω,τ (C-H), (CH2) (1300-1000), δ (C-H), (aromatic) (1260-1000), ν (C-O), alcohols (1300-1000), ν(C-C-C), δ(C-C(=O)), ketones (1070-1030), ν(S=O), compounds S (1096-1089), ν(C-Cl), halogens | 1180 (medium) | 1156 (medium) | 1120 (medium) | 1158 (medium) | --- |
| (850-550), ν(C-Cl), halogens (~850), ω(=CH2), alkenes (900-675), δ(C-H), aromatic | 870 (medium) | 868 (medium) | 822 (medium) | 828 (medium) | --- |
| (850-550), ν(C-Cl), halógens (700-450), ν (Fe-O) | 578 | 546 | 640 | 578 | --- |
| (700-450), ν (Fe-O) | 508 | 502 | 536 | 520 | 550 |
| Stretching symmetrical (ν), asymmetrical (νas), symmetrical bending (δ), asymmetrical (δas), Scissoring (δs), Rocking (ρ), Wagging (ω), Twisting (τ). |  |  |  |  |  |