Supporting materials

Synergetic photocatalytic peroxymonosulfate oxidation of benzotriazole by cupper ferrite spinel: Factors and mechanism analysis

Masoumeh Golshana, Rasool Pelalakb, c, Babak Kakavandid,e,

a Department of Environmental Health Engineering, Zabol University of Medical Sciences, Zahedam, Iran

b  Institute of Research and Development, Duy Tan University, Da Nang 550000, Vietnam

c Faculty of Environmental and Chemical Engineering, Duy Tan University, Da Nang 550000, Vietnam

d Research Center for Health, Safety and Environment, Alborz University of Medical Sciences, Karaj, Iran

e Department of Environmental Health Engineering, Alborz University of Medical Sciences, Karaj, Iran

Table S1

CCD experiments and observed and predicted removal efficiencies using CuFe2O4/UV/PMS system.

| Run | Independent variables |  |  |  | Actual (Re%) | Predicted (Re%) | Residual |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | x1 | x2 | x3 | x4 |  |  |  |
| 1 | 0.2 | 2 | 20 | 30 | 55.97 | 57.56 | ‐1.59 |
| 2 | 0.3 | 1.5 | 30 | 50 | 57.31 | 58.04 | ‐0.73 |
| 3 | 0.2 | 2 | 40 | 30 | 55.24 | 52.56 | 2.68 |
| 4 | 0.2 | 1 | 40 | 70 | 44.11 | 43.54 | 0.56 |
| 5 | 0.3 | 1.5 | 30 | 50 | 58.06 | 58.04 | 0.022 |
| 6 | 0.4 | 2 | 40 | 30 | 72.39 | 70.38 | 2.01 |
| 7 | 0.3 | 0.5 | 30 | 50 | 52.35 | 55.83 | ‐3.48 |
| 8 | 0.4 | 1 | 40 | 30 | 59.42 | 58.63 | 0.79 |
| 9 | 0.2 | 1 | 40 | 30 | 46.42 | 42.87 | 3.54 |
| 10 | 0.3 | 1.5 | 10 | 50 | 67.67 | 67.15 | 0.52 |
| 11 | 0.5 | 1.5 | 30 | 50 | 81.96 | 83.50 | ‐1.54 |
| 12 | 0.2 | 2 | 40 | 70 | 52.74 | 54.89 | ‐2.15 |
| 13 | 0.2 | 1 | 20 | 70 | 63.27 | 64.94 | ‐1.68 |
| 14 | 0.4 | 1 | 40 | 70 | 68.54 | 66.62 | 1.93 |
| 15 | 0.3 | 1.5 | 30 | 10 | 50.99 | 56.67 | ‐5.68 |
| 16 | 0.1 | 1.5 | 30 | 50 | 50.22 | 51.51 | ‐1.29 |
| 17 | 0.3 | 2.5 | 30 | 50 | 68.51 | 67.87 | 0.64 |
| 18 | 0.3 | 1.5 | 50 | 50 | 46.30 | 49.65 | ‐3.35 |
| 19 | 0.2 | 2 | 20 | 70 | 66.95 | 65.24 | 1.7 |
| 20 | 0.4 | 2 | 20 | 30 | 68.41 | 66.48 | 1.93 |
| 21 | 0.3 | 1.5 | 30 | 50 | 57.66 | 58.04 | ‐0.38 |
| 22 | 0.3 | 1.5 | 30 | 90 | 75.17 | 72.33 | 2.84 |
| 23 | 0.4 | 2 | 20 | 70 | 78.27 | 81.47 | ‐3.21 |
| 24 | 0.4 | 1 | 20 | 30 | 68.27 | 65.78 | 2.48 |
| 25 | 0.4 | 1 | 20 | 70 | 78.93 | 79.11 | ‐0.18 |
| 26 | 0.3 | 1.5 | 30 | 50 | 58.65 | 58.04 | 0.61 |
| 27 | 0.3 | 1.5 | 30 | 50 | 58.25 | 58.04 | 0.21 |
| 28 | 0.3 | 1.5 | 30 | 50 | 58.31 | 58.04 | 0.27 |
| 29 | 0.4 | 2 | 40 | 70 | 80.18 | 80.02 | 0.16 |
| 30 | 0.2 | 1 | 20 | 30 | 61.26 | 58.92 | 2.34 |

Table S2

Results of ANOVA for response surface quadratic model.

| Source | Sum of squares | df | Mean Square | F Value | p-value Prob > F |
| --- | --- | --- | --- | --- | --- |
| Model | 3081.86 | 14 | 220.13 | 24.18 | < 0.0001 |
| x1 ‒ Catalyst dosage | 1535.24 | 1 | 1535.24 | 168.65 | < 0.0001 |
| x2 ‒ PMS Conc. | 217.56 | 1 | 217.56 | 23.9 | 0.0002 |
| x3 ‒ BTA Conc. | 459.54 | 1 | 459.54 | 50.48 | <0.0001 |
| x4 ‒ Reaction time | 368.06 | 1 | 368.06 | 40.43 | <0.0001 |
| x1 x2 | 4.24 | 1 | 4.24 | 0.47 | 0.5053 |
| x1 x3 | 79.22 | 1 | 79.22 | 8.7 | 0.0099 |
| x1 x4 | 53.47 | 1 | 53.47 | 5.87 | 0.0285 |
| x2 x3 | 122.03 | 1 | 122.03 | 13.41 | 0.0023 |
| x2 x4 | 2.76 | 1 | 2.76 | 0.3 | 0.59 |
| x3 x4 | 28.6 | 1 | 28.6 | 3.14 | 0.0966 |
| x12 | 153.6 | 1 | 153.6 | 16.87 | 0.0009 |
| x22 | 24.88 | 1 | 24.88 | 2.73 | 0.1191 |
| x32 | 0.22 | 1 | 0.22 | 0.024 | 0.8778 |
| x42 | 71.48 | 1 | 71.48 | 7.85 | 0.0134 |
| Residual Lack of Fit Pure Error | 136.54 135.37 1.17 | 15 10 5 | 9.1 13.54 0.23 | 57.94 | 0.0002 |
| Correction Total | 3218.41 | 29 |  |  |  |
| Std. Dev. | 3.02 |  | R-squared | 0.9576 |  |
| Mean | 62.06 |  | Adj. R-squared | 0.918 |  |
| C.V. | 4.86 |  | Pred. R-squared | 0.7572 |  |
| Press | 781.44 |  | Adeq. Precision | 19.045 |  |

R2 = 0.9576; R2adj = 0.918; R2pred = 0.7572; adequacy precision = 19.045; C.V.% = 4.86.

Fig. S1. Correlation between predicted and experimental values of BTA degradation variability.

Fig. S2. The normal probability plot of the internally studentized residuals.

Fig. S3. The experimental run number versus studentized residual data.

Fig. S4: HPLC chromatograms of the standard aniline as well as raw and treated solution of the BTA solution at different reaction times.

Corresponding authors: Department of Environmental Health Engineering, Zabol University of Medical Sciences, Zahedam, Iran. E-mail address: mgolshan.env@gmail.com (M. Golshan).