Supporting information

Colloidal Synthesis and Optical Properties of All-inorganic Cs2CuCl4 Nanocrystals

Wanying Gu 1,†, Yicheng Zeng 1,†, Yuan Deng 1, Pan Huang 1, Geyu Jin 1, Fangze Liu 2, Jing Wei1, and Hongbo Li 1,*

1	School of Materials Science and Engineering, Beijing Institute of Technology, Beijing 100081, China

2	Advanced Research Institute of Multidisciplinary Sciences, Beijing Institute of Technology, Beijing 100081, China

*	Correspondence: hongbo.li@bit.edu.cn (H.L.)

†	These authors have contributed equally to this work.

Table 1. Summary of the Optical Performance of the lead and lead free Perovskite NCs.

| Emitting materials | PL peak | FHWM | Fabrication technology | PLQY | Ref |
| --- | --- | --- | --- | --- | --- |
| CsPb(Cl/Br)3 | 452 nm | 23 nm | Hot injection | 60% | 8 |
| CsPb(Cl/Br)3 | 465 nm | 15 nm | Hot injection | 100% | 9 |
| Ni:CsPb(Cl/Br)3 | 470 nm | — | Modified recrystallization | 89% | 10 |
| Mn:CsPb(Cl/Br)3 | 466 nm | 17.9 nm | Hot injection | 44% | 11 |
| Cs3Bi2Br9 | 414 nm | 38 nm | Modified recrystallization | 22% | 13 |
| Cs3Sb2Br9 | 408 nm |  | modified supersaturated recrystallization | 51.2% | 15 |
| Cs3Cu2I5 | 445 nm | 63 nm | Hot injection | 87% | 16 |
| Ag：Cs2CuCl4 | 434 nm | 58 nm | Hot injection | 42% | This work |

Figure S1. (a) TEM images of the Cs3Cu2Br5 NCs. (b) UV/Vis absorption, PLE, and PL spectra of Cs3Cu2Br5 NCs. (c) XPS survey scan of Cs3Cu2Br5 NCs. (d,e,f) The high-resolution XPS spectra corresponding to Cs 3d, Cu 2p and Br 3d, respectively.

Figure S2. The FITR spectra of Cs2CuCl4 NCs.

Figure S3. PL spectra for Cs2CuCl4 NCs and Ag treated samples. (b) PL spectra for Cs2CuCl4 NCs and Cs2CuCl4-OLA.

Figure S4. Schematic model representing the emission mechanism.