Electronic Supporting Information for the article

Biocompatible Phosphorescent O2-sensors Based on Ir(III) Complexes for in vivo Hypoxia Imaging

Mozhgan Samandarsangari 1, Daria O. Kozina 1, Victor V. Sokolov 1, Anastasia D. Komarova 2,3, Marina V. Shirmanova 2, Ilya S. Kritchenkov 1*, Sergey P. Tunik 1*

1Institute of Chemistry, St. Petersburg State University, Universitetskaya Embankment 7-9, 199034 St. Petersburg, Russia

2Institute of Experimental Oncology and Biomedical Technologies, Privolzhskiy Research Medical University, Minin and Pozharsky sq. 10/1, 603005 Nizhny Novgorod, Russia

3Institute of Biology and Biomedicine, Lobachevsky State University of Nizhny Novgorod, Gagarina av., 23, 603950, Nizhny Novgorod, Russia

*Correspondence: i.s.kritchenkov@spbu.ru (ISK), s.tunik@spbu.ru (SPT)

Synthesis of Ligands and Complexes

Synthesis of 6-(benzo[b]thiophen-2-yl)nicotinic acid. Methyl 6-(benzo[b]thiophen-2-yl)nicotinate (400.0 mg, 1.485 mmol) and KOH (250.0 mg, 4.455 mmol) were stirred in THF/H2O (1:1, 6 mL) at RT for 90 h. The mixture was diluted with water (60 mL) and washed with CHCl3 (60 mL). After two CHCl3 washings, the aqueous layer was separated, neutralized with 1 M HCl(aq), concentrated in vacuum (to 30 mL) and acidified to pH = 5. The precipitate was collected by filtration, washed with water and dried in vacuum to afford the title compound as a pale yellow solid, requiring no further purification. Yield: 285 mg (75%). 1H NMR ((CD3)2SO, 400 MHz, δ): 9.08 (s, 1H), 8.34 (d, J = 8.3 Hz, 1H), 8.32 (s, 1H), 8.23 (d, J = 8.3 Hz, 1H), 8.03-8.00 (m, 1H), 7.94-7.92 (m, 1H), 7.45-7.41 (m, 2H). HRMS (ESI) m/z: 256.0432 calculated for C14H10NO2S+ [M+H]+, found 256.0386.

Synthesis of N^C ligand. A suspension of 6-(benzo[b]thiophen-2-yl)nicotinic acid (125.0 mg, 0.490 mmol), 2,5,8,12,15,18-hexaoxanonadecan-10-amine (173.7 mg, 0.588 mmol), N,N′ dicyclohexylcarbodiimide (DCC, 121.3 mg, 0.588 mmol), N-hydroxysuccinimide (NHS, 67.7 mg, 0.588 mmol), 4-(dimethylamino) pyridine (DMAP, 1.8 mg, 0.015 mmol), NEt3 (59.5 mg, 0.588 mmol) in dry DMSO (1.0 mL) was stirred at 40 °C for 4 days. The reaction mixture was concentrated in vacuum, the residue was suspended in 5 mL acetonitrile, cooled for 2 days and the solution was isolated by centrifugation and vacuum-dried to give the oily substance. 2 mL of water was added to the oily residue, sonicated, the aqueous solution was decanted and the residue was vacuum dried. The oily residue was dissolved in DCM, cooled for 1 day, centrifuged and the solution was thoroughly dried to give the desired compound. Yield: 231 mg (89%).1H NMR (CDCl3, 400 MHz, δ): 9.02 (s, 1H), 8.19 (d, J = 8.3 Hz, 1H), 7.91 (s, 1H), 7.88-7.81 (m, 3H), 7.39-7.34 (m, 2H), 7.04 (d, J = 8.1 Hz, NH), 4.45 (m, 1H, CH), 3.81-3.51 (m, 20H, CH2), 3.35 (s, 6H, CH3). HRMS (ESI) m/z: 555.2141 calculated for C27H36N2NaO7S+ [M+Na]+, found 555.2105.

Synthesis of iridium dimeric complex [Ir2(N^C2)4Cl2]. IrCl3∙6H2O (88.2 mg, 0.217 mmol), N^C ligand (231 mg, 0.434 mmol), a mixture of distilled 2-methoxyethanol (10 mL) and water (2.5 mL) were placed in a 25 mL test tube with screw cap and degassed for 20 minutes. The reaction mixture was stirred at 100 °C for 18 h. The resulting dark-red solution was thoroughly evaporated, the dried substance was dissolved in 0.4 mL of CHCl3 and precipitated by adding 3 mL of n-hexane. The resulting suspension was sonicated, decanted, and the oily residue was vacuum dried. The residue was washed with water twice (2 × 1 mL) and vacuum dried. The product was dissolved in 1 mL of DCM, cooled for 1 h, centrifuged and the solution was evaporated. The resulting solid was dissolved in 0.3 mL of DCM and precipitated by adding 2 mL of Et2O and then 1 mL of n-hexane, solicited, decanted, the precipitate was dried under reduced pressure to give dark-red solid. Yield: 260 mg (93%).1H NMR ((CD3)2SO, 400 MHz, δ): 10.39 (s, 1H), 10.11 (s, 1H), 8.74 (d, J = 8.0 Hz, 1H, NH), 8.65 (d, J = 8.0 Hz, 1H, NH), 8.60 (d, J = 8.4 Hz, 1H), 8.51 (d, J = 8.4 Hz, 1H), 8.04 (d, J = 8.4 Hz, 1H), 7.89 (d, J = 8.4 Hz, 1H), 7.86 (d, J = 8.1 Hz, 1H), 7.81 (d, J = 8.2 Hz, 1H), 7.22 (t, H = 7.7 Hz, 1H), 7.15 (t, J = 7.7 Hz, 1H), 6.92 (t, J = 7.7 Hz, 1H), 6.78 (t, J = 7.7 Hz, 1H), 6.25 (d, J = 8.1 Hz, 1H), 5.56 (d, J = 8.3 Hz, 1H), 4.30 (m, 2H, CH), 3.63-3.42 (m, 40H, CH2), 3.23 (s, 9H, CH3), 3.22 (s, 3H, CH3). HRMS (ESI) m/z: 1313.3537 calculated for C54H70ClIrN4NaO14S2+ [Ir(N^C)2Cl+Na]+, found 1313.3737.

General procedure for the synthesis of iridium complexes Ir1, Ir2 and Ir3. To obtain [Ir(N^C)2(N^N#)]Cl complexes, the [Ir2(N^C2)4Cl2] dimeric complex (50 mg, 0.019 mmol),  was added to the 2 mL methanol solution of the corresponding N^N# ligand (0.040 mmol) and reacted for 20 h at RT. Then the solutions were dried under reduced pressure and worked up as follows.

Complexes Ir1 and Ir2. The resulting residues were dissolved in 0.3 mL of acetone and then precipitated by adding of 3.0 mL of Et2O, solicited, decanted and dried. The residues were dissolved in 1.5 mL of water, centrifuged, and the aqueous solutions were vacuum dried. The dried residues were dissolved in 1 mL of ethyl acetate, centrifuged and the solvents were evaporated in vacuo, and the products were purified by silica gel column chromatography (CHCl3/methanol 20:1, then 10:1 and then 5:1 mixture). The target fractions were combines, dried in vacuum, and the obtained solid residues were dissolved in 0.3 mL of acetone and then precipitated by adding of 3.0 mL of Et2O and 1 mL of n-hexane, sonicated, decanted and the precipitates were thoroughly dried to obtain the final Ir(III) complexes.

Complex Ir1. Yield: 50 mg (72%). 9.53 (s, 1H), 8.57 (d, J = 8.3 Hz, 1H), 8.44-8.38 (m, 3H), 8.05 (s, 1H), 7.99 (s, 1H), 7.95-7.89 (m, 3H), 7.83 (d, J = 8.3 Hz, 1H), 7.77 (d, J = 8.3 Hz, 1H), 7.64 (t, J = 7.5 Hz, 1H), 7.24 (t, J = 7.6 Hz, 1H), 7.20 (t, J = 7.6 Hz, 1H), 6.90 (t, J = 7.7 Hz, 1H), 6.86 (t, J = 7.7 Hz, 1H), 6.10 (d, J = 8.2 Hz, 1H), 6.03 (d, J = 8.2 Hz, 1H), 5.30 (s, 2H, CH2), 4.34-4.23 (m, 2H, CH), 4.14-4.08 (m, 1H, CH), 3.64-3.44 (m, 60H, CH2), 3.32 (s, 3H, CH3), 3.31 (s, 3H, CH3), 3.30 (s, 6H, CH3), 3.29 (s, 6H, CH3). HRMS (ESI) m/z: 915.8300 calculated for C79H109IrN9NaO23S22+ [M+Na]2+, found 915.8296.

Complex Ir2. Yield: 72 mg (95%). 9.37 (s, 1H), 8.70 (d, J = 8.0 Hz, 1H), 8.51 (d, J = 8.5 Hz, 2H), 8.46-8.39 (m, 3H), 8.23 (d, J = 8.2 Hz, 1H), 8.18 (s, 1H), 8.15 (d, J = 8.5 Hz, 1H), 8.09 (d, J = 8.6 Hz, 1H), 7.96 (d, J = 8.2 Hz, 1H), 7.91-7.89 (m, 1H), 7.87-7.83 (m, 1H), 7.78 (t, J = 8.1 Hz, 2H), 7.60 (t, J = 7.6 Hz, 1H), 7.44 (d, J = 8.3 Hz, 1H), 7.34-7.23 (m, 4H), 7.18 (t, J = 7.6 Hz, 1H), 7.12-7.09 (m, 3H), 6.81 (t, J = 7.6 Hz, 1H), 6.52 (d, J = 8.2 Hz, 1H), 6.13 (d, J = 8.3 Hz, 1H), 5.81 (t, J = 7.6 Hz, 1H), 4.55 (m, 1H, CH), 4.40 (m, 1H, CH), 4.20 (m, 1H, CH), 3.83-3.38 (m, 60H, CH2), 3.33 (s, 6H, CH3), 3.26 (s, 3H, CH3), 3.25 (s, 3H, CH3), 3.23 (s, 3H, CH3), 3.06 (s, 3H, CH3). HRMS (ESI) m/z: 985.3532 calculated for C94H114IrN8NaO21S22+ [M+Na]2+, found 985.3558.

Complex Ir3. The obtained solid was dissolved in 0.3 mL of DCM and then precipitated by adding of 3.0 mL of Et2O and 1 mL of n-hexane, sonicated, decanted and the precipitate was thoroughly dried. The residue was dissolved in 1.2 mL of water, centrifuged, and the aqueous solution was vacuum dried. The dried residue was dissolved in 1 mL of ethyl acetate, centrifuged and dried. This solid was dissolved in 1 mL of DCE, centrifuged and the solution was dried under vacuum. The resulting red solid was dissolved in 0.2 mL of DCM and then precipitated by adding of 3.0 mL of Et2O, sonicated, decanted and vacuum dried and this process was repeated six times. Then the solid residue was dissolved in 1 mL of acetonitrile, centrifuged and the solution was dried. Further, the solid was dissolved in 1 mL of toluene, centrifuged and the solution was thoroughly dried. Dried residue was dissolved in 0.2 mL of acetone and precipitated by adding 4 mL of Et2O, sonicated, decanted and vacuum dried. Yield: 47 mg (59%). 9.24 (s, 1H), 8.38 (d, J = 8.5 Hz, 1H), 8.15 (d, J = 5.6 Hz, 1H), 8.06 (s, 1H), 7.99 (d, J = 5.6 Hz, 1H), 7.93 (d, J = 8.5 Hz, 1H), 7.86 (d, J = 8.1 Hz, 1H), 7.25 (t, J = 7.6 Hz, 1H), 6.90 (t, J = 7.6 Hz, 1H), 6,13 (d, J = 8.1 Hz, 1H), 4.42 (m, 1H, CH), 4.23 (m, 1H, CH), 3.71-3.45 (m, 40H, CH2), 3.30 (s, 3H, CH3), 3.28 (s, 3H, CH3), 3.21 (s, 3H, CH3), 3.20 (s, 3H, CH3). HRMS (ESI) m/z: 1038.4058 calculated for C92H132IrN8NaO28S22+ [M+Na]2+, found 1038. 4411.

Experimental details

Photophysical experiments. Photophysical measurements were performed in aqueous media. Absorption spectra were recorded using Shimadzu UV-1800 spectrophotometer. The emission spectra were measured on Avantes AvaSpec-2048x64 spectrometer. The values of the absolute emission quantum yield in solution were measured using a comparative method, 365 nm LED as excitation source and [Ru(bpy)3][PF6]2 water solution (Φ = 0.040 air-saturated, 0.063 Ar-saturated) as the reference. For the lifetime measurements pulse laser DTL-375QT (wavelength 355 nm, pulse width 5 ns, repetition frequency 1000 Hz), Hamamatsu (H10682-01) photon counting head, FASTComTec (MCS6A1T4) multiple-event time digitizer and Ocean Optics monochromator (Monoscan-2000, interval of wavelengths 1 nm) were used. PyroScience FireStingO2 oxygen meter, equipped with an oxygen sensor OXROB10 and a temperature sensor TDIP15, was used to measure concentration and partial pressure of molecular oxygen in aqueous solutions. Quantum Northwest qpod-2e cuvette sample compartment was used for temperature control.

Computational Details. Optimized geometry of ground and exited triplet states for all complexes under consideration and their photophysical properties were calculated using the Gaussian 16[1] computer code with DFT methodology. For these purposes, the hybrid Austin-Frisch-Petersson functional with dispersion (APFD)[2] was used due to their best agreement with the experimental results. For all atoms were chosen the Stuttgart-Dresden effective core pseudopotential (SDD) with the corresponding basis set[3]. The Polarizable Continuum Model (PCM)[4] was applied for simulation of effects of water as a non-specific solvent.

Energies of emission were calculated as the difference between the energy of the optimized triplet state and the energy of singlet state at the same triplet geometry (‘vertical’ transition). The electronic absorption spectra were obtained using TD-DFT methodology with 180 excited states for all complexes. The UV/Vis absorption spectra was obtained from previously calculated oscillator strengths using the method described in work[5] with Lorentzian broadening of 2000 cm-1.

The electron density during absorption and emission transitions was investigated using Natural Transition Orbitals (NTO)[6] and Interfragment Charge Transfer (IFCT)[7] calculations. The Multiwfn 3.6 software[7] was used for both methods. The changes of electronic density Δρ during the S0 →Si transitions were estimated as:

ΔρS0→Si= kΨikvirt2-kΨik(occ)2

where Ψik(occ) and Ψik(virt) are NTO pairs for S0→Si transition. The electronic density's change during T1→S0 transition was  similarly.

Cell cultures. The experiments were carried out on cell lines CT26 (mouse colorectal cancer) and HCT116 (human colorectal cancer) that had passed at least 3 and no more than 6 passages. The cells were cultured according to the standard procedure in the complete growth medium DMEM (Gibco, Carlsbad, CA, USA) supplemented with glucose (4.5 g/l) (Gibco, Carlsbad, CA, USA), L-glutamine (Gibco, Carlsbad, CA, USA) and 10% fetal bovine serum (HyClone, USA) at 37°C, 5% CO2. Cell passage was performed 3 times a week using Versen solution (Gibco, Carlsbad, CA, USA) and 0.25% trypsin-EDTA (Thermo Fisher Scientific, Waltham, MA, USA), when the cell monolayer filled 70–90% of the area of the culture flask.

For the MTT assay, cells were seeded in 96 well plates: 2000 CT26 cells or 10,000 HCT116 cells per well in 200 µl of DMEM. For confocal microscopy, CT26 cells were seeded in 35 mm glass bottom FluoroDish dishes (Ibidi GmbH, Gräfelfing, Germany) at 300,000 cells in 2 ml of DMEM.

Tumor Model. All animal protocols were approved by the Local Ethical Committee of the Privolzhsky Research Medical University (Nizhny Novgorod, Russia). Experiments were performed on female Balb/C mice (n = 3) and nu/nu mice (n = 2) weighing 20–22 g. Tumor cells were inoculated in PBS solution intradermally into the mouse ear in the amount of 200,000 CT26 cells or 500,000 HCT116 cells. The study was carried out on the 10-12th day after the cells inoculation, when the tumors were 6-8 mm in diameter. Mice were anesthetized by an intramuscular injection of Zoletil (40 mg/kg, Virbac, Carros, France) and 2% Rometar (10 mg/kg, Spofa, Jicin, Czech Republic). After PLIM experiment, the tumors were excised and placed in a 10% formalin for pathomorphological analysis.

МТТ-assay. Ir1, Ir2 and Ir3 were added to the cells at the concentrations of 10 µM, 25 µM, 50 µM, 75 µM, 100 µM, 125 µM, and 150 µM and incubated for 24 hours at 37°C, 5% CO2. After that, the medium was replaced with the MTT reagent solution at a concentration of 0.5 mg/ml, according to the manufacturer's protocol (Alfa Aesar, Haverhill, MA, USA). After 4-hours incubation, the MTT reagent was replaced with a DMSO solution (100 µl per well) to dissolve the formazan crystals. Optical density was measured using a multimodal plate reader (Synergy Mx; BioTek Instruments, Winooski, VT, USA). For each well, the percentage of viable cells relative to the control was determined. For each concentration of the complex, 3 replications of 10 wells were performed.

Laser scanning microscopy. The studies were carried out on the LSM 880 (Carl Zeiss, Berlin, Germany) equipped with a PLIM module based on time-correlated single photon counting TCSPC (Becker&Hickl GmbH, Germany), and a Mai-Tai femtosecond Ti:Sa laser (Spectra Physics, Milpitas, CA, USA) with a pulse repetition rate of 80 MHz and a duration of 120 fs. All images were obtained using a water-immersion lens C-Apochromat 40×/1.2 NA.

In cellular accumulation and distribution assays, the phosphorescence of the Ir1 and Ir2 complexes was excited in one-photon mode at a wavelength of 405 nm using a pulse diode laser, and the emission was detected in the range of 600–740 nm. The intensity images were obtained after incubation of CT26 cells with the 75 µM solutions of the complexes for 1, 2, 3, 4, 5 and 24 hours. Before imaging, cells were washed with PBS and placed in FluoroBright DMEM (Thermo Fisher Scientific, USA) containing 10% FBS (Gibco, Carlsbad, CA, USA). Cells without the complexes were used as a control. The emission intensity of the complexes was measured in the cytoplasm of individual cells using ROI option in ImageJ software (National Institutes of Health, Bethesda, MY, USA).

Cell organelles were stained with LysoTracker Yellow HCK-123 (Thermo Fisher Scientific, Waltham, MA, USA) and MitoTracker 405 Blue (Thermo Fisher Scientific, Waltham, MA, USA). Cells were incubated with 75 μM solutions of the Ir1 and Ir2 for 3 hours, washed with PBS and then stained with the organelle-specific dyes (LysoTracker:  3 μM, 1 hour incubation; MitoTracker: 50 nM, 15 minutes incubation), according to the manufacturer’s protocols.

The fluorescence of LysoTracker was excited at a wavelength of 488 nm and detected in the range of 520–570 nm, that of MitoTracker - at 405 nm and at 420–470 nm, phosphorescence of complexes – at 405 nm and detected in the range 600-740 nm, correspondingly. Images of cells in transmitted light channel were recorded to observe cell morphology. The colocalization of the Ir1 and Ir2 complexes and organelle-specific dyes was assessed using the Jacob plugin in ImageJ to determine the Pearson’s (P) and Manders’(M1) colocalization coefficients.

PLIM in vitro and in vivo. Phosphorescence was excited at a wavelength of 750 nm (two-photon excitation) and detected in the range 495–690 nm. Laser power on a sample was 6 mW. The accumulation time of the phosphorescence signal was 120 s. The field of view was 256x256 µm in size.

For PLIM measurements, the cells were incubated with 75 μM of Ir1 and Ir2 for 3 hours in a CO2 incubator (37°C, 5% CO2). PLIM images were recorded in normoxic conditions in a stage top incubator (37°C, 5% CO2) or upon simulated hypoxia. To model hypoxia in vitro, a cover slip was placed on the monolayer of cancer cells for 1.5 hours[8]. PLIM images of 4-5 microscopic fields of view were recorded in each culture dish.

The protocol of PLIM in vivo was adopted from literature[9]. Briefly, the Ir1 sensor was injected locally into the tumor at a concentration of 250 µM 30 minutes before PLIM. A skin flap over the tumor was surgically opened in sterile conditions, the mouse was placed on a glass coverslip and the ear with a tumor was secured with surgical tape. The search of the regions of interest was performed by detecting cellular autofluorescence upon two-photon excitation at 750 nm, and signal registration at 450-490 nm. After focusing on the cell-rich area, the microscope was switched in PLIM mode. In a total, 5-7 PLIM images were obtained from each tumor.

Processing of the PLIM images was performed using SPCImage 8.5 software (Becker & Hickl GmbH, Germany). Monoexponential phosphorescence decay curve were approximated by the least squares method. Phosphorescence signal was analyzed in the cytoplasm of the individual cells by selecting the cell area without nucleus as a region of interest. For each tumor, 30-50 cells were analyzed. The average number of photons was 1500-2000 in a pixel, so that the binning factor 4 was applied to build a decay curve.

Histopathological analysis. To verify tumors, the tissue samples were embedded in paraffin and histological 7 μm thickness sections were obtained and stained with hematoxylin-eosin. Microscopic images of histological sections were taken using a Leica DFC290 microscope (Leica Microsystems, Wetzlar, Germany) at x20 magnification.

NMR and ESI HRMS data

Figure S1. 1H NMR spectrum of 6-(benzo[b]thiophen-2-yl)nicotinic acid, (CD3)2SO, 298 K.

Figure S2. 1H-1H COSY NMR spectrum of 6-(benzo[b]thiophen-2-yl)nicotinic acid, (CD3)2SO, 298 K.

Figure S3. ESI+ mass-spectrum of 6-(benzo[b]thiophen-2-yl)nicotinic acid ([M+H]+cation area), solvent – methanol.

Figure S4. 1H NMR spectrum of N^C, CDCl3, 298 K.

Figure S5. 1H-1H COSY NMR spectra of N^C, CDCl3, 298 K.

Figure S6. ESI+ mass-spectrum of N^C ([M+Na]+cation area), solvent – methanol.

Figure S7. 1H NMR spectrum of dissociated dimer [Ir2(N^C)4Cl2], (CD3)2SO, 298 K.

Figure S8. 1H-1H COSY NMR spectrum of dissociated dimer [Ir2(N^C)4Cl2], (CD3)2SO, 298 K.

Figure S9. ESI+ mass-spectrum of dissociated dimer ([Ir(N^C)2Cl+Na]+cation area), solvent – methanol.

Figure S10. 1H NMR spectrum of Ir1, CD3OD, 298 K.

Figure S11. 1H-1H COSY NMR spectrum of Ir1, CD3OD, 298 K.

Figure S12. ESI+ mass-spectrum of Ir1 ([M+Na]2+cation area), solvent – methanol.

Figure S13. 1H NMR spectrum of Ir2, CD3OD, 298 K.

Figure S14. 1H-1H COSY NMR spectrum of Ir2, CD3OD, 298 K.

Figure S15. ESI+ mass-spectrum of Ir2 ([M+Na]2+cation area), solvent – methanol.

Figure S16. 1H NMR spectrum of Ir3, CD3OD, 298 K. Peak assignments: * - CD3OD impurities.

Figure S17. 1H-1H COSY NMR spectrum of Ir3, CD3OD, 298 K.

Figure S18. ESI+ mass-spectrum of Ir3 ([M+Na]2+cation area), solvent – methanol.

Photophysical data

Table S1. Values of excitation state lifetime of complexes Ir1 and Ir2 in various aqueous media and at different oxygen concentrations. Excitation at 355 nm, T = 37°C, C(Complex) = 10 M.

| Complex | Water |  | 0.01M PBS |  | DMEM + 10% FBS |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | C(O2), M | , ns | C(O2), M | , ns | C(O2), M | , ns |
| Ir1 | 215 | 1238 | 205 | 1394 | 201 | 1433 |
|  | 169 | 1501 | 141 | 1939 | 128.4 | 1998 |
|  | 116 | 2004 | 92.9 | 2556 | 82.9 | 2815 |
|  | 91.1 | 2435 | 54.7 | 3690 | 31.8 | 5435 |
|  | 24.3 | 5453 | 28.4 | 5322 | 15.7 | 7236 |
|  | 1.04 | 10164 | 1.97 | 9971 | 2.92 | 9287 |
| Ir2 | 218 | 1524 | 208 | 1800 | 199 | 1904 |
|  | 192 | 1672 | 164 | 2113 | 140 | 2292 |
|  | 156 | 1935 | 121 | 2547 | 103 | 2803 |
|  | 103 | 2523 | 108 | 2701 | 61.5 | 3418 |
|  | 50.4 | 3481 | 15.5 | 4789 | 48.1 | 3735 |
|  | 1.1 | 5322 | 0.9 | 5341 | 2.8 | 5158 |

Computational data

Table S2. Calculated and experimental wavelength of emission maxima of complexes Ir1-Ir3

| Complex | Calculated wavelength, nm | Experimental wavelength, nm |
| --- | --- | --- |
| Ir1 | 625 | 632 |
| Ir2 | 646 | 638 |
| Ir3 | 683 | 655 |

Figure S19. Absorption spectra of Ir1: experimental (red) and calculated (black) lines with oscillator strengths of electronic transitions (bars).

Table S3. Calculated absorption maxima (λ) and oscillator strengths (f) of complex Ir1.

| Transitions | λabs, nm | f | Contribution of main NTO pair in transition (%) |
| --- | --- | --- | --- |
| S0-S5 | 261 | 0.088 | 66 |
| S0-S4 | 333 | 0.182 | 90 |
| S0-S3 | 380 | 0.209 | 95 |
| S0-S2 | 449 | 0.115 | 96 |
| S0-S1 | 504 | 0.002 | 97 |

Table S4. Natural transition orbitals (NTO) for Ir1-0, violet and terracotta colors show decrease and increase in electron density, respectively. The calculations have been simplified by substitution of OEG pendants of Ir1 complex for methyl groups in Ir1-0 structure. Atom colors: Ir–lilac; S–yellow; O–red; N–blue; C–gray, H–white. The data for the corresponding interfragment charge transfer (IFCT) are given below the figures. Diagonal values represent intraligand transitions, off-diagonal values represent a charge transfer from “Donor” to “Acceptor”.

| S0→S1 Donor; Acceptor. Ir; N^N; N^C; N^C’. Ir; 0.005; 0.177; 0.006; 0.002. N^N; 0.000; 0.011; 0.000; 0.000. N^C; 0.011; 0.408; 0.014; 0.004. N^C’; 0.009; 0.339; 0.012; 0.003. | S0→S2 Donor; Acceptor. Ir; N^N; N^C; N^C’. Ir; 0.007; 0.006; 0.176; 0.001. N^N; 0.000; 0.000; 0.011; 0.000. N^C; 0.015; 0.013; 0.407; 0.001. N^C’; 0.012; 0.011; 0.338; 0.001. |
| --- | --- |
| S0→S3 Donor; Acceptor. Ir; N^N; N^C; N^C’. Ir; 0.000; 0.000; 0.000; 0.004. N^N; 0.000; 0.000; 0.000; 0.005. N^C; 0.015; 0.010; 0.022; 0.414. N^C’; 0.018; 0.011; 0.026; 0.474. | S0→S4 Donor; Acceptor. Ir; N^N; N^C; N^C’. Ir; 0.005; 0.010; 0.011; 0.129. N^N; 0.001; 0.001; 0.002; 0.018. N^C; 0.002; 0.004; 0.005; 0.051. N^C’; 0.026; 0.050; 0.055; 0.629. |
| S0→S5 Donor; Acceptor. Ir; N^N; N^C; N^C’. Ir; 0.006; 0.020; 0.040; 0.169. N^N; 0.001; 0.003; 0.007; 0.028. N^C; 0.008; 0.030; 0.061; 0.257. N^C’; 0.009; 0.031; 0.064; 0.267. | T1→S0 Donor; Acceptor. Ir; N^N; N^C; N^C’. Ir; 0.004; 0.000; 0.030; 0.001. N^N; 0.002; 0.000; 0.013; 0.000. N^C; 0.104; 0.006; 0.813; 0.023. N^C’; 0.000; 0.000; 0.003; 0.000. |

Fig S20. Absorption spectra of Ir2: experimental (red) and calculated (black) lines with oscillator strengths of electronic transitions (bars).

Table S5. Calculated absorption maxima (λ) and oscillator strengths (f) of complex Ir2.

| Transitions | λabs, nm | f | Contribution of main NTO pair in transition (%) |
| --- | --- | --- | --- |
| S0-S5 | 254 | 0.145 | 32 |
| S0-S4 | 309 | 0.122 | 47 |
| S0-S3 | 382 | 0.283 | 84 |
| S0-S2 | 464 | 0.141 | 93 |
| S0-S1 | 513 | 0.004 | 95 |

Table S6. Natural transition orbitals (NTO) for Ir2-0, violet and terracotta colors show decrease and increase in electron density, respectively. The calculations have been simplified by substitution of OEG pendants of Ir2 complex for methyl groups in Ir2-0 structure. Atom colors: Ir–lilac; S–yellow; O–red; N–blue; C–gray, H–white. The data for the corresponding interfragment charge transfer (IFCT) are given below the figures. Diagonal values represent intraligand transitions, off-diagonal values represent a charge transfer from “Donor” to “Acceptor”.

| S0→S1 Donor; Acceptor. Ir; N^N; N^C; N^C’. Ir; 0.002; 0.177; 0.024; 0.004. N^N; 0.000; 0.031; 0.004; 0.001. N^C; 0.003; 0.376; 0.052; 0.008. N^C’; 0.002; 0.272; 0.037; 0.006. | S0→S2 Donor; Acceptor. Ir; N^N; N^C; N^C’. Ir; 0.008; 0.006; 0.065; 0.129. N^N; 0.001; 0.001; 0.011; 0.023. N^C; 0.016; 0.012; 0.137; 0.273. N^C’; 0.012; 0.009; 0.099; 0.198. |
| --- | --- |
| S0→S3 Donor; Acceptor. Ir; N^N; N^C; N^C’. Ir; 0.000; 0.013; 0.002; 0.001. N^N; 0.007; 0.652; 0.105; 0.041. N^C; 0.001; 0.103; 0.017; 0.007. N^C’; 0.000; 0.042; 0.007; 0.003. | S0→S4 Donor; Acceptor. Ir; N^N; N^C; N^C’. Ir; 0.003; 0.017; 0.039; 0.051. N^N; 0.005; 0.032; 0.075; 0.095. N^C; 0.006; 0.039; 0.090; 0.114. N^C’; 0.010; 0.068; 0.157; 0.198. |
| S0→S5 Donor; Acceptor. Ir; N^N; N^C; N^C’. Ir; 0.001; 0.068; 0.005; 0.007. N^N; 0.003; 0.378; 0.027; 0.039. N^C; 0.002; 0.235; 0.017; 0.024. N^C’; 0.001; 0.163; 0.012; 0.017. | T1→S0 Donor; Acceptor. Ir; N^N; N^C; N^C’. Ir; 0.005; 0.002; 0.030; 0.001. N^N; 0.006; 0.002; 0.037; 0.001. N^C; 0.113; 0.047; 0.709; 0.026. N^C’; 0.003; 0.001; 0.017; 0.001. |

Fig S21. Absorption spectra of Ir3: experimental (red) and calculated (black) lines with oscillator strengths of electronic transitions (bars).

Table S7. Calculated absorption maxima (λ) and oscillator strengths (f) of complex Ir3.

| Transitions | λabs, nm | f | Contribution of main NTO pair in transition (%) |
| --- | --- | --- | --- |
| S0-S5 | 279 | 0.432 | 42 |
| S0-S4 | 334 | 0.189 | 88 |
| S0-S3 | 378 | 0.231 | 92 |
| S0-S2 | 455 | 0.164 | 96 |
| S0-S1 | 601 | 0.002 | 98 |

Table S8. Natural transition orbitals (NTO) for Ir3-0, violet and terracotta colors show decrease and increase in electron density, respectively. The calculations have been simplified by substitution of OEG pendants of Ir3 complex for methyl groups in Ir3-0 structure. Atom colors: Ir–lilac; S–yellow; O–red; N–blue; C–gray, H–white. The data for the corresponding interfragment charge transfer (IFCT) are given below the figures. Diagonal values represent intraligand transitions, off-diagonal values represent a charge transfer from “Donor” to “Acceptor”.

| S0→S1 Donor; Acceptor. Ir; N^N; N^C; N^C’. Ir; 0.004; 0.195; 0.002; 0.002. N^N; 0.000; 0.010; 0.000; 0.000. N^C; 0.007; 0.379; 0.005; 0.004. N^C’; 0.007; 0.378; 0.005; 0.004. | S0→S2 Donor; Acceptor. Ir; N^N; N^C; N^C’. Ir; 0.007; 0.008; 0.055; 0.133. N^N; 0.000; 0.000; 0.003; 0.007. N^C; 0.013; 0.016; 0.106; 0.259. N^C’; 0.013; 0.016; 0.106; 0.258. |
| --- | --- |
| S0→S3 Donor; Acceptor. Ir; N^N; N^C; N^C’. Ir; 0.000; 0.000; 0.002; 0.002. N^N; 0.000; 0.000; 0.002; 0.002. N^C; 0.018; 0.026; 0.227; 0.215. N^C’; 0.019; 0.027; 0.236; 0.223. | S0→S4 Donor; Acceptor. Ir; N^N; N^C; N^C’. Ir; 0.008; 0.007; 0.072; 0.117. N^N; 0.001; 0.001; 0.011; 0.018. N^C; 0.011; 0.010; 0.106; 0.174. N^C’; 0.017; 0.015; 0.164; 0.267. |
| S0→S5 Donor; Acceptor. Ir; N^N; N^C; N^C’. Ir; 0.004; 0.278; 0.011; 0.011. N^N; 0.006; 0.409; 0.017; 0.016. N^C; 0.002; 0.107; 0.004; 0.004. N^C’; 0.002; 0.119; 0.005; 0.005. | T1→S0 Donor; Acceptor. Ir; N^N; N^C; N^C’. Ir; 0.004; 0.000; 0.009; 0.009. N^N; 0.183; 0.009; 0.385; 0.381. N^C; 0.002; 0.000; 0.004; 0.004. N^C’; 0.002; 0.000; 0.004; 0.004. |

Optimized structures data

Figure S22. Optimized structure of the model Ir2-0 complex (hydrogen atoms are omitted for clarity). The calculations have been simplified by substitution of OEG pendants in Ir2 complex for methyl groups in Ir2-0 structure. Atom colors: Ir–blue; S–yellow; O–green; N–red; C–gray.

Figure S23. Optimized structure of the model Ir3-0 complex (hydrogen atoms are omitted for clarity). The calculations have been simplified by substitution of OEG pendants in Ir3 complex for methyl groups in Ir3-0 structure. Atom colors: Ir–blue; S–yellow; O–green; N–red; C–gray.

Biological experiments data

Figure S24. MTT-assay for viability of HCT116 cells after incubation with complexes Ir1-Ir3. Mean ± SD. N = 3 repeats by 10 wells.

Figure S25. In vivo PLIM of human colorectal tumor HCT116 with the Ir1 complex. Representative microscopic images of cellular autofluorescence, Ir1 luminescence intensity, PLIM (Scale bar = 50 µm.) and Histological verification (Scale bar = 150 µm).

Table S9. The key structural parameters of complex Ir1-0 (R = NHMe) and its literature analog[10].

| Complex Ir1 |  |  |
| --- | --- | --- |
| Distances, A° |  |  |
| Ir-C1 | 2.006 | 2.040(6) |
| Ir-N1 | 2.076 | 2.074(5) |
| Ir-C2 | 2.002 | 2.049(6) |
| Ir-N2 | 2.068 | 2.070(5) |
| Ir-N3 | 2.116 | 2.093(5) |
| Ir-N4 | 2.152 | 2.130(5) |
| Angles, ° |  |  |
| N1-Ir-C1 | 80.59 | 80.1(2) |
| N2-Ir-C2 | 80.59 | 79.7(2) |
| N3-Ir-N4 | 76.05 | 77.52(19) |
| C1-Ir-C2 | 91.12 | 88.8(2) |
| C2-Ir-N1 | 99.13 | 100.0(2) |
| C2-Ir-N4 | 96.51 | 94.8(2) |
| C1-Ir-N2 | 98.73 | 97.4(2) |
| N2-Ir-N4 | 86.54 | 90.14(18) |
| N4-Ir-N1 | 94.18 | 92.4(2) |
| N3-Ir-N2 | 96.47 | 92.09(19) |
| N3-Ir-N1 | 83.89 | 88.54(19) |
| N3-Ir-C1 | 96.47 | 99.9(2) |
| N3-Ir-C2 | 172.21 | 168.8(2) |
| N2-Ir-N1 | 179.26 | 177.49(19) |
| C1-Ir-N4 | 171.37 | 172.1(2) |

Table S10. The key structural parameters of complex Ir2-0 (R = NHMe) and its literature analog[11].

| Complex Ir2 |  |  |
| --- | --- | --- |
| Distances, A° |  |  |
| Ir-C1 | 1.997 | 2.014(10) |
| Ir-N1 | 2.062 | 2.043(8) |
| Ir-C2 | 2.008 | 2.014(10) |
| Ir-N2 | 2.080 | 2.069(8) |
| Ir-N3 | 2.146 | 2.147(9) |
| Ir-N4 | 2.180 | 2.199(8) |
| Angles, ° |  |  |
| N1-Ir-C1 | 80.54 | 80.3(4) |
| N2-Ir-C2 | 80.05 | 79.9(4) |
| N3-Ir-N4 | 76.36 | 76.2(3) |
| C1-Ir-C2 | 88.11 | 85.3(4) |
| C2-Ir-N1 | 100.55 | 98.9(4) |
| C2-Ir-N4 | 98.82 | 102.3(3) |
| C1-Ir-N2 | 100.95 | 96.5(4) |
| N2-Ir-N4 | 81.54 | 87.4(3) |
| N4-Ir-N1 | 96.93 | 95.9(3) |
| N3-Ir-N2 | 93.00 | 95.5(3) |
| N3-Ir-N1 | 86.30 | 85.8(3) |
| N3-Ir-C1 | 96.88 | 96.3(4) |
| N3-Ir-C2 | 172.14 | 175.2(4) |
| N2-Ir-N1 | 178.43 | 176.7(4) |
| C1-Ir-N4 | 172.97 | 172.0(4) |

Table S11. The key structural parameters of complex Ir3-0 (R = NHMe) and its literature analog[12].

| Complex Ir3 |  |  |
| --- | --- | --- |
| Distances, A° |  |  |
| Ir-C1 | 2.010 | 2.013(5) |
| Ir-N1 | 2.073 | 2.052(4) |
| Ir-C2 | 2.010 | 2.018(5) |
| Ir-N2 | 2.073 | 2.055(4) |
| Ir-N3 | 2.130 | 2.122(4) |
| Ir-N4 | 2.131 | 2.112(4) |
| Angles, ° |  |  |
| N1-Ir-C1 | 80.41 | 80.48(19) |
| N2-Ir-C2 | 80.39 | 79.98(18) |
| N3-Ir-N4 | 77.24 | 76.89(16) |
| C1-Ir-C2 | 89.59 | 87.3(2) |
| C2-Ir-N1 | 99.73 | 98.30(18) |
| C2-Ir-N4 | 96.58 | 96.80(18) |
| C1-Ir-N2 | 99.66 | 96.29(18) |
| N2-Ir-N4 | 85.06 | 86.06(15) |
| N4-Ir-N1 | 94.86 | 97.26(16) |
| N3-Ir-N2 | 94.24 | 95.62(16) |
| N3-Ir-N1 | 85.64 | 86.41(16) |
| N3-Ir-C1 | 96.90 | 99.09(18) |
| N3-Ir-C2 | 172.22 | 172.62(18) |
| N2-Ir-N1 | 179.87 | 176.44(16) |
| C1-Ir-N4 | 172.81 | 175.55(18) |

References

[1]	M.J. Frisch, G.W. Trucks, H.B. Schlegel, G.E. Scuseria, M.A. Robb, J.R. Cheeseman, G. Scalmani, V. Barone, G.A. Petersson, X. Nakatsuji, H.; Li, M. Caricato, A. V. Marenich, J. Bloino, B.G. Janesko, R. Gomperts, B. Mennucci, H.P. Hratchian, J. V. Ortiz, A.F. Izmaylov, J.L. Sonnenberg, D. Williams-Young, F. Ding, F. Lipparini, F. Egidi, J. Goings, B. Peng, A. Petrone, T. Henderson, D. Ranasinghe, V.G. Zakrzewski, J. Gao, N. Rega, G. Zheng, W. Liang, M. Hada, M. Ehara, K. Toyota, R. Fukuda, J. Hasegawa, M. Ishida, T. Nakajima, Y. Honda, O. Kitao, H. Nakai, T. Vreven, K. Throssell, J. Montgomery, J. A., J.E. Peralta, F. Ogliaro, M.J. Bearpark, J.J. Heyd, E.N. Brothers, K.N. Kudin, V.N. Staroverov, T.A. Keith, R. Kobayashi, J. Normand, K. Raghavachari, A.P. Rendell, J.C. Burant, S.S. Iyengar, J. Tomasi, M. Cossi, J.M. Millam, M. Klene, C. Adamo, R. Cammi, J.W. Ochterski, R.L. Martin, K. Morokuma, O. Farkas, J.B. Foresman, D.J. Fox, Gaussian 16, Revision B.01, (2016).

[2]	A. Austin, G.A. Petersson, M.J. Frisch, F.J. Dobek, G. Scalmani, K. Throssell, A Density Functional with Spherical Atom Dispersion Terms, J. Chem. Theory Comput. 8 (2012) 4989–5007. https://doi.org/10.1021/ct300778e.

[3]	M. Dolg, U. Wedig, H. Stoll, H. Preuss, Energy‐adjusted ab initio pseudopotentials for the first row transition elements, J. Chem. Phys. 86 (1987) 866–872. https://doi.org/10.1063/1.452288.

[4]	J. Tomasi, B. Mennucci, R. Cammi, Quantum Mechanical Continuum Solvation Models, Chem. Rev. 105 (2005) 2999–3094. https://doi.org/10.1021/cr9904009.

[5]	N.M. O’boyle, A.L. Tenderholt, K.M. Langner, cclib: A library for package-independent computational chemistry algorithms, J. Comput. Chem. 29 (2008) 839–845. https://doi.org/https://doi.org/10.1002/jcc.20823.

[6]	R.L. Martin, Natural transition orbitals, J. Chem. Phys. 118 (2003) 4775–4777. https://doi.org/10.1063/1.1558471.

[7]	T. Lu, F. Chen, Multiwfn: A multifunctional wavefunction analyzer, J. Comput. Chem. 33 (2012) 580–592. https://doi.org/10.1002/jcc.22885.

[8]	J.R.W. Conway, S.C. Warren, D. Herrmann, K.J. Murphy, A.S. Cazet, C. Vennin, R.F. Shearer, M.J. Killen, A. Magenau, P. Mélénec, M. Pinese, M. Nobis, A. Zaratzian, A. Boulghourjian, A.M. Da Silva, G. del Monte-Nieto, A.S.A. Adam, R.P. Harvey, J.J. Haigh, Y. Wang, D.R. Croucher, O.J. Sansom, M. Pajic, C.E. Caldon, J.P. Morton, P. Timpson, Intravital Imaging to Monitor Therapeutic Response in Moving Hypoxic Regions Resistant to PI3K Pathway Targeting in Pancreatic Cancer, Cell Rep. 23 (2018) 3312–3326. https://doi.org/10.1016/j.celrep.2018.05.038.

[9]	Y.P. Parshina, A.D. Komarova, L.N. Bochkarev, T.A. Kovylina, A.A. Plekhanov, L.G. Klapshina, A.N. Konev, A.M. Mozherov, I.D. Shchechkin, M.A. Sirotkina, V.I. Shcheslavskiy, M. V Shirmanova, Simultaneous Probing of Metabolism and Oxygenation of Tumors In Vivo Using FLIM of NAD(P)H and PLIM of a New Polymeric Ir(III) Oxygen Sensor, Int. J. Mol. Sci. 23 (2022). https://doi.org/10.3390/ijms231810263.

[10]	P.-N. Lai, T.S. Teets, Ancillary Ligand Effects on Red-Emitting Cyclometalated Iridium Complexes, Chem. – A Eur. J. 25 (2019) 6026–6037. https://doi.org/https://doi.org/10.1002/chem.201900829.

[11]	A.I. Solomatina, K.M. Kuznetsov, V. V Gurzhiy, V. V Pavlovskiy, V. V Porsev, R.A. Evarestov, S.P. Tunik, Luminescent organic dyes containing a phenanthro[9,10-D]imidazole core and [Ir(N^C)(N^N)]+ complexes based on the cyclometalating and diimine ligands of this type, Dalt. Trans. 49 (2020) 6751–6763. https://doi.org/10.1039/D0DT00568A.

[12]	Y.-C. Huang, Z.-B. Li, H.-Q. Guo, D. Mu, H.-Y. Li, A.-D. Lu, T.-Y. Li, Synthesis, structures, photophysical properties, and theoretical study of four cationic iridium(III) complexes with electron-withdrawing groups on the neutral ligands, Inorganica Chim. Acta. 496 (2019) 119060. https://doi.org/https://doi.org/10.1016/j.ica.2019.119060.