Supplementary Tables

Table S1: Quality target product profile (QTPP) postulated for SNEDDS of Bedaquiline

| QTPP elements | Target | Justification |
| --- | --- | --- |
| Dosage form | SNEDDS | Selection of lipid-based solid self-nano emulsifying system helps in the oral bioavailability enhancement of poorly bioavailable drug, Bedaquiline. |
| Dosage type | Sustain release | Faster onset of action leading to enhanced therapeutic benefits. |
| Dosage strength | 5 mg | Unit dose of Bedaquiline incorporated in a single formulation of SNEDDS |
| Route of administration | Oral | Recommended route for delivery of Bedaquiline |
| Stability | 6 months of Accelerated and long-term stability studies | To maintain therapeutic potential of the drug during storage period |
| Container closure system | Airtight glass bottles | To protect against the degradation of the drug and lipids in the presence of atmospheric air. |
| Alternative methods of administration | Salt, polymorphs, solid dispersions, nano crystals, co-crystals, inclusion complexes | These systems can only improve the dissolution rate (but not the extent) of which may eventually lead only to enhancement in rate of oral adsorption. |
| Contraindications | None | None |

Abbreviations:  QTPP, quality target product profile; SNEDDS, self-nano emulsifying drug delivery system

Table S2: Critical quality attributes (CQAs) for SNEDDS of Bedaquiline and their justifications.

| CQAs | Target | Is this a CQA | Justification |
| --- | --- | --- | --- |
| Physical attributes colour | Acceptable to patient | No | Color, odor and appearance were not considered as critical, as these are not directly linked to patient efficacy and safety. |
| Odour and appearance | Acceptable to patient | No |  |
| Assay and content uniformity | 100% | No | SNEDDS being the homogenous dispersions containing drug solubilized in the blend of lipidic excipients, these variables were regarded as less critical. |
| Drug release | 100% | Yes | Drug release rate is important for fast absorption of the drug in blood; hence was regarded as highly critical. |
| Liquefaction time | Low | yes* | Lower value of liquefaction time is important for faster drug release from the dosage form. Thus, it was considered as critical. |
| Emulsification time | Low | yes* | Lower values of emulsification time help in ease of formation of nanoemulsion; hence was taken up as highly critical. |
| Globule size | <100nm | yes* | Smaller droplet size allows easy penetration through GI epithelial lining and paracellular pathways; hence was regarded as highly critical. |
| Mean dissolution time | Low | yes* | It is an indicator of faster and complete drug release solubilization of drug in the dissolution medium, thus taken up as highly critical. |
| PDI | Low | yes* | Highly important for achieving the therapeutically effectiveness he hence considered as highly critical. |

*CQAs considered as critical

Abbreviations:  CQAs, critical quality attributes; SNEDDS, self-nano emulsifying drug delivery system, PDI, polydispersity index

Table S3: Protocol of stability study

| Name of Product: BDQ-F-SNEDDS |  |  | Purpose of Study : New Formulation |  |
| --- | --- | --- | --- | --- |
| Batch Size : 100 ml |  |  | Batch No. : BDSND22 |  |
| Sr. No. | Storage Condition | Storage Period | Testing Frequency (Monthly) | Tests |
| 1. | 40 ± 2 ºC & 75 ± 5 % | 6 Months | 0 3 6 | Following test to be performed at all stations of both Accelerated and Long Term Studies. Physical Appearance Phase Separation Caking Size (nm) PDI % Entrapment Efficiency |
| 2. | 25 ± 2 ºC & 60 ± 5 % | Upto Shelf Life | 0 3 6 9 12 18 24 |  |

Abbreviations: BDQ-F-SNEDDS, Bedaquiline-fumarate-self-nano emulsifying drug delivery system, PDI, polydispersity index

Table S4: Responses to selected factors

| Run | Factor 1 A: Oil (%) | Factor 2 B: Smix (%) | Factor 3 C: Sonication time (sec) | Response 1 droplet size (nm) | Response 2 PDI | Response 3 Transmittance (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 30 | 50 | 30 | 125.9 | 0.21 | 93.6 |
| 2 | 10 | 50 | 60 | 94.3 | 0.168 | 98.5 |
| 3 | 20 | 60 | 60 | 95.2 | 0.237 | 97.8 |
| 4 | 20 | 50 | 45 | 89.8 | 0.21 | 96.9 |
| 5 | 20 | 60 | 30 | 83.1 | 0.19 | 97.2 |
| 6 | 10 | 50 | 30 | 86.7 | 0.176 | 97.8 |
| 7 | 10 | 60 | 45 | 78.4 | 0.16 | 98.9 |
| 8 | 30 | 60 | 45 | 119.1 | 0.236 | 94.4 |
| 9 | 10 | 40 | 45 | 90.25 | 0.11 | 97.3 |
| 10 | 20 | 40 | 30 | 97.5 | 0.153 | 95.6 |
| 11 | 30 | 40 | 45 | 130.5 | 0.325 | 93.1 |
| 12 | 30 | 50 | 60 | 135.7 | 0.449 | 93.9 |
| 13 | 20 | 40 | 60 | 105.6 | 0.331 | 96.4 |
| 14 | 20 | 50 | 45 | 88.5 | 0.2 | 96.8 |

Abbreviations: PDI, polydispersity index

Supplementary Figures

Figure S1: Ishikawa fishbone diagram illustrating a cause-and-effect relationship among the formulation and process variables for the formulation of SNEDDS.

Figure S2: Pseudoternary phase diagram showing different ratios of Smix 1:0, 1:1, 1:2, 2:1, 3:1, 4:1, 5:1

Figure S3: Linear correlation plot between observed and predicted values of droplet size, PDI and Transmittance and their corresponding residual plots.