Supporting Information

for

PEDOT:PSS versus Polyaniline: A Comparative Study of Conducting Polymers for Organic Electrochemical Transistors

Ryotaro Kawamura and Tsuyoshi Michinobu*

Department of Materials Science and Engineering, Tokyo Institute of Technology, 2-12-1 Ookayama, Meguro-ku, Tokyo 152-8552, Japan.

*E-mail: michinobu.t.aa@m.titech.ac.jp

General Measurements

A patterned electrode (BAS 0011598) was used as the substrate electrode of OECTs. A ultraviolet ozone cleaner (TECHNOVISION, INC. UV-208) was used to clean the substrate of OECTs. A spin coater used was MIKASA MS-B100. For thermal annealing, a digital hotplate of CORNING PC-400D was used. Output and transfer characteristics were measured using a parameter analyzer, KEITHLEY 4200A-SCS. Film thickness measurements were done with a surface prolifometer, KLA-Tencor D-100. Atomic force microscopy (AFM) was measured by using an SPI3800N and SPA300 with a stiff cantilever DF-20.

Supporting Tables

Table S1 Characteristics of OECTs based on PEDOT:PSS

| Sample | P1000-5s | P1500-5s | P2000-5s | P2500-5s | P3000-5s | P2000-0s | P2000-5min | P2000-15min | P2000-1h | P2000-18h |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ON Resistance [Ω] | 1400 | 1200 | 1160 | 1300 | 1470 | 940 | 1310 | 1350 | 1310 | 1080 |
| Resistivity [Ω・m] | 0.12 | 0.090 | 0.067 | 0.065 | 0.055 | 0.052 | 0.075 | 0.078 | 0.075 | 0.062 |
| Conductivity [S/m] | 8.16 ±0.23 | 11.1 ±0.4 | 15.0 ±1.6 | 15.4 ±1.4 | 18.1 ±1.7 | 19.3 ±1.7 | 13.3 ±1.4 | 12.9 ±1.4 | 13.3 ±1.4 | 16.1 ±1.8 |
| Thickness [nm] | 350 ±10 | 300 ±11 | 230 ±25 | 200 ±18 | 150 ±14 | 220 ±19 | 230 ±25 | 230 ±25 | 230 ±25 | 230 ±25 |

Table S2 Characteristics of OECTs based on PANI

| Sample | PA1000-5s | PA1500-5s | PA2000-5s | PA2500-5s | PA3000-5s | PA1500-0s | PAD1500-5s | PAD3000-5s | PAD1500-0s |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ON Resistance [Ω] | 2790 | 3380 | 3410 | 3750 | 3990 | 2920 | 3770 | 4710 | 4240 |
| Resistivity [Ω・m] | 1.10 ±0.04 | 1.13 ±0.03 | 0.96 ±0.03 | 0.98 ±0.03 | 0.98 ±0.03 | 0.83 ±0.01 | 0.91 ±0.06 | 0.99 ±0.02 | 1.29 ±0.02 |
| Conductivity [S/m] | 0.91 ±0.04 | 0.88 ±0.03 | 1.05 ±0.04 | 1.03 ±0.03 | 1.02 ±0.03 | 1.20 ±0.01 | 1.09 ±0.07 | 1.01 ±0.02 | 0.77 ±0.01 |
| Thickness [μm] | 1.57 ±0.06 | 1.34 ±0.04 | 1.12 ±0.04 | 1.04 ±0.03 | 0.98 ±0.03 | 1.14 ±0.01 | 0.97 ±0.06 | 0.84 ±0.02 | 1.22 ±0.02 |

Table S3 Surface roughness (Ra) of PEDOT:PSS films

| Sample | P1000-5s | P2000-5s | P3000-5s | P2000-0s | P2000-5min | P2000-15min | P2000-18h |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1μm2[nm] | 2.72 ±0.07 | 2.84 ±0.09 | 2.47 ±0.14 | 2.68 ±0.20 | 2.56 ±0.14 | 2.43 ±0.12 | 1.73 ±0.10 |
| 10μm2[nm] | 4.51 ±0.52 | 4.62 ±0.54 | 3.44 ±0.34 | 3.83 ±0.24 | 4.76 ±0.43 | 3.05 ±0.39 | 2.71 ±0.16 |

Table S4 Surface roughness (Ra) of PANI films

| Sample | PA1500-5s | PA3000-5s | PA1500-0s | PAD1500-5s | PAD3000-5s | PAD1500-0s |
| --- | --- | --- | --- | --- | --- | --- |
| 1μm2[nm] | 0.652 ±0.03 | 0.764 ±0.03 | 0.841 ±0.05 | 0.761 ±0.07 | 0.708 ±0.04 | 0.784 ±0.06 |
| 10μm2[nm] | 3.78 ±1.49 | 3.94 ±1.28 | 6.07 ±1.45 | 3.17 ±0.52 | 5.31 ±1.19 | 1.78 ±0.25 |