| Table S2 - Chemical composition of the powdered pastes of the ceramic fragments collected in the Almaraz archaeological site, obtained by XRF. Data are presented as wt.% for major and minor constituents and ppm for trace elements. (nd: not detected; nq: not quantified). |  |  | MgO | Al2O3 | SiO2 |  | P2O5 |  | K2O | CaO |  | TiO2 | Fe2O3 | Mn |  | V | Cr |  | Ni | Cu |  | Zn |  | As | Rb |  | Sr |  | Zr | Nb |  | Pb | (SiO2+Al2O3+K2O)/CaO |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Red Slip Tableware |  | RS1 | 1.2 | 16.9 | 65.2 |  | nd/nq |  | 4.8 | 2.2 |  | 1.3 | 8.4 | nd/nq |  | 269 | 182 |  | nd/nq | 52 |  | 178 |  | 23 | 115 |  | 67 |  | 249 | 24 |  | 47 | 40 |  |  |  |
|  |  | RS2 | nd/nq | 18.2 | 64.6 |  | nd/nq |  | 4.6 | 2.5 |  | 1.3 | 8.6 | nd/nq |  | 378 | 270 |  | 412 | 114 |  | 266 |  | 43 | 118 |  | 115 |  | 282 | 33 |  | 70 | 35 |  |  |  |
|  |  | RS3 | nd/nq | 14.1 | 71.2 |  | 0.4 |  | 3.6 | 2.6 |  | 0.9 | 6.7 | nd/nq |  | 213 | 132 |  | 2571 | 66 |  | 138 |  | 48 | 88 |  | 94 |  | 258 | 20 |  | 61 | 34 |  |  |  |
|  |  | RS4 | 1.4 | 14.5 | 64.9 |  | nd/nq |  | 4.6 | 5.4 |  | 1.2 | 7.9 | nd/nq |  | 240 | 159 |  | 281 | 134 |  | 219 |  | nd/nq | 91 |  | 107 |  | 206 | 24 |  | 59 | 16 |  |  |  |
|  |  | RS5 | nd/nq | 13.5 | 56.8 |  | nd/nq |  | 4.1 | 15.4 |  | 1.3 | 8.8 | nd/nq |  | 225 | 201 |  | nd/nq | 75 |  | 191 |  | 22 | 78 |  | 225 |  | 197 | 24 |  | 54 | 5 |  |  |  |
|  |  | RS6 | 1.6 | 17.8 | 63.0 |  | nd/nq |  | 4.7 | 2.5 |  | 1.3 | 9.0 | nd/nq |  | 273 | 209 |  | nd/nq | 93 |  | 215 |  | 33 | 101 |  | 86 |  | 217 | 22 |  | 39 | 34 |  |  |  |
|  |  | RS7 | 1.2 | 16.8 | 65.2 |  | nd/nq |  | 4.6 | 2.3 |  | 1.3 | 8.6 | nd/nq |  | 271 | 203 |  | nd/nq | 55 |  | 163 |  | 25 | 87 |  | 71 |  | 188 | 18 |  | 31 | 38 |  |  |  |
|  |  | RS8 | 1.6 | 20.0 | 60.4 |  | nd/nq |  | 4.9 | 2.4 |  | 1.4 | 9.0 | nd/nq |  | 482 | 284 |  | 301.3 | 133 |  | 315 |  | 38 | 124 |  | 90 |  | 295 | 26 |  | 59 | 36 |  |  |  |
| Dercorated Ceramics |  | DC 1 | 1.3 | 17.4 | 60.8 |  | nd/nq |  | 4.4 | 5.7 |  | 1.3 | 9.0 | nd/nq |  | 321 | 251 |  | 196 | 63 |  | 216 |  | nd/nq | 102 |  | 130 |  | 234 | 23 |  | 42 | 15 |  |  |  |
|  |  | DC 2 | 1.2 | 19.6 | 61.5 |  | nd/nq |  | 4.9 | 2.0 |  | 1.4 | 9.2 | nd/nq |  | 356 | 289 |  | nd/nq | 132 |  | 276 |  | 33 | 118 |  | 100 |  | 245 | 27 |  | 51 | 43 |  |  |  |
|  |  | DC 3 | 1.5 | 17.4 | 65.1 |  | 0.2 |  | 4.5 | 1.9 |  | 1.3 | 7.8 | nd/nq |  | 263 | 172 |  | nd/nq | 56 |  | 178 |  | 27 | 113 |  | 84 |  | 287 | 26 |  | 35 | 45 |  |  |  |
|  |  | DC 4 | 1.8 | 18.4 | 63.1 |  | 0.2 |  | 4.9 | 1.6 |  | 1.3 | 8.5 | nd/nq |  | 363 | 213 |  | 204 | 110 |  | 204 |  | 37 | 112 |  | 58 |  | 231 | 23 |  | 41 | 55 |  |  |  |
| Yellow Slip Tableware |  | YS 1 | 1.4 | 14.9 | 58.1 |  | 0.0 |  | 4.4 | 10.0 |  | 1.4 | 9.5 | nd/nq |  | 288 | 234 |  | 410 | 73 |  | 217 |  | 24 | 97 |  | 191 |  | 226 | 29 |  | 41 | 8 |  |  |  |
|  |  | YS 2 | 1.5 | 14.1 | 59.8 |  | 0.0 |  | 4.3 | 9.7 |  | 1.3 | 9.1 | nd/nq |  | 280 | 213 |  | 205 | nd/nq |  | 173 |  | 26 | 81 |  | 155 |  | 187 | 23 |  | 36 | 8 |  |  |  |
|  |  | YS 3 | 0.0 | 17.3 | 50.4 |  | 0.2 |  | 3.2 | 16.7 |  | 1.5 | 10.3 | 509 |  | 519 | 430 |  | 812 | 204 |  | 234 |  | 58 | 76 |  | 509 |  | 219 | 32 |  | 45 | 4 |  |  |  |
|  |  | YS 4 | 1.6 | 15.2 | 53.2 |  | 0.3 |  | 3.1 | 15.9 |  | 1.3 | 9.1 | 352 |  | 399 | 288 |  | 318 | 92 |  | 151 |  | 43 | 61 |  | 388 |  | 191 | 22 |  | 37 | 5 |  |  |  |
| Grey Tableware |  | G 1 | nd/nq | 16.5 | 66.5 |  | nd/nq |  | 5.0 | 1.9 |  | 1.3 | 8.6 | nd/nq |  | 248 | 190 |  | 360 | 47 |  | 209 |  | nd/nq | 110 |  | 60 |  | 262 | 25 |  | 63 | 47 |  |  |  |
|  |  | G 2 | nd/nq | 17.5 | 65.4 |  | nd/nq |  | 5.1 | 1.8 |  | 1.4 | 8.7 | nd/nq |  | 311 | 222 |  | 318 | 56 |  | 216 |  | nd/nq | 105 |  | 56 |  | 236 | 23 |  | 59 | 49 |  |  |  |
|  |  | G 3 | 1.5 | 14.5 | 68.4 |  | 0.4 |  | 2.8 | 2.9 |  | 1.1 | 8.1 | 793 |  | 249 | 162 |  | 1086 | 52 |  | 140 |  | 41 | 56 |  | 111 |  | 253 | 18 |  | 41 | 29 |  |  |  |
|  |  | G 4 | 1.2 | 14.4 | 68.2 |  | 0.6 |  | 2.8 | 3.0 |  | 1.1 | 8.3 | 723 |  | 241 | 184 |  | 970 | 53 |  | 137 |  | 55 | 64 |  | 150 |  | 257 | 23 |  | 41 | 29 |  |  |  |
|  |  | G 5 | nd/nq | 17.9 | 58.9 |  | 0.3 |  | 4.9 | 3.2 |  | 1.3 | 13.3 | nd/nq |  | 249 | 188 |  | 126 | 73 |  | 187 |  | 58 | 79 |  | 89 |  | 159 | 15 |  | 32 | 26 |  |  |  |
|  |  | G 6 | 1.4 | 20.3 | 57.3 |  | 0.3 |  | 5.2 | 3.1 |  | 1.4 | 10.6 | nd/nq |  | 521 | 352 |  | 189 | 149 |  | 334 |  | 69 | 99 |  | 99 |  | 177 | 23 |  | 58 | 26 |  |  |  |
| Table S2 - Continued. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

|  |  | MgO | Al2O3 | SiO2 | P2O5 | K2O | CaO | TiO2 | Fe2O3 | Mn | V | Cr | Ni | Cu | Zn | As | Rb | Sr | Zr | Nb | Pb | (SiO2+Al2O3+K2O)/CaO |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Handmade Ceramics | H 1 | nd/nq | 14.3 | 63.9 | nd/nq | 4.4 | 3.2 | 0.9 | 13.0 | 395 | 222 | 195 | 1189 | 108 | 200 | 43 | 83 | 146 | 166 | 17 | 34 | 26 |
|  | H 2 | 1.9 | 15.3 | 63.7 | 0.3 | 1.2 | 4.9 | 0.9 | 11.5 | 490 | 289 | 519 | 430 | 89 | 63 | 42 | 22 | 244 | 104 | 15 | 17 | 16 |
|  | H 3 | 1.7 | 16.9 | 52.5 | 0.4 | 1.7 | 6.6 | 4.6 | 15.2 | 1304 | 610 | 501 | nd/nq | 68 | 125 | 41 | 19 | 351 | 220 | 58 | nd/nq | 11 |
|  | H 4 | 1.3 | 18.4 | 63.1 | 0.3 | 5.0 | 1.2 | 1.3 | 9.3 | nd/nq | 299 | 194 | nd/nq | 53 | 175 | 26 | 118 | 76 | 253 | 29 | 45 | 72 |
| Common Tableware | C1 | nd/nq | 14.7 | 69.0 | nd/nq | 4.9 | 2.0 | 1.3 | 8.0 | nd/nq | 208 | 192 | nd/nq | 45 | 158 | 29 | 86 | 47 | 219 | 20 | 114 | 44 |
|  | C 2 | nd/nq | 13.4 | 68.3 | 0.23 | 3.7 | 6.2 | 1.2 | 6.9 | nd/nq | 205 | 134 | 225 | 57 | 102 | 37 | 61 | 68 | 327 | 20 | 76 | 14 |
|  | C 3 | 1.41 | 13.9 | 64.8 | 0.22 | 4.2 | 7.0 | 0.8 | 7.4 | nd/nq | 228 | 139 | 1715 | 94 | 184 | 26 | 84 | 126 | 183 | 22 | 76 | 12 |
|  | C 4 | 1.81 | 14.0 | 50.3 | nd/nq | 2.9 | 21.7 | 1.4 | 7.7 | nd/nq | 252 | 219 | 434 | 59 | 147 | nd/nq | 62 | 196 | 212 | 29 | 81 | 3 |
|  | C 5 | nd/nq | 14.0 | 60.4 | nd/nq | 3.0 | 14.0 | 1.2 | 7.3 | nd/nq | 209 | 150 | 228 | nd/nq | 110 | nd/nq | 50 | 133 | 185 | 23 | 25 | 6 |