Supporting Information

A Remarkable Impact of pH to the Thermoresponsive Properties of Alginate-Based Composite Hydrogels Incorporating P2VP-PEO Micellar Nanoparticles

Amalia Iliopoulou1, Zacharoula Iatridi1, Constantinos Tsitsilianis1,*

1Department of Chemical Engineering, University of Patras, 26500 Patras

Table S1. Molecular characteristics of the ALG-g-HG heterograft copolymer.

| ALG-g-HG heterograft copolymer |  |
| --- | --- |
| Molecular weight, Mw (g/mol) | 262,000 |
| Average number of P(NIPAM86-co-NtBAM14) chains per Alginate backbone | 3.5 |
| Average number of PNIPAM chains per Alginate backbone | 1.8 |

Table S2. Molecular characteristics of the P2VP-b-PEO copolymer.

| Composition* |  | Molecular weight** |  |
| --- | --- | --- | --- |
|  | (P2VP %moles) | Mn (g/mol) | Mw (g/mol) |
| P2VP block | - | 2583 | 2678 |
| P2VP-b-PEO | 9 | 13144 | 14384 |

*by 1H-NMR; ** by Size Exclusion Chromatography

Table S3. Characteristic factors of thermoresponsiveness at various pH for the pure ALG-g-HG copolymer.

Table S4. The hydrodynamic diameters of P2VP-b-PEO polymeric micelles obtained from the number- and volume- weighted distributions of the DLS analyses. Values are reported as the mean value of the peak size.

| Particle Size Distributions |  |  |
| --- | --- | --- |
| Diameter, nm |  |  |
| pH | Number-weighted | Volume-weighted |
| 7.4 | 20.03 | 22.38 |
| 5.4 | 28.92 | 33.73 |
| 3.5 | 3.21 | 3.50 |

Figure S1. Storage (G’) and loss (G”) modulus as a function of temperature of ALG-g-HG solutions (a) 5 wt% and (b) 4 wt%.

Figure S2. Zeta potential of aqueous P2VP‐b‐PEO (■) and ALG-g-HG (▲) solutions at different pH.

Figure S3. Storage (G’) and loss (G”) modulus as a function of temperature of 4 wt% ALG-g-HG hydrogels at (a) pH 4.5 and (b) pH 3.5.

Figure S4. Oscillatory strain sweep data at 1 Hz of the 4 wt% ALG-g-HG hydrogel at pH 4 and 37 oC.

Figure S5. pH dependence of complex viscosity (1Hz) at 37 oC. The data were extracted from the experiments of Figure 2 (heating ramp).