SUPPLEMENTARY INFORMATION

Eu3+:YF3 and Eu3+, Nd3+:YF3 nanoparticles for optical temperature sensing: the influence of annealing on temperature dependence of the spectral-kinetic characteristics

*Ekaterina I. Oleynikova1, Oleg. A. Morozov1,2, Stella L. Korableva1, and **Maksim S. Pudovkin1

1Kazan Federal University, Institute of physics, Department of quantum electronics and radiospectroscopy, 18 Kremlyovskaya str, Kazan, 420008, Russian Federation

2FRC Kazan Scientific Center of RAS, Sibirsky Trakt str. 10, 420029, Kazan, Russia

Corresponding author:

Ekaterina I. Oleynikova, kate15-05@mail.ru

Maksim S. Pudovkin, jaz7778@list.ru

Full postal address: 18th Kremlyovskaya street. Kazan 420008, Russian Federation, Institute of physics, Department of quantum electronics and radiospectroscopy, office 168

Keywords

Lifetime thermometry, Nd3+/Yb3+, Nd3+/Yb3+:YF3, down-conversion, optical temperature sensors, thermal expansion

YF3: Eu3+

Table  S1. The sample classification (the only “green” sample Eu3+ (2.5%), Nd3+(4.0%) :YF3 was chosen for further investigation

Figure 1. XRD patterns of YF3: Eu3+ (2.5 mol.%) nanoparticles before   and after  annealing in air (400 °C, 4 hours)

| (a) | (b) |
| --- | --- |
| Figure S2. Luminescence decay curves at 589.5 nm (5D0 – 7F1 transition) for YF3: Eu3+ (a) 2.5; b) 5.0 and c) 7.5 mol.%) samples annealed in air in the temperature range 80-320 K |  |

| (a) | (b) |
| --- | --- |
| (c) |  |

Figure S3.

Figure S4. The schematic representation of LIR choice