Title: Efficient bioprocess for mixed PET waste depolymerization using crude cutinase

Authors: Virender Kumar a, Reinhard Wimmer a, Cristiano Varrone a*

a Department of Chemistry and Bioscience, Aalborg University, Fredrik Bajers Vej 7H, 9220 Aalborg, Denmark

*Corresponding author:

Email: cva@bio.aau.dk  (C. Varrone)

Supplementary Information

S1.1. Calculations for mass balance and molar yield (%)

The complete hydrolysis of 100 g PET (molar mass of repeating unit C10H804 =192.16 g/mol) would yield 0.5204 mol of TPA and EG.

Moles of PET =100 g/192.16g/mol =0.5204 mol

Theoretical Mass of TPA =0.5204 mol*166.13 g/mol =86.45 g

Theoretical Mass of EG=0.5204 mol*62.07 g/mol =32.29 g

Molar yield (%) =Tolal yield obtained in actual hydrolysisTheoretical molar yieldX100   (Eq. A1)

S1.2. Polymer weight loss

The weight loss of the PET film and powder was measured. For this, the weight of the empty reaction tube and then the weight after the addition of the polymer was measured. After the enzymatic treatment, the reaction tubes were centrifuged at 10000 rpm for 10 min. The supernatant was transferred to a new vial. The residual film or powder was washed with water twice carefully. After washing, the tubes were lyophilized for 24 h at 0.1 bar. The weight of the tube was measured, and the polymer weight loss was calculated using the following formula:

Weight loss of PET %=(Initial weight-Final weight)Initial weight×100    (Eq. 2)

Table S1. Purification table of the enzymes produced in 1L of culture medium

|  | FastPETase (cytoplasmic, mg L-1) | LCC (Extracellular supernatant, mg L-1) | LCCICCG (Extracellular supernatant, mg L-1) |
| --- | --- | --- | --- |
| Total protein | 322 | 70 | 75 |
| Purified (HisTrap FF) | 26 | 35 | 32 |

Table S2. DSC analysis of different PET materials used in the study

|  | Sample code |  |  |  | Sample name | ΔHc melt (J/g) | ΔHc heat (J/g) | ΔHf (J/g) | ΔXc (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | F250A |  |  |  | PET 0.25 mm Amorphous | 25.7 | 26.5 | 140.1 | 0.6 |
|  | F250C |  |  |  | PET (0.25 mm) crystalline | 9.0 | 58.2 | 140.1 | 35.1 |
|  | P80A |  |  |  | PET powder cryo-milled (80 µm) | 33.32 | 46.48 | 140.1 | 9.3 |
|  | P750C |  |  |  | PET powder (50 µm) | 2.5 | 55.4 | 140.1 | 37.7 |
|  | P250C |  |  |  | PET powder (100 µm) | 2.8 | 55.0 | 140.1 | 37.2 |
|  | P250C |  |  |  | PET powder (250 µm) | 1.50 | 61.3 | 140.1 | 42.6 |
|  | P750A |  |  |  | PET powder (750 µm) | 16.2 | 39.5 | 140.1 | 16.6 |
|  |  |  |  |  | PET tray (<500 µm) | 19.8 | 42.1 | 140.1 | 15.9 |
|  |  |  |  |  | PET bottle (<500 µm) | 9.5 | 48.21 | 140.1 | 28 |

Table S3. Composition of Minimal salt medium (M9)

| Chemical | g L-1 |
| --- | --- |
| KH2PO4 | 15 |
| (NH4)2SO4 | 1 |
| KH2PO4 | 3 |
| NaCl | 5 |
| ZnCl2 | 0,1 |
| FeSO4·7H2O | 0,15 |
| CaCl2·2H2O | 0,02 |
| Followings autoclaved separately |  |
| Glycerol | 5 |
| MgSO4*7H2O | 3 |
| Mineral salt solution (composition below) | 3 mL L-1 |
| Al2(SO4)3·18H2O | 2 |
| CoSO4·6H2O | 0,75 |
| CuSO4·5H2O | 2,5 |
| H3BO3 | 0,5 |
| MnSO4·H2O | 24 |
| Na2MoO4·2H2O | 3 |
| NiSO4·3H2O | 2,5 |
| ZnSO4·7H2O | 15 |

Table S4. Different studies on enzyme production and PET degradation (Bioreactor scale)

| Enzyme used | Organisms | Scale (L) | Growth Medium | Crude/purified | Type of waste | Enzyme loading (mg g-1 PET) | Substrate loading (g L-1) | Depolymerization (%) | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| LCC ICCGDAQI | E. coli | 2 | LB/Autoinduction | Crude | PET fibers | 3 | 10 | 97.5 | [1] |
| LCC ICCG | E. coli | 1 | ZYM-5052 auto-induction medium | Purified | Recycled PET | 0.29 | 200 | 80 | [2] |
| LCC ICCG | E. coli | 0.25 | ZYM-5052 auto-induction medium | Purified | Postconsumer PET waste | 1 | 165 | 98 | [3] |
| FastPETase | E. coli | 0.25 | ZYM-5052 auto-induction medium | Purified | Postconsumer PET waste | 1 | 165 | 20 | [3] |
| HotPETase | E. coli | 0.25 | ZYM-5052 auto-induction medium | Purified | Postconsumer PET waste | 1 | 165 | 26 | [3] |
| PES-H1 | E. coli | 0.25 | ZYM-5052 auto-induction medium | Purified | Postconsumer PET waste | 1 | 165 | 80 | [3] |
| FastPETase | Pichia Pastoris | 10 | BMGY | Crude | PET | 2 | 5 | 90 | [4] |
| LCC ICCG | E. coli | 2 | Minimal medium | Crude | Post-consumer PET trays | 0.8 | 100 | 80 | This work |
| LCC ICCG | E. coli | 2 | Minimal medium | Crude | Post-consumer PET trays and bottles | 0.8 | 100 | 50 | This work |

Fig. S1 SDS PAGE analysis of LCC, and LCCICCG. Lanes contain different samples and are named as follows: Blank (B), purified LCC (L1), ICCG crude (I1 and I2), ICCG purified and concentrated (I3, I4), and protein marker (M). The proteins appear as a single band (LCC 29.9 kDa) with an actual molecular weight of 29.0 kDa, and (LCCICCG 27.2 kDa) with an actual molecular weight of 28.6 kDa. The gels were prepared twice with the gel shown representative of the set.

Fig. S2. Depolymerization (MHET and TPA release) of PET film (F250A) by (a) FastPETase, (b) LCC, and (c) LCCICCG in different buffers. The reaction mixture contained 50 mM of each buffer with different pH, 13 g L-1 PET film at 0.5 mg g-1 PET enzyme loading. It was incubated for 96 h at the respective optimum temperature of the enzymes i.e., 50℃ (FastPETase), 65℃ (LCC), and LCCICCG (72℃) without any pH control.

Fig. S3. Depolymerization (Weight loss and monomer release) of PET film (F250A) by (a) FastPETase, (b) LCC, and (c) LCCICCG. The reaction mixture contained 50 mM KH2PO4-NaOH buffer (pH 8.0), 13 g L-1 PET film at 0.5, 1 mg g-1 PET enzyme loading respectively at different temperatures (30, 40, 50, 65, 72, 80℃) without any pH control and incubated for 96 h.

Fig. S4. Thermostability analysis of FastPETase, LCC, and LCCICCG at 50, 65, and 72℃. For the stability analysis, 2 µM enzyme was incubated at the respective temperatures for 36 h, and the residual activity was measured after different time intervals using pNPB assay in 50 mM phosphate-NaOH buffer (pH 8.0).

Fig. S5. 1H-NMR (quantitative) spectra of supernatant after treatment of PET film with crude supernatant. The concentration of different compounds analyzed in the sample is presented in the tabular form.

Fig. S6. 1H-NMR (quantitative) spectra of supernatant after treatment of PET film with purified enzyme. The concentration of different compounds analyzed in the sample is presented in tabular form. The large peaks between 3.5.3.8 ppm belong to glycerol, which is a part of the concentrated protein solution.

Fig. S7. Mixed PET waste used in the present study

Fig. S8. 1H-NMR (quantitative) spectra of supernatant after treatment of MW1 with crude supernatant.

Fig. S9. 1H-NMR (quantitative) spectra of supernatant after treatment of MW2 with crude supernatant.

Fig. S10. DSC analysis of different PET materials

Amino acid sequences

>FastPETase

MQTNPYARGPNPTAASLEASAGPFTVRSFTVSRPSGYGAGTVYYPTNAGGTVGAIAIVPGYTARQSSIKWWGPRLASHGFVVITIDTNSTLDQPESRSSQQMAALRQVASLNGTSSSPIYGKVDTARMGVMGWSMGGGGSLISAANNPSLKAAAPQAPWHSSTNFSSVTVPTLIFACENDSIAPVNSSALPIYDSMSQNAKQFLEIKGGSHSCANSGNSNQALIGKKGVAWMKRFMDNDTRYSTFACENPNSTAVSDFRTANCSLELEHHHHHH

>LCC

MSNPYQRGPNPTRSALTADGPFSVATYTVSRLSVSGFGGGVIYYPTGTSLTFGGIAMSPGYTADASSLAWLGRRLASHGFVVLVINTNSRFDYPDSRASQLSAALNYLRTSSPSAVRARLDANRLAVAGHSMGGGGTLRIAEQNPSLKAAVPLTPWHTDKTFNTSVPVLIVGAEADTVAPVSQHAIPFYQNLPSTTPKVYVELDNASHFAPNSNNAAISVYTISWMKLWVDNDTRYRQFLCNVNDPALSDFRTNNRHCQLEHHHHHH

>ICCG

MSNPYQRGPNPTRSALTADGPFSVATYTVSRLSVSGFGGGVIYYPTGTSLTFGGIAMSPGYTADASSLAWLGRRLASHGFVVLVINTNSRFDGPDSRASQLSAALNYLRTSSPSAVRARLDANRLAVAGHSMGGGGTLRIAEQNPSLKAAVPLTPWHTDKTFNTSVPVLIVGAEADTVAPVSQHAIPFYQNLPSTTPKVYVELCNASHIAPNSNNAAISVYTISWMKLWVDNDTRYRQFLCNVNDPALCDFRTNNRHCQLEHHHHHH

References

- S. Fritzsche, H. Hübner, M. Oldiges, and K. Castiglione, Comparative evaluation of the extracellular production of a polyethylene terephthalate degrading cutinase by Corynebacterium glutamicum and leaky Escherichia coli in batch and fed-batch processes. Microbial cell factories, 23 (2024) 274. https://doi.org/10.1186/s12934-024-02547-2

- Y.V. Soong, U. Abid, A.C. Chang, C. Ayafor, A. Patel, J. Qin, J. Xu, C. Lawton, H.W. Wong, M.J. Sobkowicz, and D. Xie, Enzyme selection, optimization, and production toward biodegradation of post-consumer poly(ethylene terephthalate) at scale. Biotechnol J, 18 (2023) e2300119. https://doi.org/10.1002/biot.202300119

- G. Arnal, J. Anglade, S. Gavalda et al., Assessment of Four Engineered PET Degrading Enzymes Considering Large-Scale Industrial Applications. ACS Catal. 26, (2023) 13156-13166. 10.1021/acscatal.3c02922. https://doi.org/10.1021/acscatal.3c02922

- C.C. Chen, X. Li, J. Min, Z.  Zeng, Z. Ning, H. He et al., Complete decomposition of poly (ethylene terephthalate) by crude PET hydrolytic enzyme produced in Pichia pastoris. Chem. Eng. J. 48, (2024) 148418. https://doi.org/10.1016/j.cej.2023.148418