Supporting Information

Synergistic Cs/P Co-doping in Tubular g-C3N4 for Enhanced Photocatalytic Hydrogen Evolution

Juanfeng Gao, Xiao Lin*, Bowen Jiang, Haiyan Zhang, Youji Li*

National Experimental Teaching Demonstration Center for Chemistry, College of Chemistry and Chemical Engineering, Jishou University, Jishou 416000, PR China

2.3 Material Characterizations and Photocatalytic (Photoelectrochemical) Tests

# 2.3.1 Material Characterizations

# The surface morphology of the photocatalysts was examined using scanning electron microscopy (SEM, ZEISS SIGMA-500) and transmission electron microscopy (TEM, JEOL JEM-2100), acceleration voltage of 20 kV. Elemental composition was analyzed by energy-dispersive X-ray spectroscopy (EDX, JED-2300T) at an accelerating voltage of 20 kV. Fourier-transform infrared spectroscopy (FTIR, Nicolet IS10) was employed to identify surface functional groups, and the crystal structure was determined by X-ray diffraction (XRD, Bruker D8). The chemical states of the elements were characterized using X-ray photoelectron spectroscopy (XPS, Thermo Fisher ESCALAB 250xi), 284.8 eV was used as an exogenous carbon correction peak. UV-visible diffuse reflectance spectra (DRS, Shimadzu UV-2600) were recorded with BaSO4 as the reference material. Photoluminescence (PL) emission spectra were obtained using a fluorescence spectrophotometer (Jasco FP-8300).

# 2.3.2 Photoelectrochemical Measurement

Photoelectrochemical measurements were conducted using a standard three-electrode system on a CHI 650E electrochemical workstation, with 0.1 M sodium sulfate solution serving as the electrolyte. The working electrode was prepared by dispersing the photocatalyst (10.0 mg) in a mixture of ethanol (1.00 mL) and Nafion (20 μL), followed by 30 minutes of ultrasonication. The resulting dispersion was uniformly coated onto fluorine-doped tin oxide (FTO) glass and dried in an oven at 60 °C. A platinum wire and an Ag/AgCl electrode were used as the counter and reference electrodes, respectively. Photocurrent measurements were performed under visible light irradiation for 300 seconds using a 300 W xenon lamp. Electrochemical impedance spectroscopy (EIS) was conducted within a frequency range of 0.01 Hz to 100 kHz under the same three-electrode setup. The open circuit voltage was used as the reference for parameterization. Mott-Schottky plots were recorded at an AC voltage amplitude of 5 mV with frequencies of 500 and 1000 Hz.

# 2.3.3 Photocatalytic Hydrogen Experiments

Typically, 20 mg of catalyst was dispersed in 50 mL of an aqueous methanol solution (CH3OH, 20 vol%), with 1% K2PtCl6 added as a co-catalyst deposited onto the catalytic material. The reaction system was then degassed for 30 min and irradiated using a 300 W xenon lamp equipped with a 400 nm cutoff filter. The photocatalytic reaction was conducted under a constant-temperature circulating water bath (10 ± 0.5°C). The amount of H2 generated during the reaction was monitored using a gas chromatograph (GC-7920, TCD detector, high-purity N2 as carrier gas).

Hydrogen volume was quantified via the gas chromatography system, and the amount of evolved hydrogen was calculated based on a calibration curve (Figure S1) to determine hydrogen production yield and rate.

Fig S1. H2 calibration curve

Under identical illumination conditions to those employed in the hydrogen evolution experiments, the apparent quantum efficiency (AQE) of hydrogen evolution for each catalyst was investigated1.

AQY(%)=2×Number of evolved H2 coleculesNumber of incident photons×100%

=2×C×NAS×P×t×λh×c×100%

# Where, C is the H2 production amount (mol) per hour; NA is the Avogadro constant (6.02×1023 mol−1); S is the irradiation area (cm2); P is the monochromatic light intensity (W⋅cm−2); t is the light irradiation time (s); λ is the wavelength of the monochromatic light (nm); h is the Plank constant (6.626×10−34 J⋅s); c is the speed of light (3×108 m⋅s−1).

3 Results and discussion

# 3.1 Elemental and Structural Analysis

Table S1. The elemental percentages in Cs/PTCN-3 were determined via Energy Dispersive X-ray Spectroscopy.

| Elemental | C | N | P | Cs |
| --- | --- | --- | --- | --- |
| Atom% | 64.18 | 33.91 | 0.03 | 1.88 |

Fig.S2 (a)BJH pore size distribution from adsorption branch, (b)surface area of PTCN and Cs/PTCN-3

# 3.2 Evaluation of Photocatalytic Hydrogen Evolution Performance

Fig.S3 Comparison of hydrogen evolution performance via photocatalytic water splitting with other catalytic systems reported in the literature2-17.

References

(1) Li, Z. Y.; Chen, Y. G.; Zhang, Y. H.; et al. Tuning interfacial charge transfer for efficient visible-light-driven photodegradation and simultaneous H2 evolution. Journal of Materials Science & Technology 2024, 168, 35-49. DOI: 10.1016/j.jmst.2023.05.033.

(2) Tahereh, M. S.; Hossein, F.; Byeong Kyu, L.; et al. Caesium sites coordinated in Boron-doped porous and wrinkled graphitic carbon nitride nanosheets for efficient charge carrier separation and Transfer: Photocatalytic H2 and H2O2 production. Chemical Engineering Journal 2021, 423, 130067. DOI: 10.1016/j.cej.2021.130067.

(3) Jang, D.; Lee, S.; Kwon, N. H.; et al. Preparation of carbon nitride nanotubes with P-doping and their photocatalytic properties for hydrogen evolution. Carbon 2023, 208, 290-302. DOI: 10.1016/j.carbon.2023.03.038.

(4) Li, G. Q.; Liang, H. O.; Fan, X. Y.; et al. Modulating and optimizing 2D/2D Fe-Ni2P/ZnIn2S4 with S vacancy through surface engineering for efficient photocatalytic H2 evolution. Journal of Materials Chemistry A 2023, 11 (27), 14809-14818. DOI: 10.1039/d3ta02519e.

(5) Zhang, H. H.; Liu, Z.; Fang, J. Z.; et al. Modulation of π‐Electron Density in Ultrathin 2D Layers of Graphite Carbon Nitride for Efficient Photocatalytic Hydrogen Production. Small 2024, 20 (47), 2404929. DOI: 10.1002/smll.202404929.

(6) Dai, W.; Wang, R. H.; Chen, Z. J.; et al. Highly-efficient photocatalytic hydrogen evolution triggered by spatial confinement effects over co-crystal templated boron-doped carbon nitride hollow nanotubes. Journal of Materials Chemistry A 2023, 11 (14), 7584-7595. DOI: 10.1039/d3ta00199g.

(7) Zhao, S.; Liu, Y. P.; Wang, Y. Y.; et al. Carbon and Phosphorus Co-doped Carbon Nitride Hollow Tube for Improved Photocatalytic Hydrogen Evolution. Journal of Colloid and Interface Science 2022, 616, 152-162. DOI: 10.1016/j.jcis.2022.02.057.

(8) Chen, M. H.; Xiong, J.; Li, X. Y.; et al. In-situ doping strategy for improving the photocatalytic hydrogen evolution performance of covalent triazine frameworks. Science China Chemistry 2023, 66 (8), 2363-2370. DOI: 10.1007/s11426-023-1624-7.

(9) Wang, H. T.; Jiang, J. Z.; Yu, L. L.; et al. Tailoring Advanced N-Defective and S-Doped g-C3N4 for Photocatalytic H2  Evolution. Small 2023, 19 (28), 2301116. DOI: 10.1002/smll.202301116.

(10) Pang, Y. Y.; Li, L. J.; Bu, Q. J.; et al. Stimulating Protonation Capability by Eliminating Detrimental Defects in Crystalline Carbon Nitride for Photocatalytic Hydrogen Evolution. Advanced Functional Materials 2025, 2501108. DOI: 10.1002/adfm.202501108.

(11) Wu, Y. H.; Yan, Y. Q.; Deng, Y. X.; et al. Rational construction of S-scheme CdS quantum dots/In2O3 hollow nanotubes heterojunction for enhanced photocatalytic H2 evolution. Chinese Journal of Catalysis 2025, 70, 333-340. DOI: 10.1016/s1872-2067(24)60213-5.

(12) Wang, X. H.; Xue, S.; Shi, T. Y.; et al. Localized Phosphorization Manipulating Internal Electric Field Orientation in Carbon Nitride Homojunction for Efficient Photocatalytic Hydrogen Evolution. Advanced Functional Materials 2025, 2424853 DOI: 10.1002/adfm.202424853.

(13) Xing, W. N.; Shao, W. F.; Li, Y. F.; et al. Rapid Charge Transfer Endowed by Heteroatom Doped Z-Scheme Van Der Waals Heterojunction for Boosting Photocatalytic Hydrogen Evolution. Small 2025, 21 (10), 2412036. DOI: 10.1002/smll.202412036.

(14) Zhang, D. L.; Zhang, C.; Zhao, G. F.; et al. Single-atom Pt supported on defective graphitic carbon nitride for efficient photocatalytic hydrogen production. Chemical Engineering Journal 2025, 505, 159567. DOI: 10.1016/j.cej.2025.159567.

(15) Fan, Z. Y.; Xu, Q. H.; Wang, Y. Q.; et al. Electron regulation accelerates photocatalytic hydrogen evolution for bimetallic Pt, Au on CdS nanorods. Chemical Engineering Journal 2025, 511, 162016. DOI: 10.1016/j.cej.2025.162016.

(16) Zhang, C.; Hu, S.; Cui, W. G.; et al. Integrating photocatalytic hydrogen evolution with antibiotic degradation over a dual Z-scheme heterojunction. Chemical Engineering Journal 2025, 510, 160317. DOI: 10.1016/j.cej.2025.160317.

(17) Wang, W. B.; Liu, J.; Cui, M. X.; et al. Z-type ZnIn2S4 homojunction for high performance photocatalytic hydrogen evolution. Chemical Engineering Journal 2025, 507, 160370. DOI: 10.1016/j.cej.2025.160370.