Supplementary File

TS 1. List of conductive additives.

| Conductive Additive | Purpose |
| --- | --- |
| Super-P 80% | Used primarily in battery applications to enhance the conductivity of the electrode material. |
| Silver flakes and graphene nanoplatelets | Combine to provide high electrical conductivity and mechanical strength in composites and inks. |
| rGO (Reduced Graphene Oxide) | Utilized for its excellent electrical properties and flexibility in printed electronics and energy storage applications. |
| Carbon black | Commonly used as a conductive agent in battery electrodes and other electronic applications. |
| AgNWs (Silver Nanowires) | Employed for their high conductivity and flexibility, making them ideal for transparent conductive films and flexible electronics. |
| Nanotube graphene platelets | Provide high conductivity and mechanical reinforcement in composites. |
| mGO (Modified Graphene Oxide) | Used to enhance the electrical conductivity and mechanical properties of materials. |
| Acetylene black | A form of carbon black with high purity and conductivity, used in batteries to increase electrode conductivity. |
| Activated carbon | Applied in various applications for its high surface area and adsorption properties, also adds conductivity. |
| Graphite particles | Used for their conductivity and lubricity in composites and coatings. |
| MWCNT (Multi-Walled Carbon Nanotubes) | Known for their exceptional strength and electrical conductivity, used in various nanocomposite applications. |
| Copper microflakes coated with FA and DT | These coatings enhance the oxidation resistance and chemical stability of copper microflakes, crucial for durability in flexible electronics. |
| Citrate-capped copper nanoparticles | Employed for their conductivity and stability, often used in conductive inks and electronics. |
| Cu nanoparticles (Copper nanoparticles) | Utilized for their excellent electrical conductivity in applications requiring fine conductive features. |
| Metal nanowires (CuNWs and AgNWs) | Used for their high conductivity and flexibility, important in making flexible conductive paths. |
| Graphene oxide | Applied for its electrical properties and as a substrate for further chemical modification in sensor applications. |
| Copper-amino complexes, submicron copper seeds | Used to facilitate the deposition of copper, enhancing the conductivity and stability of conductive paths. |
| Silver nanoparticles | Provide high electrical conductivity, used in conductive inks and coatings to enable electrical connections. |
| Silver nanowires | Applied in applications requiring transparent conductive films due to their excellent conductivity and flexibility. |
| Sodium dodecyl sulphate (SDS) optimized as a conductive filler | Used to enhance the dispersion of conductive nanoparticles within a medium. |
| Carbon nanotubes; enhanced conductivity and mechanical flexibility | Utilized to boost both the conductivity and the mechanical properties of composites and inks. |
| Sn particles (Tin particles) | Used to enhance conductivity and reduce the sintering energy in conductive pastes and inks. |
| Aluminium oxide (Al₂O₃) nanoparticles | Improve ionic conductivity and mechanical stability, often used in battery separators and protective coatings. |
| Nickel (Ni) for anodes | Utilized for its conductivity and stability in anode materials for batteries. |
| Dispersants like Solsperse 3000 | Aid in reducing viscosity and improving the spreadability of conductive pastes. |
| Graphene flakes and WS2 (Tungsten disulfide) | Used as conductive and photoactive materials, enhancing the electrical and optical properties of composites. |
| SWCNTs (Single-Walled Carbon Nanotubes) | Known for their ultra-high conductivity and strength, used in next-generation electronic applications. |
| Acetylene black | Used particularly in battery applications to enhance the conductivity and capacity of electrodes. |

TS 2. List of substrates.

| Substrate | Characteristics | Origin |
| --- | --- | --- |
| Aluminium | High electrical conductivity, suitable for current collectors | Synthetic |
| Al-plastic pouch | Lightweight, flexible, barrier properties against moisture | Synthetic |
| Alumina | Insulating properties, thermal stability | Synthetic |
| Paper | Biodegradable, flexible, low cost | Natural |
| Carbon paper | Good electrical conductivity, mechanical strength | Both |
| Platinum-coated alumina | High conductivity, catalytic properties | Synthetic |
| Roll-fed plastic | Flexible, improved conductivity, suitable for flexible electronics | Synthetic |
| Polyester film | Durable, insulating, suitable for flexible substrates | Synthetic |
| Multi-layered film (LDPE/Nylon 6/PET/OPP) | Barrier properties, mechanical strength, flexible | Synthetic |
| Cellulose paper | Biodegradable, lightweight, flexible | Natural |
| Cu foil | High electrical conductivity, commonly used as current collector | Synthetic |
| Glass slides | Chemically stable, rigid, insulating | Synthetic |
| Silicon | High electrical conductivity, used in microelectronics | Synthetic |
| Conventional A4 paper | Low cost, readily available, flexible | Natural |
| Flexible gold film | High conductivity, corrosion resistant, flexible | Synthetic |
| Flexible aluminum foil | Lightweight, flexible, good electrical conductivity | Synthetic |
| Carbon-coated aluminum | Enhanced electrical conductivity, corrosion resistance | Both |
| Metals | Various properties depending on type, typically good conductors | Both |
| Wood | Organic, insulating, can be used in biodegradable applications | Natural |
| Fabric | Flexible, customizable, used in wearable electronics | Both |
| Ceramics | High thermal stability, insulating, durable | Both |
| Polyethylene Terephthalate | Chemical resistance, strength, used in flexible electronic substrates | Synthetic |

TS 3. List of solvents.

| Name | Purpose | Organic/Inorganic |
| --- | --- | --- |
| Toluene | Used in printed electronics for its ability to dissolve a variety of resins and polymers, enhancing ink formulation. | Organic |
| Ethanol | Commonly used to adjust viscosity and improve the drying rate of inks in printed electronics. | Organic |
| Dimethylformamide (DMF) | Utilized for dissolving various polymers and as a reaction medium due to its high boiling point, especially in the production of electronic components. | Organic |
| Tetrahydrofuran (THF) | Employed in printed electronics for dissolving PVC and other polymers, useful for creating thin films. | Organic |
| Dimethylsulfoxide (DMSO) | Used for its ability to dissolve both organic and inorganic compounds, useful in fabricating various electronic components. | Organic |
| Deionized Water (DI Water) | Essential in printed electronics for processes that require high levels of purity to avoid ion contamination. | Inorganic |
| N-Methylpyrrolidone (NMP) | Known for its excellent solvency for a wide range of materials, used in fabricating batteries and capacitors. | Organic |
| Propylene Glycol | Used in ink formulations in printed electronics to help with viscosity management and ink stability. | Organic |
| Methylether of Dipropylene Glycol | Solvent used for its low toxicity and effectiveness in solvating both hydrophilic and hydrophobic materials. | Organic |
| 2-Propanol (Isopropanol) | Commonly used in cleaning processes in electronics manufacturing due to its effectiveness at dissolving oils and other residues. | Organic |
| Terpineol | Used as a solvent in inks due to its high boiling point and non-reactive nature, ideal for slow-drying processes. | Organic |
| Milli-Q Ultrapure Water | Used in high-precision electronics manufacturing where extreme purity is required to prevent contamination. | Inorganic |
| Cyrene (Dihydrolevoglucosenone) | A newer, greener solvent used in printed electronics for its low toxicity and high solvency capabilities. | Organic |
| Triethanolamine | Utilized in electronic inks as a pH adjuster and to improve the solubility of metal complexes. | Organic |
| Hydrazine Hydrate | Used in fuel cells and as a reducing agent in various electronic components due to its reactivity. | Inorganic |
| Ethylene Glycol | Employed as a coolant and in thermal management within electronic devices due to its low freezing point. | Organic |
| Amines (e.g., 2-ethylhexylamine, hexylamine) | Used as catalysts and solvents in the synthesis of materials used in electronics. | Organic |
| Diethylene Glycol | A solvent for its hygroscopic properties and high boiling point, used in inks and coolants in electronics. | Organic |
| Dipropylene Glycol Monomethyl Ether (DPM) | Known for its low odor and good solvency for a wide range of materials, used in inks and coatings. | Organic |
| Isophorone | Utilized in specialized coatings due to its high boiling point and solvent properties. | Organic |
| Acetic Acid | Used in electronics manufacturing for cleaning and as an acidity regulator in chemical processes. | Mixed |
| Tetradecane | Employed as a solvent in laboratory settings, though less common in commercial electronics applications. | Organic |
| Ethyl Cellulose and Butyl Carbitol Acetate | Used as binders and film-formers in some specialty ink formulations. | Organic |
| Methanol | Often used as a solvent and for cleaning during the manufacturing of electronic components. | Organic |
| Di(propylene glycol) methyl ether | Used for its favorable solvent properties in coatings and inks, particularly for its compatibility with many materials. | Organic |
| Dibasic Esters (DBE) | Employed as solvents in high-performance coatings due to their low volatility and good solvency characteristics. | Organic |
| N,N’-dimethylpropyleneurea (DMPU) | Utilized for its high solvency and as a high-boiling solvent in the synthesis of advanced materials for electronics. | Organic |
| Butyl Cellosolve (Ethylene Glycol Monobutyl Ether) | Used as a solvent in coatings due to its good balance of properties, including evaporation rate and solvent strength, also found in inks for printed electronics. | Organic |
| Tetradecane | Typically used in research as a non-polar solvent, less common in industrial applications, might be used in organic electronic processes. | Organic |
| 2-Amino-2-methyl-1-propanol | Used to adjust the pH of solutions in ink formulations and improve the solubility of other compounds. | Organic |
| Dimethyl carbonate | Employed as a polar solvent in electrolytes for batteries and as a low toxicity alternative to other solvents in various resin and coating applications. | Organic |
| 2-Ethylhexylamine | Used as an organic solvent and acid neutralizer in various applications, including coatings and possibly in electronics for specific synthesis processes. | Organic |
| Hexylamine | Serves as an organic solvent and catalyst in the production of dyes, pharmaceuticals, and other chemicals, potentially used in electronic materials synthesis. | Organic |
| Gadolinia Doped Ceria (GDC) | Mainly used in solid oxide fuel cells as an electrolyte material, not a solvent but included in formulations that require mixed solvent systems. | Inorganic |
| Isophorone | Used as a high-boiling solvent in paints, varnishes, and inks, where a slow evaporation rate is beneficial, possibly in printed electronics for specialized inks. | Organic |
| Acetic Acid | Used in electronics manufacturing for cleaning and etching, due to its effectiveness at removing oxides and other residues. | Mixed |
| Xylene | Often used as a solvent in the printing, rubber, and leather industries, it can be employed in electronic inks for its strong solvency characteristics. | Organic |
| Texanol | Utilized as a coalescent in latex paints and varnishes, its application in electronics might involve ink formulation to improve film formation. | Organic |
| Dibasic Esters (DBE) | Used as a low volatility solvent in coatings, inks, and adhesives, suitable for applications requiring gradual drying. | Organic |
| Di(propylene glycol) methyl ether | Employed for its favorable solvent properties, particularly in formulations requiring a low toxicity profile, such as inks and coatings in printed electronics. | Organic |
| Dihydrolevoglucosenone (Cyrene) | A newer, greener alternative to traditional solvents, used due to its low toxicity and effectiveness in dissolving a variety of materials. | Organic |
| N,N’-dimethylpropyleneurea (DMPU) | Used for its high solvency and as a high-boiling solvent in the synthesis of advanced materials, particularly in high-tech applications. | Organic |

TS 4. List of Binders.

| Name | Purpose |
| --- | --- |
| SIS (Styrene-Isoprene-Styrene) | Used for its flexibility and stretchability in thermoplastic elastomer applications. |
| TPU (Thermoplastic Polyurethane) | Known for its elasticity and abrasion resistance, valuable in flexible electronics. |
| Poly(4-styrenesulfonic acid) | Enhances the polyelectrolyte properties in battery applications. |
| PVDF (Polyvinylidene Fluoride) | Used for its chemical resistance and stability as a binder in battery electrodes. |
| CAB (Cellulose Acetate Butyrate) | Used in inks for its transparency and toughness as a film-forming resin. |
| PC (Polycarbonate) | Valued for its mechanical strength and clarity. |
| (Hydroxypropyl)methyl cellulose | Used for its water retention, film formation, and thickening properties. |
| N-vinyl-2-pyrrolidone and vinyl acetate | Form flexible films and are used in binding and coating applications. |
| Nafion | Notable for its ionic conductivity, used in fuel cell membranes. |
| PTFE (Polytetrafluoroethylene) | Used for its non-reactive nature and as a binder to reduce electrode degradation. |
| PVP (Polyvinylpyrrolidone) | Used as a binder and stabilizer in inks due to its solubility and adhesive properties. |
| Ethyl cellulose | Provides viscosity and film-forming properties, useful in ink formulations. |
| Waterborne resin | Used for their environmental benefits and stable dispersion medium. |
| LA132 binder | Specific product designation; likely a commercial binder formulation. |
| Polyacrylic latex | Used for its flexibility and film-forming properties in coatings. |
| Chitosan | Used for its film-forming and biocompatibility properties. |
| CMC-Na (Sodium Carboxymethyl Cellulose) | A water-soluble polymer used as a thickener or binder. |
| Waterborne polyurethane | Offers good film-forming and elastic properties. |
| CMC + MFC (Carboxymethyl Cellulose + Microfibrillated Cellulose) | Used for viscosity and mechanical reinforcement. |
| PEDOT (Poly(3,4-ethylenedioxythiophene)) | A conductive polymer used in antistatic coatings and electronics. |
| Phenol resin | Used for its strong adhesive properties and thermal stability. |
| Sodium alginate paste | A natural polymer used for its gel-forming abilities, beneficial in printing processes. |
| Alpha-terpineol matrix | Used as a solvent in inks, affecting the viscosity and drying characteristics. |
| N,N-Dimethylformamide, Hydroxyethyl Cellulose | Solvent and binder combination, providing desired viscosity and film characteristics. |
| Lead borosilicate glass frit | Used as a component in pastes for electronic applications due to its bonding properties after firing. |
| Acrylic-styrene resin | Used for film formation, offering durability and stability on various substrates. |
| Polyvinyl chloride (PVC) | Provides rigidity and stability, used in specific formulation conditions. |
| Graphite flakes | Enhance conductivity and electromagnetic interference (EMI) shielding in composite inks. |
| PVDF-co-HFP (Polyvinylidene fluoride-co-hexafluoropropylene) | Provides excellent chemical resistance and mechanical properties, useful in separator membranes. |
| Vinyl chloride-acetate copolymer | Provides flexibility and film-forming capabilities, often used in paint and coatings. |
| Polyvinylbutyral (PVB) | Used for its adhesive properties and clarity, often in safety glass interlayers. |

TS 5. List of inks.

| Ink | Binders | Conductive Additives | Solvents | Screen printing conditions | key features | Challenges | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Zn/Ag2O ink | SIS | Super-P 80% | Toluene + 20% ethanol | • Printing Equipment: MPM-SPM semi-automatic screen printer was used. | • High elasticity with ≈1300% elongation using SIS binder. • Reversible capacity density of ≈2.5 mA h /cm2 after multiple 100% stretches. • Low-cost, high-throughput screen printed components. • Maintains performance under severe strain conditions. | • Formulating elastic inks is highly challenging. • Significant resistance increases upon stretching. • Micro-cracks in Zn and Ag2O electrodes limit electron pathways. | [55] |
| Silver and graphene ink | TPU | Silver flakes and graphene nanoplatelets | DMF + THF | • 60 T mesh was used. • After each printing process, the layers were dried at 150°C for about 5 minutes in a tunnel infrared dryer. | • High conductivity and flexibility with silver flakes and graphene nanoplatelets. • Suitable for cost-effective screen printing. • No noticeable delamination during mechanical tests. • Retains functionality after multiple washing cycles. | • Complex control needed for appropriate rheological properties. • Critical to ensure even deposition of layers during screen printing to avoid damage. • Challenging to balance high conductivity and mechanical strength for flexible applications. | [56] |
| RuO2 ink | Poly (4-styrenesulfonic acid) | rGO | DMSO + DI water | - | • High conductivity (1570 S /cm) and large specific capacitance (820 F /g). • Enhanced stability and performance with PEDOT, graphene, and RuO2 NPs. • Good adhesion and uniform thickness through screen printing. • Scalable and reproducible for industrial applications. | • Managing viscosity and binder content to maintain conductivity. • Ensuring stability and dispersion of RuO2 NPs. • Preventing degradation and maintaining redox reactions under high currents. • Overcoming material limitations like conductivity reduction and degradation. | [29] |
| Conductive carbon ink | PDVF | Carbon | NMP | The printing was performed by employing an MPM-SPM semiautomatic screen printer (Speedline Technologies, Franklin, MA). | • Enhanced Cycle Life: Addition of Bi2O3 in Zn-based batteries prolong life by improving ZnO deposition, retaining zincate ions. • High Discharge Current Density: Achieves 4 mA/ cm2, among the highest for Zn-based printable batteries. • Consistent High-Power Output: Maintains about 5 mW /cm2 during discharge, showing robust performance. | • Initial Capacity Decay: Rapid capacity loss in initial cycles, possibly due to delayed zincate ion transformation. • Complex Phase Transformations: Presence of various bismuth species and new mixed oxide phases necessitate further investigation. | [57] |
| LFP ink | PVDF | Carbon black | NMP | • Screen Mesh: Polyester mesh with 62 monofilament /cm • viscosity of the ink paste was 3 Pa s for a shear rate of 100 s^-1. • Printed cathode film thickness was 26 μm. • Drying Conditions: The electrode film was dried at 80°C in a conventional oven for 90 minutes. | • Capacity ranges from 108.1 mAh/ g at C/6 to 27.4 mAh/g at 5C. • Low polarization shown by 0.3 V in CV curve. • 83% capacity retention after 50 cycles at 5C. • Ink viscosity optimized at 3 Pa·s at a shear rate of 100 s⁻¹. • Non-spherical C-LiFePO4 particles enhance contact area. | • Slight initial capacity decrease, possibly due to loss of electrical contact. • Precise formulation needed; optimal ink viscosity at 3 Pa·s. • Essential to maintain adhesion of cathode film to prevent separation. • Voids from solvent evaporation can affect mechanical stability. • Electrolyte penetration in detached areas can lead to capacity loss. | [32] |
| Cyrene-based graphene ink | CAB | - | Cyrene/NMP | • Screen Mesh 300 • Ultrahigh graphene concentration (70 mg/mL) achieved via rotary evaporation from 10 mg/mL graphene/CAB ink. • The sample was dried and annealed in a vacuum oven at 100°C for 5 hours. | • Conductivity of 7.13×10^4 S/m. • Uses non-toxic solvent Cyrene. • Efficient exfoliation in 8 hours with Cyrene versus 48 hours with NMP. • Ink concentration up to 70 mg/mL. • Printed antennas operate from MHz to GHz. | • Conductivity maximized only after compression. • Requires vacuum rotary evaporation to achieve 70 mg/mL concentration. • Challenges in maintaining optimal properties for industrial-scale applications. | [36] |
| h-BN ink | PC | - | DMF | • A rubber squeegee was used | • High viscosity (12 Pa·s) suitable for screen printing. • Thermal stability up to 150°C. • Effective dielectric properties (constant of 2.57, loss of 0.09 at 1 MHz). • Durable under multiple folding cycles. | • Complex ink formulation with precise viscosity. • Risk of nanosheet reaggregation. • Viscosity adjustments for screen printing. • Dielectric constant variability affects high-frequency use. | [58] |
| AgNWs ink | Hydroxypropyl-methyl cellulose | - | DI water + propylene glycol | • 400 mesh count, 0.0007 inches wire diameter and 0.0018 inches mesh opening. • Printing speed 60 mm/s • Printing force 32.2 N • Squeegee angle: approximately 45° • Thermal annealing temperature: 150°C | • High initial conductivity up to 4.67 × 10⁴ S /cm; maintains >10,000 S/ cm at 70% strain. • Low solid content (6.6 % wt) in AgNW ink reduces costs. • Environmentally friendly, using distilled water as solvent. • Achieves high-resolution patterns with 50 µm feature size. • Stretchable with high conductivity (8002 S /cm at 70% strain). • Stable and durable through 1000 wear cycles on a glass vial. | • Varying viscosities (50.73 to 201.0 Pa·s) affect print quality. • Post-processing required to optimize conductivity. • Conductivity decreases under extreme strain. • Optimization needed for defoaming agents to improve conductivity. | [31] |
| Graphene ink | N-vinyl-2-pyrrolidone and vinyl acetate | - | methyl ether of dipropylene glycol | • Printing Speed: 50 mm/s | • High conductivity at 30 Ω/sq with 25 µm thickness after 100 °C drying. • Prints narrow 40 µm lines. • Low drying temperature of 80–100 °C, fits plastic and paper substrates. • Maintains stable and consistent print quality. | • Over 100 Pa. s viscosity complicates printing. • Sensitive gelation needs careful concentration control. • Isopropanol unsuitable, requires solvent switch to DPM. • Graphene-to-binder ratio of 1:3 critical to stability. | [59] |
| Carbon ink | Nafion | Carbon | 2-propanol | • A dense silk mesh (200T, Wai Hang Co.) was used for screen printing. • Distance between screen mesh and substrate 100 μm. | • Capacity doubled to 6840 mAh/ g. • Stable cycle life over 30 cycles, extendable with anode replacement. • Enhanced oxygen transport through ~10 μm pores, improving Li2O2 distribution. • Reduced overpotential at 4.06 V boosts performance. | • Anode degradation limits cyclability due to Solid Electrolyte Interphase (SEI) layer formation. | [60] |
| NGP/PANI ink | PTFE | Nanotube graphene platelets | Ethanol | • Squeegee Speed of 35 cm /s • Thickness ranging from 5 to 15 μm. | • High Capacitance and Energy Density with capacitance of 269 F /g, power 454 kW/ kg, energy 9.3 Wh/ kg in 1M H2SO4. • Mechanical Integrity maintained with no delamination after 200 bends, retaining 146 F /g capacitance. • Electrochemical Stability ensured over 1000 cycles without degradation. | • Requires specific formulation steps like temperature-controlled ball milling, complicating scalability • Quality heavily reliant on precise printing conditions, with necessary management of ink viscosity at 125 mPa.s at 10 s−1 | [27] |
| mGO ink | PVP | mGO | Terpineol | • Mesh Opening: 77 μm • Mesh Count: 195/inch • Thread Diameter: 48 μm • Theoretical Ink Volume (Wet Thickness): 27 cm³/m² • Screen Tension: 25 Newtons • Angle of Squeegee: 22° • Substrates: Flexible PET or paper • Drying Conditions: Dried for 30 minutes at 100°C | • Achieves high conductivity below 1Ω/sq with a 3 μm thick film. • Cost-effective and scalable using mGO and PVP, without expensive processing. • Ink compatible with various substrates including heat-sensitive ones. • Supports high-definition printing with sub-100 μm resolution. | • Initial resistance of about 697 Ω/sq needs roll-compression for better conductivity. • Porous structure from non-co-planar flakes reduces conductivity. • Complex graphite synthesis requires multiple oxidizing steps. • PVP binder necessary for ink stability but must be carefully mixed to avoid reducing conductivity. | [37] |
| Pb3O4 ink | Ethyl cellulose | - | Terpineol | • Mismatic model 60–90 equipped with a 34T polyester mesh screen. • Sintering Conditions: Incremental temperature increases were necessary during the sintering process, peaking at 465°C for a final 12-hour phase to achieve proper film characteristics. | • Supports deposition on non-conductive substrates, needing thermal stability up to 500°C. • Enhanced photoresponse across irradiance levels (334–1036 W/m²). • Effective charge separation improves functionality of photoresponsive devices. • Flexible in creating various device architectures. | • Low photoconversion efficiency at 0.065% due to high resistivity. • Pb3O4 material limited by resistivity and lead toxicity. • Complex sintering process (up to 465°C for 12 hours) increases production costs. | [61] |
| Ag@PPy@MnO2 and AC ink | Waterborne resin | Carbon black | DI water | - | • High energy density of 0.0337 mWh /cm2, power density of 0.38 mW /cm2. • Retains 90.8% capacitance after 5000 cycles, 86.2% after 40% stretch. • High flexibility and stability under mechanical stress. | • Complex synthesis process for Ag@PPy@MnO2. • Capacitance drops to 86.2% after 40% stretch. | [20] |
| N-Doped MXene ink | LA132 binder | Super P | DI water | • A squeegee moves at a velocity of 2 cm /s • It maintains high viscosity at lower shear rates (>104 Pa s at 0.05 s^−1) | • High conductivity (10^4 S /cm) and capacitance (1500 F /cm3) • Nitrogen doping improves performance • Flexible printing on various substrates, with 70.1 mF /cm2 (screen printed) and 8.2 F/ cm2 (3D-printed) • Scalable, efficient production for energy storage devices | • Restacking limits ion transport, addressed by template-guided synthesis | [38] |
| AgNWs ink | - | - | DI water | • 500 mesh count, 18 µm wire diameter, and 33 µm mesh opening. • Employs a rubber squeegee formed at a 45° angle with the screen mesh. • Printing speed of approximately 60 mm /s and a force of around 32.2 N | • Volumetric capacitance of 338 F /cm3 • Energy density of 18.8 mWh /cm3, power density of 40.9 W/ cm3 • Retains 91.6% capacitance after 8,000 cycles, 88.6% after 2,000 bends • Conductivity over 5,000 S cm^-1 | • Complex synthesis requires precise control • Managing ink viscosity and thixotropy is critical • Scalability and integration pose engineering challenges | [62] |
| FeOOH/MnO2 ink | Polyacrylic latex | Acetylene black | DI water | - | • High capacitance of 350.2 F /g at 0.5 A /g, 159.5 F /g at 20 A /g • 95.6% capacitance retention after 10,000 cycles • High mechanical flexibility, maintaining performance after bending and stretching | • Complex low-temperature wet-chemical synthesis • Ensuring consistency and scalability in production • Integration and commercialization with consistent performance | [33] |
| AgNWs ink | Hydroxypropyl-methyl cellulose | - | DI water | • Used a 325-mesh count screen for printing. • Printing Speed: Approximately 40 mm/s. • Printing Force: Approximately 30 N. • Printing Angle: Approximately 45°. • Post-treatment: Involved plasma treatment and thermal annealing to enhance adhesion and conductivity. | • High conductivity (8.32 × 10³ S /cm) and robustness. • 8.58 mF/ cm capacitance. • Maintains 90% capacitance after 2500 bends. | • Shift to safer water-based inks. • Optimize viscosity to prevent clogging. | [63] |
| Activated Carbon ink | Chitosan | Activated carbon | DI water | • Screen Printer Model: Semi-automatic TIC SFC 300 DE screen printer. • Printed layers were annealed at 120 °C | • Low cost, eco-friendly NaCl electrolyte. • High energy storage (200-360 mF, 7.9-12.7 Ω equivalent series resistance, ESR). • Flexible for various applications, including wearables. | • Performance varies with printing process. • Voltage limit of 1.0 V affects efficiency. • Higher ESR with graphite collectors reduces efficiency. | [64] |
| Graphene ink | CMC-Na | - | DI water | - | • High yield, scalable 100% graphite exfoliation. • Low sheet resistance under 2 Ohms/square. • Eco-friendly, cost-effective with carboxymethylcellulose stabilizer | • Difficult to achieve uniform flake size. | [65] |
| PEI-rGO ink | Waterborne polyurethane | - | DI water | - | • Tensile strength and Young’s modulus up to 9.46 and 19.8 times higher. • Wear resistance 4.5 times better after 600 cycles. • Thermal stability increased by 45 °C (initial) and 17 °C (50% degradation). | • Complex manufacturing process. • Ensuring uniform graphene dispersion. • Strong interfacial bonding required. | [66] |
| Graphite ink | CMC + MFC | - | DI water | • Printing Speed: 110 mm/s • Squeegee Angle: 60° • Squeegee Hardness: 70–75 Shore • Mesh Type: Polyamide nylon • Mesh Specifications: 208 threads per inch, 40% open area, 70 μm thread diameter, 110 μm emulsion thickness • Off-contact: 1 mm between the substrate and the mesh | • Increased capacity from 85 to 315 mAh/g by reducing porosity. • Eco-friendly with cellulose and water-based solvent. • Flexible, maintains performance under stress. | • High initial porosity (70%) reduces efficiency. | [67] |
| MWCNT/PEDOT | PEDOT | - | Milli-Q ultrapure water | 60 mesh screen | • Low-cost, efficient PEDOT and MWCNT films. • High capacitance (20.3 F /g) and energy density (3.1 Wh /kg). • Durable, retains 72% capacitance after 1000 cycles. • Flexible and lightweight for wearables. | • High equivalent series resistance of 60 Ω affects power output • Difficulty in achieving uniform material deposition • Scalability and reproducibility issues | [68] |
| LiCoO2 paste | Ethyl cellulose | - | Terpineol | 500 mesh screen | • High discharge capacity of 179 µAh/ cm² with carbon-coated LiCoO2. • Controlled film thickness (6 µm) and smooth surface. | • Paste formulation complexity; viscosity increased with carbon black. • More carbon black reduced discharge capacity to 46 µAh /cm². | [24] |
| LiCoO2 powder | Epoxy mixed with ethyl-cellulose | - | Terpineol, 2-butoxietanol, and others | - | • High discharge capacity of 125 µAh /cm² (133 mAh /g). • Improved adhesion and conductivity with epoxy-mixed paste, reducing electrical resistance to 432 kΩ cm². • A mix of carbon black (Ketjenblack 300J, Mitsubishi Chemical) and graphite (CSP-E, Nippon Graphite) used as conducting anode. | • Delamination issues | [25] |
| Antioxidant copper ink | Phenol resin | FA (formate ions) and DT (dodecyl mercaptan) | Triethanolamine, 2-Amino-2-methyl-1-propanol, Dimethyl carbonate | - | • High conductivity of 13400 S/cm, comparable to silver pastes. • Cost-effective alternative for large-scale flexible electronics. • High flexibility and stability, suitable for RFID tags and EMI shielding. | • Complex preparation involving oxide removal and corrosion inhibitors. • High susceptibility to oxidation, needing extra protection. • Requires specialized, expensive equipment for some methods. | [41] |
| Copper ink | Sodium alginate | - | Ethanol and hydrazine hydrate | • Screen Mesh Size: 156 (used for applying the sintering paste) • Sintering Temperature: Maintained at 60°C for both the drying of the sintering paste and the copper nanoparticle slurry. | • High conductivity with resistivity of 74.4 ± 9 x 10^-2 μΩ.m at sintering temperatures below 60°C. • Maintains conductivity after 2500 bending cycles. • Cost-effective process using screen printing and low-temperature sintering. | • Managing oxidation of copper nanoparticles, effective with citrate capping. | [69] |
| Copper ink | Ethyl cellulose | Cu nanoparticles | Ethylene glycol, ethanol | • Screen mesh: Used a mesh count of 400 (wires/inch) with a wire diameter of 18 μm. • Curing Conditions: Curing was done in a vacuum oven with an oxygen concentration less than 300 ppm, with temperatures ranging from 200 °C to 400 °C for 30 minutes, depending on the paste formulation | • Consistent print dimensions: Finger widths of 53-60 μm, heights above 20 μm • Low specific contact resistivity: 0.4 mΩ·cm² for Cu-ITO contact • Improved resistivity of printed lines: 27 μΩ·cm after curing at 400 °C | • High finger line resistance (>10 kΩ/cm) at low sintering temperatures (200-300 °C) • Managing paste viscosity (50,000-60,000 cps) to maintain print quality and integrity | [70] |
| Copper ink | - | Metal nanowires (CuNWs and AgNWs) | Amines (e.g., 2-ethylhexylamine, hexylamine) | - | • Low cost and high conductivity with Cu (1.72 µΩ cm). • Metal nanowires improve conductivity (14.9 µΩ cm at 140 °C). • Excellent mechanical flexibility, minimal resistance increases after 1000 bends. | • Cu particles prone to oxidation, increasing sintering temperature. • Instability of Cu particles require optimizations like adding nanowires or using amine-based ligands | [71] |
| Copper ink | PVP | - | Ethanol and Diethylene Glycol | • Printing Speed: 100 mm/s. • Drying Conditions: Near-infrared drying at 80°C for 30 minutes | • High conductivity (8.38 μΩ·cm) with silane-modified Cu oxide • Improved nanoparticle dispersion and stability | • Re-oxidation after intense pulsed light (IPL) sintering • Complex IPL sintering process control needed | [72] |
| Copper-nickel complex ink. | PVP | Graphene oxide | Ethylene glycol | - | • High conductivity (8.38 μΩ·cm) with silane-modified Cu oxide • Improved nanoparticle dispersion and stability | • Re-oxidation after intense pulsed light (IPL) sintering • Complex IPL sintering process control needed | [73] |
| Copper ink | - | Copper-amino complexes | - | The copper inks were deposited on substrates using a screen printing method where the ink-coated substrates were heated at temperatures ranging from 120°C to 180°C for 2 to 60 minutes under a nitrogen atmosphere. | • High metal load (36.8%) for thick, conductive patterns. • Low temperature sintering (140°C) with 11.3 μΩ·cm resistivity. • Strong adhesion to substrates, cost-effective with submicron copper. | • Complex fabrication needing precise copper control. • Sensitive to oxidation, requiring higher temperatures. • Inconsistent quality due to voids and pores. | [74] |
| Copper ink | PVP | Carbon Nanotubes (CNTs) | Dipropylene glycol monomethyl ether (DPM) | • Polyester mesh (100 threads/cm) • Patterns shaped like "dog bones" (24 mm length, 1.3 mm width) • Samples dried on a hot plate at 70 °C for 5 minutes • Screen printed onto substrates, then IPL treatment with PulseForge 1200 • Pulse duration (2-20 ms), voltage (220-240 V), and pulses (up to four) varied for optimization | • Rapid prototyping with IPL for fast curing, suitable for roll-to-roll production. • High conductivity with 0.5 wt% CNTs, reducing curing energy by 25%. • Environmentally stable, self-reducing copper formate avoids oxidation. | • High energy consumption with IPL. • Precise control over IPL pulse parameters needed. • Ensuring uniform conductivity through layer thickness. | [34] |
| Silver ink | Alpha-terpineol matrix | - | Organic solvent | •Used a 400-mesh screen mask. • Sintering Conditions: All circuits were sintered at 150°C in air, with times ranging from 15 to 60 minutes to examine the influence on extensibility. • Pre-stretched thermoplastic polyurethane substrate and dried at 70°C for 10 minutes to minimize dimensional changes. | • Improved extensibility with single line < zigzag < rectangular pulse < horseshoe • Enhanced electrical performance with 31 µΩcm resistivity after 60 minutes sintering | • Crack formation under stress, especially at notches • Circuit durability limit with max extensibility up to 8% for horseshoe design | [28] |
| Silver ink | N, N-Dimethylformamide, Hydroxy ethyl Cellulose | - | Ethylene glycol | •A mesh size of 250 μm • Sintering Conditions: Conductive circuits were sintered at 220 °C for 30 minutes under air atmosphere | • High conductivity and stability with silver nanoparticles (118 nm, 8.3 × 10⁻⁶ Ω·cm) • Enhanced mechanical performance for flexible wearable devices | • Control of silver nanoparticle synthesis to prevent aggregation • High production cost due to capping agents needed for dispersity and mobility | [75] |
| Silver ink | - | - | Tetradecane | • Mesh Type: 420 polyester mesh was used, suitable for the required pattern fidelity on the PU substrate. • Squeegee Angle: 22.5°, optimized for the best printing shape. • Drying and Curing Conditions: Post-printing, the electrodes were dried and cured at 130°C for 10 minutes, essential for achieving the desired electrical properties. | • Low sheet resistance (1.64-2.85 Ω/sq) at room temperature • Stretchability and flexibility (15-20% for different patterns) | • Limited stretchability compared to other materials • Complexity in pattern and material handling • Environmental sensitivity (humidity and temperature) | [39] |
| Silver ink | (Hydroxypropyl)methyl cellulose | Silver nanowires | Distilled water and propylene glycol | •Screen mesh (400 mesh count, wire diameter 0.0007, mesh opening 0.0018, mesh angle 22°. • Utilized a 45° squeegee angle and a printing speed of approximately 60 mm/s. • Printing force of about 32.2 N. | • High electrical conductivity (up to 46,000 S /cm) • Stretchable and durable (conductivity >10,000 S/ cm at 70% strain) • High resolution printing (line resolution as low as 50 μm) • Low thermal budget (sintered at 150 °C) | • Complex post-processing with multiple treatments (washing and thermal annealing) | [76] |
| Silver ink | EC and PVP | - | Ethanol | • The ink used had a viscosity of 3.2 Pa·s at a shear rate of 10 s⁻¹, suitable for screen printing. •Printing speed (50 mm/s to 200 mm/s) | • High conductivity and transparency achieved with 1.9 ohm/sq sheet resistance and 73% transmittance at 550 nm • Flexibility and stretchability with stability after 1000 bending cycles (28 mm radius) and 1000 stretch-release cycles (10% strain) | • Balancing conductivity with transparency while maintaining low sheet resistance • Complex post-processing requiring multiple steps including solvent immersion and laser sintering | [77] |
| Ag NWs paste | - | Ag NWs | - | Terpineol | • High stretchability and conductivity (6912 S/cm) across 0-50% tensile strain • Successful integration with commercial integrated circuits for wearables | • Initial resistance increases of 26.5% after PDMS (polydimethylsiloxane) casting, stabilizes with cycles • Complex fabrication requiring precise control to prevent cracking or detachment | [78] |
| MWCNT | PVP | SDS | Ethanol | • Silk screens with a mesh size of 325 were used. • A semi-automatic screen printer (XPRT2, Ekra, Asys group, Germany). • Frame Dimension: 220x220 mm. • Substrate Types: Paper, Mylar®, photopaper, cellulose acetate sheet, and silicone rubber. | • Low curing temperatures reduce energy use and substrate damage. • Achieves sheet resistance of 0.5 to 13 Ω/sq over three strokes. • Excellent adhesion on flexible substrates (Mylar®, photopaper, silicone rubber). • Uniform CNT distribution and connectivity with RMS surface roughness of 64.4 nm. | • Requires precise viscosity control (2.09 Pa·s) and CNT dispersion. • Viscosity management needed for screen printing (1-10 Pa·s). • Long-term stability issues due to CNT aggregation; needs dispersants like SDS and PVP. | [79] |
| Silver ink | - | Carbon nanotubes | Organic solvents | • Initially sintered at 120 ºC for 20 minutes followed by a final sintering between 250 ºC and 350 ºC for one hour under nitrogen atmosphere. • Viscosity of the Ink: Ranged from 48-65 Pa S with a thixotropic index of 3-4. | • Conductivity improved with CNTs, reducing resistivity to 7.26 μΩ cm • Flexibility maintained with minimal resistivity change after 1000 bending cycles • Strong adhesion and structural integrity after 500 thermal shock cycles | • Balancing conductivity and flexibility with higher sintering temperatures reducing flexibility and adhesion • Thermal stability issues during sintering without damaging the substrate limits maximum temperature | [80] |
| Silver ink | PVP | Silver nanoparticles | Ethanol | • The screen used had a mesh count of 300 fibers per centimeter. • The optimal sintering conditions found were 160°C for 75 minutes. | • Achieved low resistivity (3.83 μΩ·cm at 160°C for 75 minutes), close to bulk silver (1.58 μΩ·cm), indicating high conductivity • Low sintering temperatures (160°C) suitable for flexible substrates like PET | • Electrical properties depend on controlling particle size distribution of silver nanoparticles • Finding optimal sintering time and temperature to reduce resistivity while maintaining substrate compatibility | [81] |
| Silver ink | Acrylic acid | Silver particles. | Ethylene glycol/water solution. | • Stencil Line Openings: Ranging from 5 to 50 µm. • Squeegee Speed: Approximately 10 cm/s. | • High printing resolution with silicon stencils, achieving 22 µm line widths • Excellent electrical properties with low resistivity (5.5 × 10^-6 Ω cm) • Good bendability with tolerance for radii > 5 mm and tensile strains < 0.75% | • Complex ink formulation requiring precise control for high solid loading (77 wt %) • Managing high ink viscosity (1 × 10^4 Pa s) to ensure printability and stability | [82] |
| WO3 nanopowders | - | - | Terpineol | • Sintering Temperature: Annealed at 400°C for 12 hours. • Substrate: Alumina fitted with gold electrodes and a platinum heater. | • High sensitivity and quick response to SO2 at 5-10 ppm and 260°C • Various WO3 nanostructures (nanoplates, nanowires, nano lamellae) for tailored applications | • Temperature dependency with slower response at 220°C • Complex manufacturing involving hydrothermal treatments and high-temperature annealing (400°C for 12 hours), complicating scalability | [26] |
| SnO2-based ink with 15 wt% glass | Lead borosilicate | - | Ethyl cellulose and butyl carbinol acetate | - | • High sensitivity to H2, CO, and LPG using 15 wt% glass frit dopant, with optimal sensitivity temperatures (150°C for H2, 220°C for CO, and 190°C for LPG) • Low sheet resistivity (2.95 to 10.47 MΩ/sq) and stable TCR (-1900 ppm/K) • Fast response (10 s) and recovery times (18-20 s), competitive with previous sensors | • Optimization of glass frit percentage is critical; exceeding 15 wt% reduces sensitivity • High glass content can form new phases like PbSnO3, affecting sensor properties and phase stability | [83] |
| Silver ink | CMC | Silver nanowires | DI water | •Multiple shear rates were applied during tests to mimic the screen printing process, including very low (0.1 1/s) and very high (200 1/s) rates. • All tests were conducted at room temperature (25°C). • A pre-conditioning step at a shear rate of 0.1 1/s for 10 seconds was applied before each test to ensure uniformity. | • High viscosity at low shear rates maintains ink on screen and ensures clear printed patterns • Strong shear-thinning allows efficient printing • Rapid viscosity recovery maintains sharp lines • Water-based, environmentally friendly | • Managing complex rheological properties • High silver nanowire concentration affects viscosity • Achieving uniform printed patterns is difficult | [30] |
| Copper nanoparticles | Ethyl cellulose in terpineol. | - | Methanol | • Screen Mesh: Used a 200-mesh screen printing mesh. • Ink Preparation: Copper paste with 75 wt% copper, prepared by suspending copper nanoparticles in a polymeric matrix. • Drying and Sintering Conditions: Printed patterns were dried in a vacuum oven at 50°C for 30 minutes, followed by sintering in a furnace at 120°C with a continuous purge of H2 and N2. | • High productivity, scalable for large-scale production • Controlled particle size (12-99 nm) based on synthesis conditions • Flexible surface modification with different capping agents • Low-temperature sintering (120°C) suitable for flexible substrates | • Copper nanoparticles are prone to oxidation, requiring protective coatings • Complex handling and storage needed to maintain properties • Reliance on precise synthesis conditions, complicating production processes | [84] |
| Cu/Sn hybrid | PVP | Sn particles | Terpineol | The films were sintered using a xenon flash lamp system with energy densities ranging from 2.68 to 5.02 J/cm². The distance from the lamp to the substrate stage was 3.5 cm. | • 21% less energy for sintering • Better film quality, 84% transmittance, 14 Ω/sq resistance • Excellent mechanical stability after 2000 cycles | • Precise sintering energy control needed • Risk of Sn particle oxidation affecting reliability | [85] |
| Graphene oxide | - | - | DI water | • The squeegee angle used was 22 degrees. •A mesh with openings of 57 or 77 µm was used. •The printed structures were dried at 100 °C for 30 minutes. | • Low sheet resistance, 327 ohms per square (Ω /sq) • Compatible with moderate temperatures (80°C) • Scalable and cost-effective • Enhanced environmental and mechanical stability | • Limited print resolution (100 µm) • Maintaining ink viscosity and stability is challenging • Dependent on post-processing to reduce graphene oxide • Substrate compatibility issues | [86] |
| CNT ink | Acrylic-styrene resin | - | DI water | • Oxygen plasma treatment was employed to modify the electrode surface, crucial for enhancing conductivity and enabling enzyme immobilization. Treatment times ranged from 5 to 180 seconds, with an optimal time of 20 seconds suggested for balancing conductivity enhancement and material integrity. | • Conductivity and flexibility with a CNT layer, achieving sheet resistance of 600 Ω/sq (spin-coated) and 1800 Ω/sq (rod-coated), suitable for biosensors • Fast production, ideal for roll-to-roll printing • Enhanced electrons transfer due to electrocatalytic properties | • Oxygen plasma treatment required, increasing complexity and cost | [87] |
| MWCNT-derived ink | PVC | - | Isophorone | • The printed layers were cured at 150°C for 1 hour and allowed to cool to room temperature. | • Improved electrochemical properties with lower detection potentials for hydrogen peroxide and NADH (nicotinamide adenine dinucleotide) at 0.50 V and 0.30 V • High mechanical durability with strong resistance to abrasion and good adhesion to ceramic substrates | • Variability in performance due to nonuniform distribution of particles | [23] |
| Carbon nanotubes (CNT) | Chitosan (CS) | - | Acetic acid solution | - | • Better electrical properties with a potential difference (DE) of 131 mV in CV tests and reproducibility with a relative standard deviation (RSD) of 3.63% • Superior mechanical durability with a lower RSD increases of 8.43% under stress, ideal for flexible applications | • Sensitivity to environmental factors like humidity and temperature | [88] |
| Polyaniline nanofiber | - | - | Graphite | Toluene | • Nearly 100% EMI shielding effectiveness • High conductivity, lightweight, non-corrosive • Easy to print on various substrates, cures at room temperature • Low-cost and eco-friendly | • Limited long-term stability data • Complex synthesis requiring precise control • Precise formulation needed for consistent quality | [89] |
| Alumina ink | polyvinyl butyral | - | Xylene-ethanol | - | • Economical, room temperature curing suitable for various applications • Good dielectric properties, with a dielectric constant of 3.29 at 5 GHz and 3.26 at 15 GHz on BoPET (biaxially-oriented polyethylene terephthalate) • Strong adhesion to BoPET and photographic paper, ensuring durability | • Sensitive to printing conditions like squeegee speed and angle | [90] |
| Graphite | PVDF | Super-P C45 | NMP | • Screen Printer: AMI M-465. • Mesh Type: Stainless steel, 325 mesh count, 28 µm wire diameter, 22.5o mesh angle. | • High initial capacity with a first charge capacity of 356.2 mAh/g • Controlled porosity at 35% facilitates effective ion transport and enhances electrochemical performance | • Initial capacity loss of 10.7% suggests efficiency loss during the first use | [40] |
| Silver / graphene flakes | PVDF | Carbon black | Ethanol | • Printing Speed: 100 mm/s • Squeegee Angle: 45 degrees • Printing Force: 15 N • Screen Mesh: 200 mesh | • Stable ink viscosity of 10-12 mPa·s ensures consistent quality. • High conductivity at 200 S/m enhances device efficiency. | • Sintering at 350°C limits substrate options. • Rapid drying time of 2-3 hours requires precise control. | [43] |
| LFP (LiFePO₄) and LLZO (Li₆.₄La₃Zr₁.₄Ta₀.₆O₁₂). | Polyvinylidene fluoride (PVDF): 5 wt% | - | DMF | • The screen printing was performed using an Ekra E2 screen printer and a Koenen stencil, and speed of 40 mm/s. | • High ionic conductivity of 0.425 mS/cm at 60°C. • Wide electrochemical window above 4.6 V. • High lithium-ion transference number of 0.44. • Good interfacial compatibility with electrodes. • Strong thermal and chemical stability. | • Lower ionic conductivity at room temperature. • Degradation of materials, especially PEO, above 300°C. | [45] |
| Zinc batteries | PVDF-co-HFP | Aluminum oxide (Al₂O₃) | EG | - | • Achieves 2V and 4 mAh/cm², better than typical systems • Over 60 cycles at 2 mA/cm², showing reliability • Uses low-cost ethylene glycol (EG), eco-friendly | • Requires optimization of interfacial stress and bonding • Precise control needed for viscosity and polymer electrolyte integrity during printing | [44] |
| NMC | HSV 1810 and PVDF | - | NMP and DMF | • Printer Model Ekra E2. • Printing Speed from 30 to 60 mm/s. • Gap from 0.5 to 2.0 mm to ensure optimal ink transfer and film thickness. • The squeegee pressure from 0.4 to 1.5 bar. • Post-printing, the cathodes were dried on a hotplate at 100 °C for 1 hour • The temperature during printing was maintained at a constant 23 °C | • NMP with HSV 1810 retains 87% capacity after 1,000 cycles • HSV 1810 enhances γ-phase in the binder, boosting performance • Solvent-binder combinations show excellent solubility and compatibility | • DMF cause cracking and degradation • NMP has environmental and health concerns • Solvents and binders affect electrochemical properties and integrity | [42] |
| Graphene | Vinyl chloride-acetate copolymer | Carbon black | DBE | • Screen Printer Used: LTA-6080 Screen Printer. • Squeegee: 60-degree angle polyurethane squeegee. • Printing Speed: Approximately 50 mm/s. • Screen Meshes: Used 80 and 420 mesh counts for different applications. • Post-Printing Process: Printed patterns were dried at 100°C for 8 minutes, then pressed by compression rolling and finally dried again at 150°C for 8 minutes. | • Achieves high electrical conductivity up to 21,500 S/m for flexible electronics • Prints lines as narrow as 90 microns, suitable for various substrates and Roll-to-Roll applications • Straightforward and cost-effective production, avoiding complex processes | • Requires precise control of carbon black content to maintain performance | [91] |
| Solid oxide fuel cells (SOFC) | Ethyl cellulose (EC) | Nickel (Ni) for anodes and Silver (Ag) | Terpineol and Texanol | • Squeegee pressure: 6-9 kg • Squeegee Speed: 20-50 mm/s • Snap-off Distance: 1.5-2.0 mm • Printing Angle: 45° • Squeegee Geometry and Type: Rectangular, polyurethane • Screen Mesh Type: 305-325 mesh per inch | • Solid oxide fuel cells (SOFC) have 60% fuel-to-electricity efficiency, up to 80% with heat recovery • Screen printing produces high-quality, porous electrode films, enhancing reactions and reducing losses | • High sintering temperatures required | [92] |
| Solid oxide fuel cells (SOFC) | Polyvinylbutyral (PVB) | Solsperse 3000 | Terpineol | • Two different screens (325 mesh and 255 mesh) were used along with different squeegees (soft with round edges, stiff with sharp edges). The combination of a stiffer squeegee and a coarser screen was found optimal for printing the developed pastes. | • High solid loading of 50 vol.% YSZ powder for dense, conductive layers in solid oxide fuel cells. • Polyvinylbutyral (PVB) binders allow processing under varied conditions without sensitivity to temperature and humidity. | • Sintering at 1430°C may cause microstructure coarsening and interfacial reactions, reducing catalytic efficiency. | [93] |
| Solid oxide fuel cells (SOFCs) | PVA, PVP, and CMC | - | GDC and PG | - | • Water-based inks improve safety and reduce costs. • Enhanced stability and homogeneity ensure consistent quality. | • Fast evaporation can cause issues and cracking. | [94] |
| Titanium silicon carbide (Ti3SiC2) | Ethyl Cellulose | - | Terpineol | •Print Speed: 150 mm/s •Screen Mesh: 333 µm •Squeegee Pressure: 100 N •Snap-off Distance: 2mm | • Excellent thermal stability and conductivity, ideal for high-power electronics. | • Complex rheology requires careful management. • High viscosity pastes are difficult to process and have poor workability. | [95] |
| Carbon nano-onions/ | Polyhydroxyethers | Graphite | Di(propylene glycol) methyl ether | - | • Highly sensitive, detecting dopamine at low concentrations (10.0–99.9 µM) with a detection limit of 0.92 µM. • Enhanced conductivity and current density with carbon nano-onions and graphite, high electron transfer rate | • Difficulty in achieving stable, homogeneous ink dispersion. • Issues with aggregation affecting electrode uniformity and performance. | [96] |
| Cu ink | Hydroxymethyl cellulose | - | Deionized water | • The screen mesh used has a resolution adequate to produce a Cu mesh with a line width of approximately 219 μm and line spacing of 193 μm, indicating a high-resolution screen printing process to achieve detailed patterns. | • Lightweight and ultrathin, ideal for large-scale fabrication and high-energy lithium metal batteries. • Improved safety and stability, suppressing dendrite growth and promoting uniform lithium plating/stripping with long cyclic life and high efficiency. | • Scalability and cost-effectiveness need optimization for commercial use, ensuring quality control and maintaining low weight. | [97] |
| Graphene | - | - | NMP | • Squeegee Angle: 70° • Printing Speed: 50–150 mm/s • Screen Mesh: 24 mesh • Ink Viscosity: The graphene ink used had a viscosity adjusted to be suitable for screen printing, though specific numerical values are not mentioned. | • High responsivity and sensitivity, ideal for photoactive thermistor applications. • Low-cost and biodegradable paper substrate, reducing costs and environmental impact. • Integration for wireless applications, enabling wireless data transmission and power from a reader. | • Complex multi-stack printing process requiring precise control for quality. | [98] |
| Graphene flakes | Terpineol | SWCNTs | Water and Ethanol | • Printing Substrate: Flexible substrate, specifically polyethylene terephthalate (PET). • Screen Mesh: use of a 55T screen mesh is indicated, implying moderate resolution capabilities. | • High capacitance of up to 1.324 mF /cm2. • Stable performance over 10,000 cycles. • High power and energy density. • Flexible and waterproof, durable after bending and washing. | • Ensuring even dispersion of graphene and SWCNTs. | [99] |
| Graphene/CoS2/Ni3S4 powder | polyvinylidene fluoride (PVDF) | acetylene black | Ethanol | - | • High specific capacitance of 1739 F/g at 0.5 A/g. • Flexible and high energy density suitable for wearables, with an energy density of 44.9 Wh/kg at a power density of 224.8 W/kg. | • Complex production involving solvothermal synthesis and vulcanization, complicating scaling. • Stability issues due to partial destruction of structural integrity during production, affecting long-term performance. | [100] |

TS 6. Screen printing batteries

| Type | Anode | Cathode | Electrolyte | Solvents | Binder | Substrate | Capacity, efficiency and cycles | Dry parameters | Printing parameters | Challenges | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Lithium-ion, solid-state | Li4Ti5O12 | LiMnO2 | Solid polymer based on PEG and PEO | - | - | Aluminum | •150 mA h g^-1 capacity with excellent retention over 100 cycles | - | - | • High charge transfer resistance limits charging/discharging speed. • Poor ion transport at room temperature restricts battery performance to low power uses. | [47] |
| Pouch-type flexible thin-film | Pitch-coated natural graphite | LiCoO2 | Gel polymer electrolytes | NMP, Butyl carbinol, Acetone | HPC and PVDF | Al-plastic pouch | •2.5 mAh cm^2, 332.8 Wh L^-1, 84% retention at 50th cycle | - | •Stainless steel screen mesh #120 | • Sequential screen printing of layers complicates fabrication due to precise viscosity control. • Optimizing current collectors reduces interfacial resistance and internal resistance. | [101] |
| Zinc-Alkaline | Zinc (Zn) | Manganese Dioxide (MnO₂) | Potassium Hydroxide (KOH), 35-52 wt% | Water | PEO | Alumina | •Theoretical capacity of cathode between 3 and 4 mAh, discharge efficiency up to 97%, designed for single-use (primary battery) | - | • Semi-automatic screen printer used (MPM Corp., Franklin, MA, TF-100). •Screen Mesh: 325 | • Cathode integrity issues reduce adhesion to the substrate, needing improved stability. • Anode prone to hydrogen evolution, requiring research to inhibit this reaction for better safety and efficiency. | [48] |
| Zinc-air | Zinc/carbon/polymer | PEDOT | Lithium chloride and lithium hydroxide | Butan-1-ol, tetrahydrofuran | Polycarbonate | Paper | •Open-circuit voltage around 1.2 V, discharge capacity 0.5 mAh cm² | - | - | • Paper substrate limits battery performance, showing lower discharge capacity. • Performance varies significantly with different electrolyte compositions. | [49] |
| Non-aqueous Lithium-Oxygen | Lithium | Carbon | Lithium bis(trifluoromethanesulfonyl)imide (LiCF3SO3) | TEGDME | Lithiated Nafion | Carbon paper | • Capacity increased to 6840 mAh g⁻¹ on the first discharge • Charge efficiency remained stable over 30 cycles with a relatively low charge voltage of 4.06 V | - | •200 threads per inch (tight mesh) | • Anode deteriorates over repeated charge-discharge cycles due to SEI layer formation, increasing internal resistance and reducing efficiency. | [50] |
| Lithium-ion | Fe/Si multilayer film | Zr-incorporated LiCoO2 (Zr–LiCoO2) | 1 M LiPF6 in a mixture of ethylene carbonate (EC) and diethyl carbonate (DEC) | 2-methoxyethanol and acetic acid | - | Platinum-coated alumina | • Discharge capacity of 274 µAh cm² at first cycle; coulombic efficiency over 96% for Ag-doped films | •The screen printing of Zr–LiCoO2 involved preheating at 150°C and 380°C for 1 hour, followed by final heat treatment at 750°C for 1 hour. | Not detailed | • Electrode material utilization decreases with increased film thickness. • Preparation involves multiple steps, including Zr–LiCoO2 powder via sole-gel process, screen printing, and heat treatments, complicating scaling. | [102] |
| Ni-MH | Zinc/Manganese Dioxide | Nickel Hydroxide | 25% Caustic Potash solution | Not detailed | Not detailed | Roll-fed plastic | • Ni-MH cells showed capacities up to 32mAh, Zinc/Manganese Dioxide up to 20mAh | Not detailed | Not detailed | • Material compatibility issues, with lower conductivity of carbon black increasing internal resistance. | [51] |
| Rechargeable polymer battery | PEDOT | Base current collector layers: Silver followed by a carbon layer. | Gel electrolyte comprising poly(styrene sulfonate sodium) | Deionized water and isopropanol | Hydroxypropyl cellulose | Polyester film | Open circuit voltage 0.60 V, specific capacity 5.5 mAh g^-1, limited cycling capability | • Carbon Ink: Cured at 130°C for 5 minutes • Silver Ink: Cured at 130°C for 5 minutes • PEDOT: PSS Ink: Cured at 130°C for 5 minutes • PEI Layer: Cured at 90°C for 10 minutes | • Squeegee Angle: 45 degrees • Flood Speed: 70 mm/min • Print Speed: 70 mm/min • Snap Off: 2 mm • Squeegee Load: 10 kg | •Limited cycle life and high internal resistance affect long-term reliability and efficiency. | [103] |
| All-solid-state lithium-ion battery | Lithium metal | LiCoO2 | Nb doped Li7La3Zr2O12 (LLZONb) | Not applicable (solid-state) | Ethyl cellulose | Not detailed | 74% of theoretical capacity; 85-100% coulombic efficiency over cycles | - | - | • Ensuring material compatibility between cathode and solid electrolyte to avoid degradation. • Limited energy density compared to liquid electrolyte-based systems. | [104] |
| Leclanché primary battery in solid state | Zinc/Manganese Dioxide | - | NH4Cl | polyethyleneimine (PEI) and Carbopol 940 | Styrene-butadiene rubber, Carboxyl methylcellulose | PET | - | - | - | • Zinc and ammonium chloride interaction leads to material degradation and electrolyte changes. • Managing gas and moisture permeability is challenging to prevent electrolyte drying and maintain battery integrity. | [105] |
| Hybrid supercapacitor | Graphene Oxide | Graphene / CoS2/ Ni3S4 composite | KOH-based hydrogel | Isopropanol | PVDF | Cellulose paper | Energy density of 44.9 Wh kg-1 at power density of 224.8 W kg-1; retains 79.6% capacitance after 10,000 cycles | - | - | •Maintaining material stability during vulcanization and operation is challenging for long-term efficiency. | [106] |
| Al ion battery | Aluminum ink | Graphite ink | "Water-in-salt" AlCl3 | Ethanol-water mixture | PVDF for cathode, CMC for anode. | Cellulose paper | Achieves a high specific capacity of 120 mAh/g with a lifetime of 550 cycles at a lower specific current of 0.25 A/g | - | - | •Cycle stability issues and water electrolysis side reactions reduce energy efficiency. | [54] |
| Lithium Metal Battery | Ag-grid on Cu foil | LFP | 1 M lithium bis(trifluoromethanesulfonyl)imide | 1,2-Dimethoxyethane, 1,3-Dioxolane | - | Cu foil | High Coulombic efficiency of ~97.2%, 700 hours of cyclic stability at 1 mA cm² | It was carried out at a temperature of 120°C for 30 minutes. | • 400 mesh •Printing rate of 20-40 mm/s •Printing angle 45° •Temperature maintained at 25°C during printing. | • Complex preparation involves multiple intricate steps, challenging for industrial scale. • High material and process costs due to silver and specific equipment. | [52] |
| Lithium-ion | Graphite | LFP | LiPF6 in EC/DMC | Distilled water | CMC | Cellulose paper | Capacity ~80 mAh/g | •Initial drying at 110°C for 10 minutes, followed by room temperature drying overnight and a final vacuum drying at 105°C overnight | • DEK Horizon 03i automatic flatbed press •Polyamide nylon, 208 threads per inch •Open Area: 40% •Thread Diameter: 70 µm •Emulsion Thickness: 110 µm •Printing Speed: 30 mm/s •Printing Force: 50 N | • Capacity decay upon cycling is a common issue. • Increased material loading risks delamination, affecting structural integrity. • Residual water in the ink impacts efficiency and capacity due to cellulose's hygroscopic nature. | [53] |