Supplementary Materials: Relating catalytic activity of Cr/HZSM-5 in oxidative dehydrogenation of LPG under external DC electric field to the fermi level position and electrical properties

Amin Alamdari, Ramin Karimzadeh

Figure S1. The XRD patterns of NaZSM-5, H-ZSM-5 and different Cr loaded on H-ZSM-5.

a)

b)

c)

Figure S2. SEM images of the: (a) NaZSM-5; (b) H-ZSM-5; (c) 4%wt. Cr loaded on H-ZSM-5.

Figure S3. FTIR spectra of the NaZSM-5, H-ZSM-5 and 4%wt. Cr loaded on H-ZSM-5.

a)

b)

c)

Figure S4a-c. Comparison between experimental and predicted: (a) yield; (b) conversion; and (c) selectivity.

a)

b)

c)

Figure S5. The perturbation curve for all three responses: (a) yield; (b) conversion; and (c) selectivity

a)

b)

Figure S6a,b. The response surface and contour plots as a function of the temperature and electrical current whereas the gap distance and metal loading are constant at 10 mm and 4wt%, respectively for: (a) LPG conversion; and (b) selectivity.

a)

b)

Figure S7a,b. The response surface and contour plots as a function of the electrical current and metal loading whereas the temperature and gap distance are constant at 625 °C and 10 mm, respectively, for: (a) LPG conversion; and (b) selectivity.

a)

b)

Figure S8a,b. The response surface and contour plots as a function of the electrical current and gap distance whereas the temperature and metal loading are constant at 625 °C and 4%wt., respectively, for: (a) LPG conversion; and (c) selectivity.

Figure S9. Setup of the experiment

# Table S1. Physicochemical properties for all catalyst samples

| Sample | SBET (m2/g) | Smic (m2/g) | SEXT (m2/g) | Vt (cm3/g) | Vmic (cm3/g) | V meso (cm3/g) |
| --- | --- | --- | --- | --- | --- | --- |
| NaZSM-5 | 206.6 | 158.6 | 48 | 0.112 | 0.088 | 0.024 |
| HZSM-5 | 244.8 | 163.4 | 81.4 | 0.132 | 0.090 | 0.040 |
| 0.5%wt. CrHZSM-5 | 231.1 | 158.4 | 72.7 | 0.123 | 0.087 | 0.036 |
| 2.25%wt.CrHZSM-5 | 220.5 | 148.2 | 72.3 | 0.119 | 0.083 | 0.036 |
| 4%wt.CrHZSM-5 | 220.1 | 150.3 | 69.8 | 0.118 | 0.083 | 0.035 |
| 5.75%wt.CrHZSM-5 | 219.9 | 150.8 | 69.1 | 0.117 | 0.082 | 0.035 |
| 7.5%wt.CrHZSM-5 | 218.9 | 152.8 | 66.1 | 0.116 | 0.081 | 0.035 |

Table S2. ANOVA for response surface quadratic models.

| Source | df | yield |  |  | selectivity |  |  | conversion |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Sum of squares | F-value | P-value | Sum of squares | F-value | P-value | Sum of squares | F-value | P-value |
| Model | 14 | 1615.10 | 29.84 | <0.0001 | 3558.59 | 31.36 | <0.0001 | 1579.98 | 31.66 | <0.0001 |
| Residual | 15 | 57.99 |  |  | 121.59 |  |  | 53.47 |  |  |
| Total | 29 | 1673.09 |  |  | 3680.17 |  |  | 1633.45 |  |  |

Table S3. Coefficient of regression, standard error, F and P value

| Term | Coefficient estimate |  |  | Standard Error |  |  | F-value |  |  | P-value |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Y | X | S | Y | X | S | Y | X | S | Y | X | S |
| A | -1.50 | -0.8631 | -0.8653 | 0.40 | 0.58 | 0.39 | 272.32 | 153.01 | 142.91 | < 0.0001 | < 0.0001 | < 0.0001 |
| B | 8.19 | 3.7688 | 11.1420 | 0.40 | 0.58 | 0.39 | 62.30 | 124.83 | 2.52 | < 0.0001 | < 0.0001 | 0.1332 |
| C | -9.55 | -7.4689 | -11.2189 | 0.40 | 0.58 | 0.39 | 6.41 | 7.20 | 1.75 | 0.0230 | 0.0170 | 0.2063 |
| D | 7.30 | -6.0093 | 17.8940 | 0.49 | 0.58 | 0.39 | 29.58 | 53.71 | 1.99 | < 0.0001 | < 0.0001 | 0.1792 |
| AB | -0.01 | 0.0051 | -0.0269 | 0.49 | 0.71 | 0.47 | 8.08 | 0.67 | 41.39 | 0.0123 | 0.4244 | < 0.0001 |
| AC | 0.0067 | -0.0040 | 0.0179 | 0.49 | 0.71 | 0.47 | 1.10 | 0.18 | 8.13 | 0.3111 | 0.6780 | 0.0121 |
| AD | -0.0118 | 0.0041 | -0.0255 | 0.49 | 0.71 | 0.47 | 2.51 | 0.15 | 12.61 | 0.1336 | 0.7068 | 0.0029 |
| BC | 0.0844 | -0.2438 | 0.3406 | 0.49 | 0.71 | 0.47 | 1.06 | 4.23 | 18.75 | 0.3188 | 0.0576 | 0.0006 |
| BD | -0.2016 | 0.3141 | -0.6271 | 0.49 | 0.71 | 0.47 | 4.64 | 5.37 | 48.65 | 0.0479 | 0.0350 | < 0.0001 |
| CD | 0.1212 | -0.3645 | 0.5079 | 0.38 | 0.71 | 0.47 | 0.75 | 3.21 | 14.19 | 0.4016 | 0.0932 | 0.0019 |
| A^2 | 0.0013 | 0.0008 | 0.0008 | 0.38 | 0.54 | 0.36 | 27.09 | 4.70 | 10.39 | 0.0001 | 0.0467 | 0.0057 |
| B^2 | 0.0491 | -0.3058 | 0.4195 | 0.38 | 0.54 | 0.36 | 1.39 | 25.63 | 109.68 | 0.2573 | 0.0001 | < 0.0001 |
| C^2 | 0.1878 | 0.6061 | -0.2162 | 0.38 | 0.54 | 0.36 | 4.01 | 19.89 | 5.76 | 0.0637 | 0.0005 | 0.0299 |
| D^2 | 0.1703 | 0.9506 | -0.3671 | 0.40 | 0.54 | 0.36 | 1.93 | 28.68 | 9.73 | 0.1851 | < 0.0001 | 0.0070 |

Table S4. Obtained optimum values of the process variables and responses.

| Variable | Optimum value |  |  |
| --- | --- | --- | --- |
|  | Yield (%wt.) | Conversion (%) | Selectivity (%) |
| Temperature (°C) | 673.66 | 625.57 | 697.20 |
| Electrical current (mA) | 11.01 | 12 | 3.30 |
| Gap distance (mm) | 6.55 | 9.70 | 10.24 |
| Metal loading (wt.%) | 3.98 | 7.5 | 3.98 |
| Experimental response(%) | 46.94 | 93.29 | 65.29 |
| Predicted response(%) | 47.62 | 94.20 | 64.42 |