Supporting Information

Cost-effective, Highly Selective and Environmentally Friendly Superhydrophobic Absorbent from Cigarette Filters for Oil Spillage Cleanup

Qiancheng Xionga,b, Qiuhong Baia, Cong Lia, Huan Leib, Chaoyun Liub, Yehua Shena,*, Hiroshi Uyamaa,c,*

aKey Laboratory of Synthetic and Natural Functional Molecule Chemistry of Ministry of Education, College of Chemistry and Materials Science, Northwest University, Xi’an 710127, Shaanxi Province, China

bCollege of Pharmaceutical Engineering, Shaanxi Fashion Engineering University, Xi’an 712046, Shaanxi Province, China

cDepartment of Applied Chemistry, Graduate School of Engineering, Osaka University, Suita 565-0871, Japan

*Corresponding author: Tel: +86-29-88302635; E-mail: yhshen@nwu.edu.cn

*Corresponding author. Tel.: +81-6-6879-7364; Fax: +81-6-6879-7367;

E-mail: uyama@chem.eng.osaka-u.ac.jp

Content:

Figure S1. SEM images of unmodified and modified CF: CF0:0 (a), CF1:0 (b), CF4:1 (c), CF3:2 (d), CF1:1 (e), CF2:3 (f), CF1:4 (g), and CF0:1 (h).

Figure S2. SEM images of SiO2 particles (a) and (b) at different magnification, SiO2/OTS (c), and SiO2/OTS/MTMS (d).

Figure S3. SEM images of CF modified by SiO2/OTS (a and b), and CF modified by SiO2/OTS/MTMS (c and d) at different magnification.

Figure S4. EDX spectra of unmodified and modified CF: CF0:0 (a), CF1:0 (b), CF4:1 (c), CF3:2 (d), CF1:1 (e), CF2:3 (f), CF1:4 (g), and CF0:1 (h).

Figure S5. Wide scan of XPS spectra of unmodified and modified CF (a) and high-resolution spectrum for Si 2p of CF1:1 (b).

Figure S6. TGA thermograms of the CF and CF3:2

Figure S7. Selectivity test of oil absorption by CF3:2.

Figure S8. Pump oil absorption of unmodified and modified CF: CF0:0 (a), CF1:0 (b), CF4:1 (c), CF3:2 (d), CF1:1 (e), CF2:3 (f), CF1:4 (g), and CF0:1 (h).

Figure S9. Silicone oil absorption of unmodified and modified CF: CF0:0 (a), CF1:0 (b), CF4:1 (c), CF3:2 (d), CF1:1 (e), CF2:3 (f), CF1:4 (g), and CF0:1 (h).

Table S1. Recycling of used cigarette filters

Video S1. CF3:2 floated from the bottom of the water to the top.

Video S2. Water droplet flowed away quickly from CF3:2.

Video S3. CF3:2 had completely adsorbed the pump oil with 6 s.

Video S4. CF3:2 was reused, and the absorbed pump oil could be readily recovered by simple mechanical squeezing.

20 µm

(a)

(b)

Figure S1. SEM images of unmodified and modified CF: CF0:0 (a), CF1:0 (b), CF4:1 (c), CF3:2 (d), CF1:1 (e), CF2:3 (f), CF1:4 (g), and CF0:1 (h).

Figure S2. SEM images of SiO2 particles (a) and (b) at different magnification, SiO2/OTS (c), and SiO2/OTS/MTMS (d).

Figure S3. SEM images of CF (a and b), CF modified by SiO2/OTS (a and b), and CF modified by SiO2/OTS/MTMS (c and d) at different magnification.

Figure S4. EDX spectra of unmodified and modified CF: CF0:0 (a), CF1:0 (b), CF4:1 (c), CF3:2 (d), CF1:1 (e), CF2:3 (f), CF1:4 (g), and CF0:1 (h).

Figure S5. Wide scan of XPS spectra of unmodified and modified CF (a) and high-resolution spectrum for Si 2p of CF1:1 (b).

Figure S6. TGA thermograms of the CF and CF3:2

Figure S7. Selectivity test of oil absorption by CF3:2.

Figure S8. Pump oil absorption of unmodified and modified CF: CF0:0 (a), CF1:0 (b), CF4:1 (c), CF3:2 (d), CF1:1 (e), CF2:3 (f), CF1:4 (g), and CF0:1 (h).

Figure S9. Silicone oil absorption of unmodified and modified CF: CF0:0 (a), CF1:0 (b), CF4:1 (c), CF3:2 (d), CF1:1 (e), CF2:3 (f), CF1:4 (g), and CF0:1 (h).

Table S1. Recycling of used cigarette filters