Valorization of Agroindustrial wastes from Maranhão (Brazil) as a support for the immobilization of lipase from Thermomyces lanuginosus and application in the synthesis of hexyl laurate

Regiane K. S. Lira,1 Rochele T. Zardini,2 Marcela C. C. de Carvalho,3 Robert Wojcieszak,4 Selma G. F. Leite1 and Ivaldo Itabaiana Jr1,4*

1 - Federal University of Rio de Janeiro, Department of Biochemical Engineering, School of Chemistry, RJ, 21941-909, Brazil

2 - Federal University of Rio de Janeiro, Campus Xerém, RJ, 25245-390, Brazil

3 - Federal University of Rio de Janeiro, Chemistry Institute, RJ, 21941-909, Brazil.

4 - Univ. Lille, CNRS, Centrale Lille, Univ. Artois, UMR 8181 – UCCS – Unité de Catalyse et Chimie du Solide, F-59000 Lille, France

*Corresponding author: ivaldo@eq.ufrj.br

Supporting Information

Figura S1 – Espectro de FTIR do laurato de hexila obtido a partir da reação de esterificação do ácido láurico e n-hexanol catalisado pela TLL imobilizada em suporte MB (mesocarpo de babaçu).   1739 cm-1 (éster) e 1708 cm-1 (ácido orgânico). Condições de análise: Espectrofotômetro Thermo-Nicolet Magna® (IR 760), na faixa espectral de 400 - 4000 cm-1.

1708

1739

Table 1 – Chemical composition of agro-industrial wastes studied.

| Chemical composition (%) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Support | CNHS (%) |  |  |  | Cellulose | Hemicellulose | Lignin | Free Protein | Umidity (%) | Ash (%) |
|  | C | N | H | S |  |  |  |  |  |  |
| CG | 57,36 ± 0,4 | 3,87 ± 0,41 | 6,64 ± 0,14 | ˂1 | 7,69 ± 0,6 | 30,78 ± 0,1 | 28,11 ± 0,5 | 0,25 ± 0,1 | 6,68 ± 0,1 | 0,38 ± 0,0 |
| SC | 44,43 ± 0,1 | 1,40 ± 0,51 | 5,61 ± 0,24 | ˂1 | 32,38 ± 0,1 | 12,99 ± 0,0 | 21,34 ± 0,5 | 0,07 ± 0,1 | 4,66 ± 0,1 | 14,79 ± 0,1 |
| BM | 40,23 ± 0,6 | 2,39 ± 0,18 | 5,52 ± 0,64 | ˂1 | 50,25 ± 0,3 | 8,77 ± 0,7 | 7,90 ± 0,3 | 0,12 ± 0,1 | 9,62 ± 0,1 | 0,35 ± 0,3 |
| CC | 43,66 ± 0,7 | 2,84 ± 0,46 | 5,58 ± 0,52 | ˂1 | 33,38 ± 0,3 | 31,72 ± 0,6 | 8,55 ± 0,1 | 0,09 ± 0,1 | 9,56 ± 0,1 | 0,57 ± 0,1 |
| RH | 42,35 ± 0,2 | 2,56 ± 0,05 | 4,91 ± 0,52 | ˂1 | 37,10 ± 0,9 | 12,53 ± 0,6 | 18,08 ± 0,1 | 0,13 ± 0,1 | 9,94 ± 0,1 | 0,52 ± 0,1 |