Supporting Information

Heterogeneous double metal cyanide catalyzed synthesis of poly(ε-caprolactone) polyols for the preparation of thermoplastic elastomers

Chinh Hoang Tran, Min Woong Lee, Sang Woo Park, Jae Eon Jeong, Soo Jeong Lee, Wenliang Song, PilHo Huh*, and Il Kim*

Department of Polymer Science and Engineering, Pusan National University, Busandaehag-ro 63-2, Geumjeong-gu, Busan 46241, Republic of Korea.
* Correspondence: IK: ilkim@pusan.ac.kr; PH: pilho.huh@pusan.ac.kr

# Table of Contents

Table of Contents	S2

1. Supplementary figures	S6

1.1 Characterization of DMC catalysts	S6

Fig. S1 Characterization of the DMC catalysts used in this work. (a) FTIR spectra, (b) XPS spectra, and (c) XRD patterns.	S6

1.2 Polymerization of lactones	S7

Fig. S2 1H NMR spectrum (400 MHz, CDCl3) of the crude reaction mixture of CL without using initiator after 24 h. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, Tp = 120 °C.	S7

Fig. S3 1H NMR spectrum (400 MHz, CDCl3) of the crude reaction mixture of CL polymerization using PPG400 initiator (run 1 of Table 1). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[PPG400]0 = 10, Tp = 120 °C.	S7

Fig. S4 1H NMR spectrum (400 MHz, CDCl3) of the crude reaction mixture of CL polymerization using EG initiator (run 2 of Table 1). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[EG]0 = 10, Tp = 120 °C.	S8

Fig. S5 1H NMR spectrum (400 MHz, CDCl3) of the crude reaction mixture of CL polymerization using PG initiator (run 3 of Table 1). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[PG]0 = 10, Tp = 120 °C.	S8

Fig. S6 1H NMR spectrum (400 MHz, CDCl3) of the crude reaction mixture of CL polymerization using GL initiator (run 4 of Table 1). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[GL]0 = 10, Tp = 120 °C.	S9

Fig. S7 1H NMR spectrum (400 MHz, CDCl3) of the crude reaction mixture of CL polymerization using EG initiator (run 6 of Table 1). Conditions: DMC-TBA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[I]0 = 10, Tp = 160 °C.	S9

Fig. S8 1H NMR spectrum (400 MHz, CDCl3) of the crude reaction mixture of CL polymerization using EG initiator (run 7 of Table 1). Conditions: DMC-IBN = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[I]0 = 10, Tp = 160 °C.	S10

Fig. S9 1H NMR spectrum (400 MHz, CDCl3) of the PCL produced by SB initiator (run 10 of Table 1). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[I]0 = 10, Tp = 120 °C.	S10

Fig. S10 GPC curves of the resultant PCLs using different initiators (run 1–4 of Table 1). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [M]0 = 9 M, [M]0/[I]0 = 10, Tp = 120 °C.	S11

Fig. S11 MALDI-TOF MS spectrum of PG-PCL (Table 1, run 5). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [M]0 = 9 M, [M]0/[PG]0 = 10, Tp = 160 °C.	S11

Fig. S12 MALDI-TOF MS spectrum of GL-PCL (Table 1, run 6). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [M]0 = 9 M, [M]0/[GL]0 = 10, Tp = 160 °C.	S12

Fig. S13 MALDI-TOF MS spectrum of SB-PCL (Table 1, run 7). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [M]0 = 9 M, [M]0/[SB]0 = 10, Tp = 160 °C.	S12

Fig. S14 Recycling experiment of the ROP of CL using DMC-EAA catalyst.	S13

Fig. S15 GPC curves of the PCLs obtained using various amount of PG initiator. Condition: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, reaction temperature: 160 °C.	S13

Fig. S16 GPC curves of the PCLs obtained using various amount of GL initiator. Condition: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, reaction temperature: 160 °C.	S14

Fig. S17 GPC curves of the resultant PCLs using different ILs. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[GL]0 = 10, [IL]0/[Zn]0 = 2.5, Tp = 160 °C.	S14

Fig. S18 GPC curves of the resultant PCLs using various amount of PG in the presence of BMIMCl (IL). Conditions: DMC-EAA = 10 mg [Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [IL]0/[Zn]0 = 2.5, Tp = 160 °C.	S15

Fig. S19 GPC curves of the resultant PCLs using various amount of GL in the presence of BMIMCl (IL). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [IL]0/[Zn]0 = 2.5, Tp = 160 °C.	S15

Fig. S20 GPC curves of the resultant PCLs using various amount of BMIMCl (IL). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[PG]0 = 10, Tp = 160 °C.	S16

1.3 Kinetic Studies	S17

Fig. S21 1H NMR (400 MHz, CD3OD) spectra of the PCL collected at different intervals. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[GL]0 = 20, Tp = 130 °C. Dashed lines denote the monomer signals.	S17

Fig. S22 1H NMR (400 MHz, CD3OD) spectra of the PCL collected at different intervals. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[GL]0 = 20, Tp = 140 °C. Dash lines denote the monomer signals.	S17

Fig. S23 1H NMR (400 MHz, CDCl3) spectra of the PCL collected at different intervals. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[GL]0 = 20, Tp = 150 °C. Dash lines denote the monomer signals.	S18

Fig. S24 1H NMR (400 MHz, CDCl3) spectra of the PCL collected at different intervals. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[GL]0 = 20, Tp = 160 °C. Dash lines denote the monomer signals.	S18

Fig. S25 1H NMR (400 MHz, CDCl3) spectra of the PCL collected at different intervals. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[SB]0 = 20, Tp = 160 °C. Dash lines denote the monomer signals.	S19

Fig. S26 GPC curves of PCL collected at different intervals. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[GL]0 = 20, Tp = 140 °C.	S20

Fig. S27 Plots of Mn and Ð versus (a) monomer conversion (xp) and (b) polymerization time in Fig. S26.	S20

Fig. S28 GPC curves of PCL collected at different intervals. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[GL]0 = 20, Tp = 150 °C.	S21

Fig. S29 Plots of Mn and Ð versus (a) monomer conversion (xp) and (b) polymerization time in Fig. S28.	S21

Fig. S30 GPC curves of PCL collected at different intervals. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[GL]0 = 20, Tp = 160 °C.	S22

Fig. S31 Plots of Mn and Ð versus (a) monomer conversion (xp) and (b) polymerization time in Fig. S30.	S22

1.4 Copolymerization of CL with Glycidol	S23

Fig. S32 1H NMR spectrum (400 MHz, CDCl3) of the copolymerization of  CL with glycidol (G) in CDCl3. Condition: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[G]0 = 7 : 3, Tp = 160 °C.	S23

Fig. S33 1H NMR spectrum (400 MHz, CDCl3) of the copolymerization of  CL with glycidol (G) in CDCl3. Condition: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[G]0 = 6 : 4, Tp = 160 °C.	S23

Fig. S34 1H NMR spectrum (400 MHz, CDCl3) of the copolymerization of  CL with glycidol (G) in CDCl3. Condition: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[G]0 = 5 : 5, Tp = 160 °C.	S24

Fig. S35 2D NMR spectra (400 MHz, CDCl3) of the copolymerization of  CL with glycidol (G) in CDCl3. Condition: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[G]0 = 6 : 4, Tp = 160 °C.	S24

Fig. S36 13C NMR spectra (400 MHz, CDCl3) of the PCL (top) and branched PCL (bottom) obtained from the copolymerization of  CL with glycidol (G). Condition: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[G]0 = 7 : 3, Tp = 160 °C.	S25

Fig. S37 1H NMR (400 MHz, CDCl3) spectra of the copolymerization of CL with glycidol (G) collected at different intervals. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[G]0 = 5/5, Tp = 160 °C.	S25

Fig. S38 GPC curves of the resultant copolymers obtained from the copolymerization of CL and glycidol (G). Condition: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, Tp = 160 °C.	S26

1.5 Synthesis of TPEs and TPUs	S27

Fig. S39 1H-NMR spectrum of the PCL-TPE-1 produced by EG-PCL-1000 diol.	S27

Fig. S40 1H-NMR spectrum of the PCL-TPE-3 produced by PG-PCL-1000 diol.	S27

Fig. S41 1H-NMR spectrum of the TPEE produced by PTMEG-1000 diol.	S28

Fig. S42 1H-NMR spectrum of the PCL-TPU produced by PG-PCL-1000 diol.	S28

Fig. S43 1H-NMR spectrum of the TPU produced by PTMEG-1000 diol.	S29

Fig. S44 FTIR spectra of the TPU and PCL-TPU produced by PTMEG-1000 and PG-PCL-1000 diols, respectively.	S29

Fig. S45 (a) TGA and (b) DTG curves for TPEE, PCL-TPE-1, and PCL-TPE-3 produced by PTMEG-1000, EG-PCL-1000, and PG-PCL-1000 diols, respectively.	S30

Fig. S46 (a) TGA and (b) DTG curves for TPU and PCL-TPU produced by PTMEG-1000 and PG-PCL-1000 diols, respectively.	S30

Fig. S47 DSC curves for TPEE, PCL-TPE-1, and PCL-TPE-3 produced by PTMEG-1000, EG-PCL-1000, and PG-PCL-1000 diols, respectively: (a) during cooling from melt, (b) during second heating run.	S31

Fig. S48 DSC curves for TPU and PCL-TPU produced by PTMEG-1000 and PG-PCL-1000 diols, respectively during second heating run.	S31

Fig. S49 Stress–strain curves for PCL-TPEs produced by PG-PCL diols with different molecular weights conducted at a crosshead speed of 100 mm min−1 (Table 5).	S32

2. Supplementary Schemes	S33

Scheme S1 Proposed mechanism for the copolymerization of CL and glycidol using DMC catalyst.	S33

Scheme S2 Synthesis of PCL-TPEs using PCL diols.	S33

Scheme S3 Synthesis of PCL-TPU using PG-PCL diol.	S34

3. Supplementary tables	S35

Table S1 Results of the batch ROP of CL by DMC catalyst using various amount of PG and BMIMCl (IL)a	S35

Table S2 Results of the batch ROP of CL in IL by DMC catalyst using various amount of GLa	S36

# 1. Supplementary figures

## 1.1 Characterization of DMC catalysts

### Fig. S1 Characterization of the DMC catalysts used in this work. (a) FTIR spectra, (b) XPS spectra, and (c) XRD patterns.

## 1.2 Polymerization of lactones

### Fig. S2 1H NMR spectrum (400 MHz, CDCl3) of the crude reaction mixture of CL without using initiator after 24 h. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, Tp = 120 °C.

### Fig. S3 1H NMR spectrum (400 MHz, CDCl3) of the crude reaction mixture of CL polymerization using PPG400 initiator (run 1 of Table 1). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[PPG400]0 = 10, Tp = 120 °C.

### Fig. S4 1H NMR spectrum (400 MHz, CDCl3) of the crude reaction mixture of CL polymerization using EG initiator (run 2 of Table 1). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[EG]0 = 10, Tp = 120 °C.

### Fig. S5 1H NMR spectrum (400 MHz, CDCl3) of the crude reaction mixture of CL polymerization using PG initiator (run 3 of Table 1). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[PG]0 = 10, Tp = 120 °C.

### Fig. S6 1H NMR spectrum (400 MHz, CDCl3) of the crude reaction mixture of CL polymerization using GL initiator (run 4 of Table 1). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[GL]0 = 10, Tp = 120 °C.

### Fig. S7 1H NMR spectrum (400 MHz, CDCl3) of the crude reaction mixture of CL polymerization using EG initiator (run 6 of Table 1). Conditions: DMC-TBA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[I]0 = 10, Tp = 160 °C.

### Fig. S8 1H NMR spectrum (400 MHz, CDCl3) of the crude reaction mixture of CL polymerization using EG initiator (run 7 of Table 1). Conditions: DMC-IBN = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[I]0 = 10, Tp = 160 °C.

### Fig. S9 1H NMR spectrum (400 MHz, CDCl3) of the PCL produced by SB initiator (run 10 of Table 1). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[I]0 = 10, Tp = 120 °C.

### Fig. S10 GPC curves of the resultant PCLs using different initiators (run 1–4 of Table 1). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [M]0 = 9 M, [M]0/[I]0 = 10, Tp = 120 °C.

### Fig. S11 MALDI-TOF MS spectrum of PG-PCL (Table 1, run 5). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [M]0 = 9 M, [M]0/[PG]0 = 10, Tp = 160 °C.

### Fig. S12 MALDI-TOF MS spectrum of GL-PCL (Table 1, run 6). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [M]0 = 9 M, [M]0/[GL]0 = 10, Tp = 160 °C.

### Fig. S13 MALDI-TOF MS spectrum of SB-PCL (Table 1, run 7). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [M]0 = 9 M, [M]0/[SB]0 = 10, Tp = 160 °C.

### Fig. S14 Recycling experiment of the ROP of CL using DMC-EAA catalyst.

### Fig. S15 GPC curves of the PCLs obtained using various amount of PG initiator. Condition: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, reaction temperature: 160 °C.

### Fig. S16 GPC curves of the PCLs obtained using various amount of GL initiator. Condition: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, reaction temperature: 160 °C.

### Fig. S17 GPC curves of the resultant PCLs using different ILs. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[GL]0 = 10, [IL]0/[Zn]0 = 2.5, Tp = 160 °C.

### Fig. S18 GPC curves of the resultant PCLs using various amount of PG in the presence of BMIMCl (IL). Conditions: DMC-EAA = 10 mg [Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [IL]0/[Zn]0 = 2.5, Tp = 160 °C.

### Fig. S19 GPC curves of the resultant PCLs using various amount of GL in the presence of BMIMCl (IL). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [IL]0/[Zn]0 = 2.5, Tp = 160 °C.

### Fig. S20 GPC curves of the resultant PCLs using various amount of BMIMCl (IL). Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[PG]0 = 10, Tp = 160 °C.

## 1.3 Kinetic Studies

### Fig. S21 1H NMR (400 MHz, CD3OD) spectra of the PCL collected at different intervals. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[GL]0 = 20, Tp = 130 °C. Dashed lines denote the monomer signals.

### Fig. S22 1H NMR (400 MHz, CD3OD) spectra of the PCL collected at different intervals. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[GL]0 = 20, Tp = 140 °C. Dash lines denote the monomer signals.

### Fig. S23 1H NMR (400 MHz, CDCl3) spectra of the PCL collected at different intervals. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[GL]0 = 20, Tp = 150 °C. Dash lines denote the monomer signals.

### Fig. S24 1H NMR (400 MHz, CDCl3) spectra of the PCL collected at different intervals. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[GL]0 = 20, Tp = 160 °C. Dash lines denote the monomer signals.

### Fig. S25 1H NMR (400 MHz, CDCl3) spectra of the PCL collected at different intervals. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[SB]0 = 20, Tp = 160 °C. Dash lines denote the monomer signals.

### Fig. S26 GPC curves of PCL collected at different intervals. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[GL]0 = 20, Tp = 140 °C.

### Fig. S27 Plots of Mn and Ð versus (a) monomer conversion (xp) and (b) polymerization time in Fig. S26.

### Fig. S28 GPC curves of PCL collected at different intervals. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[GL]0 = 20, Tp = 150 °C.

### Fig. S29 Plots of Mn and Ð versus (a) monomer conversion (xp) and (b) polymerization time in Fig. S28.

### Fig. S30 GPC curves of PCL collected at different intervals. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[GL]0 = 20, Tp = 160 °C.

### Fig. S31 Plots of Mn and Ð versus (a) monomer conversion (xp) and (b) polymerization time in Fig. S30.

## 1.4 Copolymerization of CL with Glycidol

### Fig. S32 1H NMR spectrum (400 MHz, CDCl3) of the copolymerization of  CL with glycidol (G) in CDCl3. Condition: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[G]0 = 7 : 3, Tp = 160 °C.

### Fig. S33 1H NMR spectrum (400 MHz, CDCl3) of the copolymerization of  CL with glycidol (G) in CDCl3. Condition: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[G]0 = 6 : 4, Tp = 160 °C.

### Fig. S34 1H NMR spectrum (400 MHz, CDCl3) of the copolymerization of  CL with glycidol (G) in CDCl3. Condition: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[G]0 = 5 : 5, Tp = 160 °C.

### Fig. S35 2D NMR spectra (400 MHz, CDCl3) of the copolymerization of  CL with glycidol (G) in CDCl3. Condition: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[G]0 = 6 : 4, Tp = 160 °C.

### Fig. S36 13C NMR spectra (400 MHz, CDCl3) of the PCL (top) and branched PCL (bottom) obtained from the copolymerization of  CL with glycidol (G). Condition: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[G]0 = 7 : 3, Tp = 160 °C.

### Fig. S37 1H NMR (400 MHz, CDCl3) spectra of the copolymerization of CL with glycidol (G) collected at different intervals. Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, [CL]0/[G]0 = 5/5, Tp = 160 °C.

### Fig. S38 GPC curves of the resultant copolymers obtained from the copolymerization of CL and glycidol (G). Condition: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M), [CL]0 = 9 M, Tp = 160 °C.

## 1.5 Synthesis of TPEs and TPUs

### Fig. S39 1H-NMR spectrum of the PCL-TPE-1 produced by EG-PCL-1000 diol.

### Fig. S40 1H-NMR spectrum of the PCL-TPE-3 produced by PG-PCL-1000 diol.

### Fig. S41 1H-NMR spectrum of the TPEE produced by PTMEG-1000 diol.

### Fig. S42 1H-NMR spectrum of the PCL-TPU produced by PG-PCL-1000 diol.

### Fig. S43 1H-NMR spectrum of the TPU produced by PTMEG-1000 diol.

### Fig. S44 FTIR spectra of the TPU and PCL-TPU produced by PTMEG-1000 and PG-PCL-1000 diols, respectively.

### Fig. S45 (a) TGA and (b) DTG curves for TPEE, PCL-TPE-1, and PCL-TPE-3 produced by PTMEG-1000, EG-PCL-1000, and PG-PCL-1000 diols, respectively.

### Fig. S46 (a) TGA and (b) DTG curves for TPU and PCL-TPU produced by PTMEG-1000 and PG-PCL-1000 diols, respectively.

### Fig. S47 DSC curves for TPEE, PCL-TPE-1, and PCL-TPE-3 produced by PTMEG-1000, EG-PCL-1000, and PG-PCL-1000 diols, respectively: (a) during cooling from melt, (b) during second heating run.

### Fig. S48 DSC curves for TPU and PCL-TPU produced by PTMEG-1000 and PG-PCL-1000 diols, respectively during second heating run.

### Fig. S49 Stress–strain curves for PCL-TPEs produced by PG-PCL diols with different molecular weights conducted at a crosshead speed of 100 mm min−1 (Table 5).

# 2. Supplementary Schemes

### Scheme S1 Proposed mechanism for the copolymerization of CL and glycidol using DMC catalyst.

### Scheme S2 Synthesis of PCL-TPEs using PCL diols.

### Scheme S3 Synthesis of PCL-TPU using PG-PCL diol.

# 3. Supplementary tables

### Table S1 Results of the batch ROP of CL by DMC catalyst using various amount of PG and BMIMCl (IL)a

| Run | [IL]0/[Zn]0 | [CL]0/[PG]0 | tb (h) | xpc (%) | GPC |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Mn | Ð |
| 1 | 2.5 | 100 | 12 | 17 | 3740 | 1.05 |
| 2 | 2.5 | 50 | 10 | 56 | 2500 | 1.07 |
| 3 | 2.5 | 20 | 8 | 62 | 1700 | 1.03 |
| 4 | 2.5 | 10 | 8 | 91 | 1400 | 1.11 |
| 5 | 2.5 | 5 | 8 | 86 | 1100 | 1.01 |
| 6 | 1.25 | 10 | 8 | 58 | 1220 | 1.02 |
| 7 | 3.0 | 10 | 8 | 61 | 1240 | 1.01 |
| 8 | 4.0 | 10 | 8 | 58 | 1310 | 1.02 |
| 9 | 5.0 | 10 | 8 | 84 | 1470 | 1.08 |
| 10 | [IL]0d | 10 | 12 | < 3 | – | – |

a Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M); [CL]0 = 9 M; Tp = 160 °C. b Reaction time. c Monomer conversion determined by 1H NMR. d The polymerization was performed in the absence of DMC catalyst.

### Table S2 Results of the batch ROP of CL in IL by DMC catalyst using various amount of GLa

| Run | ILb | [CL]0/[GL]0 | tc (h) | xpd (%) | GPC |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Mn | Ð |
| 1 | BMIMCl | 100 | 12 | 31 | 4050 | 1.01 |
| 2 | BMIMCl | 50 | 10 | 65 | 2750 | 1.02 |
| 3 | BMIMCl | 20 | 8 | 89 | 2520 | 1.07 |
| 4 | BMIMCl | 10 | 8 | 95 | 1730 | 1.11 |
| 5 | BMIMCl | 5 | 8 | 95 | 1280 | 1.06 |
| 6 | TMAP | 10 | 8 | 24 | 1900 | 1.16 |
| 7 | TEAB | 10 | 8 | 29 | 2340 | 1.32 |
| 8 | TDAB | 10 | 8 | 29 | 2510 | 1.26 |

a Conditions: DMC-EAA = 10 mg ([Zn]0 = 30 × 10−3 M); [CL]0 = 9 M; Tp = 160 °C. b Ionic liquid: [IL]0/[Zn]0 = 2.5. c Reaction time. d Monomer conversion determined by 1H NMR.