Supplementary Information

Photocatalytic degradation of fluoroquinolone antibiotics in solution

Abniel Machín1*, Kenneth Fontánez2, José Duconge3, María Cotto3, Florian I. Petrescu4, Carmen Morant5, Francisco Márquez3*

1	Arecibo Observatory, Universidad Ana G. Méndez-Cupey Campus, 00926PR, United States

2	Department of Chemistry, University of Puerto Rico, Rio Piedras Campus, San Juan, 00925PR, United States

3 	Nanomaterials Research Group, School of Natural Sciences and Technology, Universidad Ana G. Méndez-Gurabo Campus, 00778PR, United States

4	IFToMM-ARoTMM, Bucharest Polytechnic University, Bucharest, (CE), Romania

5	Department of Applied Physics, Autonomous University of Madrid and Instituto de Ciencia de Materiales Nicolas Cabrera, 28041, Spain

*	Correspondence: fmarquez@uagm.edu (FM), machina1@uagm.edu (AM)

Figure S1. Evaluation of the initial concentration of CFX (a) and LFX (b) on the catalytic efficiency of 10%Au@ZnONPs, 10%Au@ZnONPs-3%rGO, and 10%Au@ZnONPs-3%rGO-3%gC3N4 in the photodegradation reaction.

Figure S2. Evaluation of the initial concentration of 10%Au@ZnONPs, 10%Au@ZnONPs-3%rGO, and 10%Au@ZnONPs-3%rGO-3%gC3N4 on the efficiency of the photodegradation reaction of CFX (a) and LFX (b).

Figure S3. Pseudo-first order kinetics of photodegradation of CFX (a) and LFX (b) using different catalysts.

Figure S4. Control experiments for 10%Au@ZnONPs-3%rGO-3%gC3N4 with CFX (a) and LFX (b), under visible radiation.

Figure S5. Recyclability of 10%Au@ZnONPs-3%rGO-3%gC3N4 after five consecutive catalytic cycles of photodegradation of CFX (a) and LFX (b) under visible radiation.

Figure S6. Photocatalytic activity of 10%Au@ZnONPs-3%rGO-3%gC3N4 on the degradation of CFX (a) and LFX (b) in the presence of various scavengers under visible radiation.

Table S1. The pseudo-first-order kinetics constants for the photodegradation of CFX and LFX.

| Material | Apparent rate CFX1 | Apparent rate LFX1 |
| --- | --- | --- |

| 1%Au@ZnONPs 5%Au@ZnONPs 10%Au@ZnONPs 1%Au@ZnONPs-3%rGO 5%Au@ZnONPs-3%rGO 10%Au@ZnONPs-3%rGO 1%Au@ZnONPs-3%rGO-3%gC3N4 5%Au@ZnONPs-3%rGO-3%gC3N4 10%Au@ZnONPs-3%rGO-3%gC3N4 | 0.008 0.004 0.012 0.006 0.026 0.009 0.009 0.011 0.013 0.016 0.024 0.019 0.018 0.014 0.022 0.021 0.028 0.023 |
| --- | --- |

1(k, min-1)