Article

Lignin-based ILs as corrosion inhibitors

Sharon Monaci1,2; Daniela Minudri1; Lorenzo Guazzelli3; Andrea Mezzetta3; David Mecerreyes1,4; Maria Forsyth 1,2,4; Anthony Somers2*

1	POLYMAT, University of the Basque Country, UPV/EHU,20018 Donostia-San Sebastian, Spain.

2	Institute for Frontier Materials, Deakin University, Burwood, VIC 3125, Australia.

3	Universita di Pisa, Dipartimento di Farmacia, Via B. Pisano, 12, 56126 Pisa, Italy

4	IKERBASQUE Basque Foundation for Science, 48009 Bilbao, Spain.

*	 Correspondence: anthony.somers@deakin.edu.au

Figure S1 Bode plot (left) and Cyclic Potentiodynamic Polarization (right) results of AS1020 mild steel after 24h at OCV in control (0.01M NaCl; dotted line) and inhibited solutions (0.01M NaCl + 5 mM inhibitor).

Figure S2 EDS data of mild steel immersed in 0.01M NaCl + [Emim]Gal 10 mM (a); 0.01M NaCl + [Emim]Syr 10 mM (b) after 24h.

|  | (Wt%) |  |
| --- | --- | --- |
| Fe |  | 95 |
| O |  | 0 |
| C |  | 5 |
| N |  | - |

(b)

(a)

|  | (Wt%) |  |
| --- | --- | --- |
| Fe |  | 67.6 |
| O |  | 1.8 |
| C |  | 30.0 |
| N |  | - |

Figure S3 EDS data of mild steel immersed in 0.01M NaCl + [Emim]Gal 10 mM (a); 0.01M NaCl + [Emim]Syr 10 mM (b) after 24h.

|  | (Wt%) |  |
| --- | --- | --- |
| Fe |  | 91.5 |
| O |  | 7.0 |
| C |  | 1.5 |
| N |  | - |

(b)

(a)

|  | (Wt%) |
| --- | --- |
| Fe | 91.4 |
| O | 3.1 |
| C | 5.0 |
| N | 0.5 |

1

3

2

4

|  | 1 | 2 | 3 | 4 |
| --- | --- | --- | --- | --- |
|  | (Wt%) |  |  |  |
| Fe | 91.8 | 34.2 | 25.0 | 83.1 |
| O | 1.0 | 24.3 | 25.6 | 8.3 |
| C | 6.5 | 36.0 | 45.1 | 8.1 |
| N | 0.7 | 5.3 | 4.2 | 0.4 |

Figure S4 EDS data of 3 different zones (1,4: mild steel surface; 2,3: inhibitor deposits) of mild steel immersed in 0.01M NaCl + [Chol]Gal 10 mM (b); 0.01M NaCl + [Chol]Syr 10 mM (b) after 24h.

|  | Sa (µm) | σ |
| --- | --- | --- |
| Pristine control | 0.101 | 0.005 |
| [Emim]Gal | 0.27 | 0.04 |
| [Emim]Syr | 0.24 | 0.03 |
| [Chol]Gal | 0.161 | 0.004 |
| [Chol]Syr | 0.109 | 0.007 |

Table S1. Average area roughness of mild steel samples immersed in the inhibited solutions containing 0.01M NaCl and the inhibitor 10 mM, compared to pristine control immersed in 0.01M NaCl.

Table_label. Average area roughness of mild steel samples immersed in the inhibited solutions containing 10 mM of the inhibitors.

Figure S5 1H NMR and 13C NMR spectra of [Emim]Gal

Figure S6 1H NMR and 13C NMR spectra of [Emim]Syr

Figure S7 1H NMR and 13C NMR spectra of [Emim]Van

Figure S8 1H NMR and 13C NMR spectra of [Chol]Gal

Figure S9 1H NMR and 13C NMR spectra of [Chol]Syr

Figure S10 1H NMR and 13C NMR spectra of [Chol]Van

Figure S11 1H NMR and 13C NMR spectra of [DBU]Gal

Figure S12 1H NMR and 13C NMR spectra of [DBU]Syr

Figure S13 1H NMR and 13C NMR spectra of [DBU]Van

Figure S14 Thermogravimetric and derivative curves of [Emim]Gal

Figure S15 Thermogravimetric and derivative curves of [Emim]Syr

Figure S16 Thermogravimetric and derivative curves of [Emim]Van

Figure S17 Thermogravimetric and derivative curves of [Chol]Gal

Figure S18 Thermogravimetric and derivative curves of [Chol]Syr

Figure S19 Thermogravimetric and derivative curves of [Chol]Van

Figure S20 Thermogravimetric and derivative curves of [DBU]Gal

Figure S21 Thermogravimetric and derivative curves of [DBU]Syr

Figure S22 Thermogravimetric and derivative curves of [DBU]Van

Figure S23 DSC curve of [Emim]Gal

Figure S24 DSC curves of 1st and 2nd heating run of [Emim]Syr

Figure S25 DSC curve of [Emim]Van

Figure S26 DSC curves of 1st and 2nd heating run of [Chol]Gal

Figure S27 DSC curves of 1st and 2nd heating run of [Chol]Syr

Figure S28 DSC curve of [Chol]Van

Figure S29 DSC curves of [DBU]Gal

Figure S30 DSC curves of [DBU]Syr

Figure S31 DSC curves of [DBU]Van