Supplemental Table 1 Amount of Fe catalyst on AlN and its standard deviation in X-ray fluorescence (XRF) measurement

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
|  | Fe content  (×10-2 mass%) | Al content  (mass%) | Fe/Al ratio | |
| Value (×10-3) | STD (×10-5) |
| Vacuum filtration | 2.42 | 10.6 | 2.28 | 2.80 |
| Dip coating | 2.51 | 12.4 | 2.03 | 9.82 |