Support information

Thermal Surface Properties, London Dispersive and Polar Surface Energy of Graphene and Carbon Materials by Inverse Gas Chromatography at Infinite Dilution

Tayssir Hamieh1,2

1Faculty of Science and Engineering, Maastricht University, P.O. Box 616, 6200 MD Maastricht, Netherlands, E-mail: t.hamieh@maastrichtuniversity.nl

2Laboratory of Materials, Catalysis, Environment and Analytical Methods (MCEMA), Faculty of Sciences, Lebanese University, 1533, Hadath, Lebanon

(a)

(b)

(c)

(d)

(e)

Figure S1. Variations of RTlnVn(T) of n-alkanes and polar molecules adsorbed on the various solid materials against the temperature. (a): Graphene, (b): Graphene oxide, (c): Reduced graphene oxide, (d) Untreated carbon fibers, and (e): Oxidized carbon fibers.

Table S1. Values of -∆GapT (in kJ/mol) of polar molecules adsorbed on the various solid materials against the temperature. Graphene, Graphene oxide, Reduced graphene oxide, Untreated carbon fibers, and Oxidized carbon fibers.

| -∆GapT (in kJ/mol) |  | Graphene |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| T(K) | Dichloromethane |  | Diethyl ether | THF | Ethyl acetate | Acetone | Acetonitrile |
| 313.15 | 12.938 |  | 21.537 | 20.104 | 22.191 | 25.247 | 32.890 |
| 323.15 | 12.993 |  | 20.456 | 19.156 | 21.658 | 24.461 | 33.199 |
| 333.15 | 13.048 |  | 19.376 | 18.207 | 21.125 | 23.676 | 33.508 |
| 343.15 | 13.102 |  | 18.294 | 17.258 | 20.591 | 22.889 | 33.816 |
| 353.15 | 13.157 |  | 17.214 | 16.310 | 20.057 | 22.104 | 34.125 |
| 363.15 | 13.211 |  | 16.134 | 15.362 | 19.524 | 21.318 | 34.434 |
| 373.15 | 13.265 |  | 15.052 | 14.412 | 18.990 | 20.531 | 34.742 |
| -∆GapT (in kJ/mol) |  | Graphene oxide |  |  |  |  |  |
| T(K) | Dichloromethane |  | Diethyl ether | THF | Ethyl acetate | Acetone | Acetonitrile |
| 313.15 | 2.309 |  | 9.736 | 8.668 | 11.657 | 12.238 | 18.469 |
| 323.15 | 2.749 |  | 9.445 | 8.404 | 11.603 | 12.414 | 19.019 |
| 333.15 | 3.192 |  | 9.157 | 8.143 | 11.552 | 12.592 | 19.571 |
| 343.15 | 3.639 |  | 8.873 | 7.887 | 11.504 | 12.772 | 20.122 |
| 353.15 | 4.082 |  | 8.584 | 7.626 | 11.452 | 12.950 | 20.674 |
| 363.15 | 4.523 |  | 8.294 | 7.363 | 11.400 | 13.127 | 21.225 |
| 373.15 | 4.964 |  | 8.003 | 7.100 | 11.347 | 13.304 | 21.775 |
| -∆GapT (in kJ/mol) |  | Reduced graphene oxide |  |  |  |  |  |
| T(K) | Dichloromethane |  | Diethyl ether | THF | Ethyl acetate | Acetone | Acetonitrile |
| 313.15 | 10.175 |  | 20.953 | 17.327 | 21.696 | 20.831 | 19.905 |
| 323.15 | 10.148 |  | 19.968 | 16.364 | 20.849 | 20.987 | 20.995 |
| 333.15 | 10.123 |  | 18.983 | 15.403 | 20.000 | 21.141 | 22.080 |
| 343.15 | 10.095 |  | 17.995 | 14.438 | 19.151 | 21.296 | 23.168 |
| 353.15 | 10.068 |  | 17.009 | 13.474 | 18.302 | 21.451 | 24.257 |
| 363.15 | 10.042 |  | 16.023 | 12.512 | 17.453 | 21.604 | 25.341 |
| 373.15 | 10.013 |  | 15.035 | 11.547 | 16.604 | 21.758 | 26.429 |
| -∆GapT (in kJ/mol) |  | Untreated carbon fibers |  |  |  |  |  |
| T(K) | Dichloromethane |  | Diethyl ether | THF | Ethyl acetate | Acetone | Chloroform |
| 313.15 | 4.130 |  | 2.133 | 11.809 | 9.471 | 10.681 | 15.339 |
| 323.15 | 3.872 |  | 1.873 | 11.455 | 9.381 | 10.499 | 14.255 |
| 333.15 | 3.614 |  | 1.613 | 11.101 | 9.291 | 10.317 | 13.171 |
| 343.15 | 3.356 |  | 1.353 | 10.747 | 9.201 | 10.135 | 12.087 |
| 353.15 | 3.098 |  | 1.093 | 10.393 | 9.111 | 9.953 | 11.003 |
| 363.15 | 2.840 |  | 0.833 | 10.039 | 9.021 | 9.771 | 9.919 |
| 373.15 | 2.582 |  | 0.573 | 9.685 | 8.931 | 9.589 | 8.835 |
| -∆GapT (in kJ/mol) |  | Oxidized carbon fibers |  |  |  |  |  |
| T(K) | Dichloromethane |  | Diethyl ether | THF | Ethyl acetate | Acetone | Chloroform |
| 313.15 | 10.526 |  | 7.399 | 17.009 | 13.204 | 17.919 | 12.794 |
| 323.15 | 10.235 |  | 7.187 | 16.443 | 12.962 | 17.462 | 12.519 |
| 333.15 | 9.944 |  | 6.975 | 15.877 | 12.720 | 17.005 | 12.244 |
| 343.15 | 9.653 |  | 6.763 | 15.311 | 12.478 | 16.548 | 11.969 |
| 353.15 | 9.362 |  | 6.551 | 14.745 | 12.236 | 16.091 | 11.694 |
| 363.15 | 9.071 |  | 6.339 | 14.179 | 11.994 | 15.634 | 11.419 |
| 373.15 | 8.780 |  | 6.127 | 13.613 | 11.752 | 15.177 | 11.144 |

Table S2. Values of (-∆Hap in kJ mol-1) of polar molecules adsorbed on the different graphene and carbon materials

| Materials | Dichloromethane | Diethyl ether | THF | Ethyl acetate | Acetone | Acetonitrile |
| --- | --- | --- | --- | --- | --- | --- |
| Graphene | 11.234 | 55.379 | 49.808 | 38.894 | 49.855 | 23.224 |
| Graphene oxide | -11.565 | 18.765 | 16.833 | 13.261 | 6.6652 | 1.2085 |
| Reduced graphene oxide | 11.017 | 51.84 | 47.496 | 48.277 | 21.295 | 23.168 |
| Untreated carbon fibers | 12.209 | 49.284 | 10.275 | 22.895 | 12.289 | - |
| Oxidized carbon fibers | 19.639 | 21.406 | 14.038 | 34.733 | 20.782 | - |

Table S3. Values of (-∆Sap in J K-1mol-1) of polar molecules adsorbed on the different graphene and carbon materials

| Materials | Dichloromethane | Diethyl ether | THF | Ethyl acetate | Acetone | Acetonitrile |
| --- | --- | --- | --- | --- | --- | --- |
| Graphene | -5.4 | -44.3 | 2.7 | 25.8 | 29.1 | -5.4 |
| Graphene oxide | 108.1 | 28.8 | 98.6 | 108.4 | 27.5 | 108.1 |
| Reduced graphene oxide | 94.9 | 26.1 | 96.3 | 26.0 | 21.2 | 94.9 |
| Untreated carbon fibers | 53.3 | 5.1 | 84.9 | 35.4 | 56.6 | - |
| Oxidized carbon fibers | 78.6 | -17.8 | -15.4 | 9.0 | 24.2 | - |

Table S4. Values of polar acid-base energies γs+, γs-, γsp, and total surface energy γstot. (in mJ/m2) of the different graphenes and carbon materials at various temperatures.

| Materials | T(K) | 313.15 | 323.15 | 333.15 | 343.15 | 353.15 | 363.15 | 373.15 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Graphene | γs- | 167.08 | 162.07 | 157.32 | 152.79 | 148.51 | 144.41 | 140.52 |
|  | γs+ | 73.55 | 68.61 | 63.95 | 59.53 | 55.36 | 51.42 | 47.70 |
|  | γsp | 221.71 | 210.91 | 200.61 | 190.75 | 181.34 | 172.35 | 163.73 |
|  | γstot. | 500.90 | 472.02 | 443.90 | 416.53 | 389.88 | 363.98 | 338.77 |
| Graphene oxide | γs- | 5.32 | 7.25 | 9.41 | 11.79 | 14.29 | 16.93 | 19.68 |
|  | γs+ | 20.29 | 19.69 | 19.12 | 18.58 | 18.05 | 17.53 | 17.03 |
|  | γsp | 20.78 | 23.91 | 26.84 | 29.60 | 32.12 | 34.45 | 36.61 |
|  | γstot. | 139.0 | 133.2 | 127.4 | 121.7 | 116.1 | 110.5 | 105.0 |
| Reduced graphene oxide | γs- | 103.34 | 98.87 | 94.69 | 90.70 | 86.96 | 83.44 | 80.07 |
|  | γs+ | 70.30 | 63.58 | 57.32 | 51.50 | 46.10 | 41.09 | 36.46 |
|  | γsp | 170.47 | 158.57 | 147.35 | 136.69 | 126.62 | 117.11 | 108.06 |
|  | γstot. | 321.4 | 305.8 | 290.7 | 275.9 | 261.6 | 247.4 | 233.5 |
| Untreated carbon fibers | γs- | 17.03 | 14.39 | 12.07 | 10.02 | 8.23 | 6.67 | 5.32 |
|  | γs+ | 13.40 | 12.87 | 12.37 | 11.89 | 11.42 | 10.98 | 10.55 |
|  | γsp | 30.20 | 27.22 | 24.44 | 21.83 | 19.40 | 17.12 | 14.99 |
|  | γstot. | 86.5 | 80.2 | 74.4 | 68.5 | 62.9 | 58.2 | 53.9 |
| Oxide carbon fibers | γs- | 110.59 | 100.57 | 91.37 | 82.93 | 75.19 | 68.08 | 61.56 |
|  | γs+ | 26.04 | 24.58 | 23.19 | 21.86 | 20.60 | 19.41 | 18.27 |
|  | γsp | 107.33 | 99.43 | 92.06 | 85.16 | 78.72 | 72.70 | 67.07 |
|  | γstot. | 163.2 | 151.0 | 139.4 | 128.4 | 117.9 | 107.9 | 98.4 |