Supplementary Information

Review - Safety aspects of sodium-ion batteries: Prospective analysis from 1st generation towards more advanced systems

Pempa Tshering Bhutia1,2,3,4, Sylvie Grugeon2,3, Asmae El Mejdoubi5, Stéphane Laruelle2,3, Guy Marlair1,*

1Institut National de l’Environnement Industriel et des Risques (INERIS), Parc Technologique Alata, BP2, 60550 Verneuil-en-Halatte, France

2Laboratoire de Réactivité et Chimie des Solides, CNRS UMR 7314, Université de Picardie Jules Verne, Amiens 80039, France

3RS2E, Réseau Français sur le Stockage Electrochimique de l’Energie, FR CNRS 3459, CEDEX 1, F-80039 Amiens, France

4Alistore-European Research Institute (ERI), FR CNRS 3104, F-80039 Amiens Cedex 1, France

5TIAMAT, 72 rue des Jacobins, 80000 Amiens, France

*Corresponding author: Guy.MARLAIR@ineris.fr

Table S1: Theoretical and Practical capacity of selected materials reported in main paper

| Materials | Theoretical capacity (mAh/g) | Practical capacity (mAh/g) | Sources |
| --- | --- | --- | --- |
| Cathode: |  |  |  |
| LiCoO2 | 274 | 140-170 typically, 190 (dopants) | [1] |
| LiNiO2 | 275 | 180-200 typically, 232 (Best performance) | [2] |
| LiMnO2 | 285 | 210 | [3] |
| LiNi0.33Mn0.33Co0.33O2 | 280 | 164 | [4] |
| LiMn2O4 | 148 | 140 | [5] |
| LiFePO4 | 170 | 192 (modified LFP-microrods/multi-walled carbon nanotube) | [6] |
| Na3V2(PO4)2 | 128 | 120 | [7] |
| NaFeO2 | 242 | 103 | [8] |
| Na2FeP2O7 | 97 | 90 | [9] |
| Na3.32Fe2.11Ca0.23(P2O7)2 | 148 | 100 | [10] |
| Na0.69CoO2 | 173 | 147 (Na0.12CoO2), 116 (Na0.24CoO2), 49 (Na0.52CoO2) | [11] |
| Na0.44MnO2 | 121 | 108 | [12] |
| NaNi0.33Fe0.33Mn0.33O2 | 282 | 165 | [13] |
| Na0.9[Cu0.22Fe0.30Mn0.48]O2 | 220 | 100 | [14] |
| Na[Ni0.6Co0.2Mn0.2]O2 | 276 | 153 | [15] |
| Anode: |  |  |  |
| Graphite | 372 | 348 | [16] |
| Li4Ti5O12 | 175 | 160 | [17] |
| Hard carbon | Precursors dependent | 361 | [18] |

Table S2: Selected commercial (start-ups) level sodium-ion batteries

| Company | Active Materials |
| --- | --- |
| Contemporary Amperex Technology Co., Ltd. (CATL) | Prussian blue analog material¦¦HC |
| Faradion Limited | Layered oxide materials¦¦HC |
| HiNa Battery Technology Co., Ltd. | NaCu1-y-zFeyMnzO2¦¦HC |
| Natron Energy | Prussian blue analog material¦¦HC |
| TIAMAT | Polyanionic material ¦¦ HC |
| Novasis Energies | Prussian blue analog material¦¦HC |
| Altris AB | Prussian blue analog material¦¦HC |
| Aquion Energy | Mn-oxide intercalation cathode¦¦High-capacity activated anode |

References:

1. 	Liu, Q.; Su, X.; Lei, D.; Qin, Y.; Wen, J.; Guo, F.; Wu, Y.A.; Rong, Y.; Kou, R.; Xiao, X.; et al. Approaching the Capacity Limit of Lithium Cobalt Oxide in Lithium Ion Batteries via Lanthanum and Aluminium Doping. Nat Energy 2018, 3, 936–943, doi:10.1038/s41560-018-0180-6.

2. 	Välikangas, J.; Laine, P.; Hietaniemi, M.; Hu, T.; Tynjälä, P.; Lassi, U. Precipitation and Calcination of High-Capacity LiNiO2 Cathode Material for Lithium-Ion Batteries. Applied Sciences 2020, 10, 8988, doi:10.3390/app10248988.

3. 	Myung, S.-T.; Komaba, S.; Kumagai, N. Orthorhombic LiMnO2 as a High Capacity Cathode for Lithium-Ion Battery Synthesized by Hydrothermal Route at 170 °C. Chemistry Letters 2001, 30, 80–81, doi:10.1246/cl.2001.80.

4. 	Wagner, A.C.; Bohn, N.; Geßwein, H.; Neumann, M.; Osenberg, M.; Hilger, A.; Manke, I.; Schmidt, V.; Binder, J.R. Hierarchical Structuring of NMC111-Cathode Materials in Lithium-Ion Batteries: An In-Depth Study on the Influence of Primary and Secondary Particle Sizes on Electrochemical Performance. ACS Appl. Energy Mater. 2020, 3, 12565–12574, doi:10.1021/acsaem.0c02494.

5. 	Taddesse, P.; Gebrekiros, H.; Semu, G.; Duressa, M.; Chemeda, Y.C.; Murali, N.; Babu, K.V. Investigation of Structural, Vibrational Spectroscopic and Properties Study of LiMn2O4 and LiMn1.9Cu0.05Fe0.05O4 Cathode Materials. Results in Materials 2021, 12, 100224, doi:10.1016/j.rinma.2021.100224.

6. 	Kanagaraj, A.B.; Chaturvedi, P.; Kim, H.J.; Choi, D.S. Controllable Synthesis of LiFePO4 Microrods and Its Superior Electrochemical Performance. Materials Letters 2021, 283, 128737, doi:10.1016/j.matlet.2020.128737.

7. 	Desai, P.; Forero-Saboya, J.; Meunier, V.; Rousse, G.; Deschamps, M.; Abakumov, A.M.; Tarascon, J.-M.; Mariyappan, S. Mastering the Synergy between Na3V2(PO4)2F3 Electrode and Electrolyte: A Must for Na-Ion Cells. Energy Storage Materials 2023, 57, 102–117, doi:10.1016/j.ensm.2023.02.004.

8. 	Zhao, J.; Zhao, L.; Dimov, N.; Okada, S.; Nishida, T. Electrochemical and Thermal Properties of α-NaFeO 2 Cathode for Na-Ion Batteries. J. Electrochem. Soc. 2013, 160, A3077–A3081, doi:10.1149/2.007305jes.

9. 	Barpanda, P.; Liu, G.; Ling, C.D.; Tamaru, M.; Avdeev, M.; Chung, S.-C.; Yamada, Y.; Yamada, A. Na 2 FeP 2 O 7 : A Safe Cathode for Rechargeable Sodium-Ion Batteries. Chem. Mater. 2013, 25, 3480–3487, doi:10.1021/cm401657c.

10. 	Liu, Y.; Wu, Z.; Indris, S.; Hua, W.; Casati, N.P.M.; Tayal, A.; Darma, M.S.D.; Wang, G.; Liu, Y.; Wu, C.; et al. The Structural Origin of Enhanced Stability of Na3.32Fe2.11Ca0.23(P2O7)2 Cathode for Na-Ion Batteries. Nano Energy 2021, 79, 105417, doi:10.1016/j.nanoen.2020.105417.

11. 	Hwang, S.; Lee, Y.; Jo, E.; Chung, K.Y.; Choi, W.; Kim, S.M.; Chang, W. Investigation of Thermal Stability of P2–Na  x  CoO 2 Cathode Materials for Sodium Ion Batteries Using Real-Time Electron Microscopy. ACS Appl. Mater. Interfaces 2017, 9, 18883–18888, doi:10.1021/acsami.7b04478.

12. 	Feng, J.; An, Y.; Ci, L.; Xiong, S. Nonflammable Electrolyte for Safer Non-Aqueous Sodium Batteries. J. Mater. Chem. A 2015, 3, 14539–14544, doi:10.1039/C5TA03548A.

13. 	Xie, Y.; Xu, G.-L.; Che, H.; Wang, H.; Yang, K.; Yang, X.; Guo, F.; Ren, Y.; Chen, Z.; Amine, K.; et al. Probing Thermal and Chemical Stability of Na  x  Ni 1/3 Fe 1/3 Mn 1/3 O 2 Cathode Material toward Safe Sodium-Ion Batteries. Chem. Mater. 2018, 30, 4909–4918, doi:10.1021/acs.chemmater.8b00047.

14. 	Li, Y.; Hu, Y.-S.; Qi, X.; Rong, X.; Li, H.; Huang, X.; Chen, L. Advanced Sodium-Ion Batteries Using Superior Low Cost Pyrolyzed Anthracite Anode: Towards Practical Applications. Energy Storage Materials 2016, 5, 191–197, doi:10.1016/j.ensm.2016.07.006.

15. 	Hwang, J.-Y.; Myung, S.-T.; Choi, J.U.; Yoon, C.S.; Yashiro, H.; Sun, Y.-K. Resolving the Degradation Pathways of the O3-Type Layered Oxide Cathode Surface through the Nano-Scale Aluminum Oxide Coating for High-Energy Density Sodium-Ion Batteries. J. Mater. Chem. A 2017, 5, 23671–23680, doi:10.1039/C7TA08443A.

16. 	Endo, K.; Zhang, H.P.; Fu, L.J.; Lee, K.J.; Sekine, K.; Takamura, T.; Jeong, Y.U.; Wu, Y.P.; Holze, R.; Wu, H.Q. Electrochemical Performance of a Novel Surface Modified Spherical Graphite as Anode Material for Lithium Ion Batteries. J Appl Electrochem 2006, 36, 1307–1310, doi:10.1007/s10800-006-9177-0.

17. 	Shu, J. Electrochemical Behavior and Stability of Li4Ti5O12 in a Broad Voltage Window. J Solid State Electrochem 2009, 13, 1535–1539, doi:10.1007/s10008-008-0723-z.

18. 	Xiao, L.; Lu, H.; Fang, Y.; Sushko, M.L.; Cao, Y.; Ai, X.; Yang, H.; Liu, J. Low‐Defect and Low‐Porosity Hard Carbon with High Coulombic Efficiency and High Capacity for Practical Sodium Ion Battery Anode. Advanced Energy Materials 2018, 8, 1703238, doi:10.1002/aenm.201703238.